# Growth of moulds on building materials

# Secondary metabolites, mycotoxins and biomarkers

# Kristian Fog Nielsen

The Mycology Group

Biocentrum-DTU

# Technical University of Denmark

# Lyngby 2001

Preface

# More than seven ago years ago I was introduced to the fascinating world of fungi and mycotoxins by Ole Filtenborg and Thomas O. Larsen. The opportunity to work on my own with an array of sophisticated equipment, made me stay in the Mycology Group, and lead to my M.Sc. project where Suzanne Gravesen and Thomas convinced me to work on satratoxins in buildings. Successfully ending this work, lead to my Ph.D. project financed by the Danish Building Research Institute where Erik Christophersen organised the founds for the project as well as the many travels.

# However, it has also been frustrating to work in a field where you are unable to help people, often of lower social rank, who are forced to move from their mouldy homes due to massive symptoms and the ignorance of the authorities.

Working in such a multidisciplinary area requires help from a lot of people, and at the Danish Building Research Institute I would like to thank the librarians, especially Lillian Nielsen who have been a tremendous help in ordering scientific papers. Gunnar Holm has been a great help in constructing experimental set-ups, Lotte P. Uttrup and Per Hansen have prepared material samples, Jan Carl Westphall helped with various photographic problems, and Solveig Nissen with the language revision of some of the papers as well as this thesis. Peter A. Nielsen is acknowledged for the frightful discussions on health and building related issues.

The help of Jørgen Ø. Madsen, Department of Organic Chemistry, in preparing the 4-D2-ergosterol was a great help in making the ergosterol analytical method work.

The private consultants Mikael Ø. Hansen and Peter Thompson have kindly me with supplied "real" mouldy materials, interesting field observations, and taking their time to show me the real mouldy world outside the laboratories.

I would like to thank Dr. Aino Nevalainen, Dr. Maija-Riitta Hirvonen, and their helpful Ph.D. students for letting me work in their laboratories at the National Public Health Institute, Kuopio, Finland.

Working at TNO Bouw, The Netherlands, with Dr. Olaf Adan and Gerben van den Wel helped me understand the importance of instationary environmental conditions on mould growth.

Having Professor Bruce B. Jarvis in our group for a year raised the level of my work on Stachybotrys and natural products significantly and introduced me to a number of other research groups.

The help of colleagues in the Mycology group, in particular Elisabeth Krøger, Kir, Flemming Lung, Thomas O. Larsen, Jørn Smedsgaard, Jens C. Frisvad and Birgitte Andersen has been encouraging. Ulf Thrane has been the perfect Ph.D. supervisor who always had time - if needed, and on the other hand never intervened much in my work.

# Thanks to Suzanne Gravesen who believed so much in my work and have taught me so much about so many different things and introduced me to so many people as well as helping with the language revision of this report.

# The support and understanding of my beloved wife Hanne - especially during my stays in Finland, Holland and various conference as well as the acceptance of the large piles of papers, CD, books etc. during my project cannot be underestimated.

# Lyngby, June 2001

# Kristian Fog Nielsen

Abstract

Mould growth in buildings is causing various health effects among the occupants, however the causal components is still partly unknown making scientifically based guidelines for "how much too much" and cost efficient remediation of mould buildings impossible.

The aim of this study was to document if the moulds produce mycotoxins and other biologically active metabolite when growing in buildings as well as investigate the influence of environmental conditions on the production of these metabolites. The growth of moulds under various humidities should also be investigated along with the use of chemical biomarkers for quantitation of mould growth.

It was shown that Stachybotrys chartarum produced a number of mycotoxins when growing in buildings. These components were produced in significant higher quantities than by other moulds investigated in this study. Only 35% of the isolates from buildings produced the extremely cytotoxic satratoxins, and these metabolites are probably not responsible for idiopathic pulmonary hemasiderosis in infants, which is associated with S. chartarum.

For the first time ever Stachybotrys metabolites were found in air-samples where several classes of spiriocyclic drimanes and satratoxins were detected.

Aspergillus versicolor produced high quantities of the carcinogenic mycotoxin, sterigmatocystin at water activities (aw) > 0.95. At lower aw more than 10 unknown metabolites were produced, including at least 5 metabolites also produced by A. ochraceus. A. versicolor was often growing in mixed cultures with others moulds where it sporulate poor, meaning that it may evade detection based on cultivating methods.

Penicillium chrysogenum produced surprisingly few detectable metabolites and often none when growing on materials. Combined with the no observed effects on human experimentally exposed to high quantities of the spores these observations implies that this species may not be important is actually obscuring the detection of more toxic genera and species.

On water-damaged materials Chaetomium globosum produced high quantities of chaetoglobosins, whereas P. brevicompactum produced mycophenolic acid and P. polonicum the tremorgenic verrucosidin. The A. ustus isolates from buildings were macro-morphologically and chemically very different than cereal isolates, and should be described as a new species.

Trichoderma T. longibrachiatum, T. harzianum, T. citrinoviride, T. atroviride, T. viride did not produce detectable quantities of trichothecenes when growing on materials, and even on laboratory media <1% of the isolates produced trichodermol or esters of it.

The minimal RH for growth on wood based materials and material containing starch was just below 80% at room temperature, and increased to about 90% at 5°C. On paper-mineral composites such as gypsumboard the minimal RH was approx. 90% RH from room temperature to 5°C. Pure mineral based materials with few organic additives seems to be able to support growth at RH ≥ 0.90, although 95% RH was needed to generate chemical detectable quantities of biomass.

The phylloplane Cladosporium was able to outgrow P. chrysogenum on materials under transient humidities. This is presumably why phylloplanes like Cladosporium, Ulocladium, Phoma and Aurabasidium are very common i bathrooms and other places with instationary humidity conditions.

Ergosterol content of building materials was quickly and precisely quantified (60-100 samples per day) by isotope dilution GC-MS/MS, but is only needed as a supplemented for assessing mould growth on test materials, as visual assessment, especially supported by dissection microscopy generally was just as sensitive.

Resume

Skimmelsvampevækst i bygninger er sundhedsskadeligt, med en del af de aktive stoffer om mekanismer en endnu ukendte. Derfor er det ikke muligt at fastsætte præcise grænseværdier for mængde af skimmelsvamp i bygninger ligesom det ikke er muligt at renovere angrebne bygninger økonomisk effektivt.

Målet med dette studium var at dokumentere om skimmelsvampe producere mykotoksiner  og andre biologisk aktive stoffer, når de vokser på byggematerialer. Anvendelse af kemiske markører til kvantificering af den producerede biomasse skulle også undersøges sammen med svampenes vækst og metabolisme under forskellige temperatur- og fugtforhold.

Stachybotrys chartarum producerede en række mykotoksiner når den voksede på byggematerialer og at mængderne af disse stoffer, der blev frigjort ved en let vakuum opsamling, var klart større end de mængder der blev produceret af andre skimmelsvampe. Kun 35% af isolater fra vandskadede bygninger producerede de celledræbende satratoxiner, og produktionen af disse synes ikke at årsagen lungeblødninger i spædbørn der er associeret til Stachybotrys.

For første gang blev Stachybotrys metabolitter fundet i luftprøver. Her blev flere typer af spiriocykliske drimaner samt satratoxiner påvist.

Aspergillus versicolor producerede meget store mængder af de kræftfremkaldende sterigmatocystiner når vandaktiviteten (aw) > 0.95, hvorimod den ved lavere aw i stedet producerer mindst 10 ukendte metabolitter, hvoraf 5 tidligere er set i kulturekstrakter fra A. ochraceus.

A. versicolor gror oftest i blandede kulture med mange andre svampe, og da den sporulerer dårligt vil den oftest ikke blive påvist ved dyrknings på vækstmedier.

Penicillium chrysogenum producerer stort sent ingen påviselige metabolitter når den gror på byggematerialer. Sammenholdt med de manglende humane effekter efter eksponering for meget store mængder luftbårne sporer indikerer det, at den ikke har så stor sundhedsmæssig relevans og i stedet forhindrer påvisning af mere sundhedsrelevante arter.

På vandskadede materialer producerede Chaetomium globosum store mængder af de toksiske chaetoglobosiner. P. brevicompactum producerede mycophenolsyre og P. polonicum det tremorgene verrucosidin. A. ustus isolater fra bygninger var både kemisk og makro-morfologisk forskellige fra stammer isoleret fra korn og bør derfor beskrives som en ny art.

Trichoderma spp. producerede ikke påviselige mængder trichothecener når de voksede på byggematerialer. På laboratoriesubstrater producerede <1% trichodermol eller estre af denne.

Den minimale relative fugtighed (RH) for at der kan opstå vækst af skimmelsvampe ligger lige under 80% ved stuetemperatur og stiger til ca. 90% RH ved 5°C. På gipsplader kræver skimmelsvampene ca. 90% RH for at kunne vokse. Beton med nogle organiske additiver kan tilsyneladende give anledning til meget minimal vækst ved RH > 90% og ved RH > 95% kan der blive produceret ikke ubetydelige mængder biomasse på dette materiale.

Den phylloplane Cladosporium kan udkonkurrere P. chrysogenum på materialer under transiente fugtforhold, og det er sandsynligvis årsagen til at phylloplaner som Cladosporium, Ulocladium, Phoma og Aureobasidium dominere i badeværelser og andre steder, hvor der er transiente fugtforhold.

Ergosterol-indholdet i materialer kunne hurtigt og præcist blive kvantificeret (60-100 prøver pr. dag) med isotop fortynding GC-MS/MS. Dette er kun nødvendigt som et supplement til bestemmelse af biomasse på testmaterialer, idet visuel bestemmelse kombineret med stereomikroskopi generelt er lige så følsomt.

# Table of Contents

Preface	i

Abstract	ii

Resume	iii

Abbreviations and terms	vi

Papers included in this thesis	viii

1	Introduction	1

2	Moulds in buildings	3

1.1.1	The building associated funga	3

1.2	Growth of moulds on building materials	5

1.1.1	"Water - the key factor"11	5

1.1.2	The impact of the material on the mould growth	8

1.1.3	Modelling mould growth on materials	8

1.3	Health problems associated with airborne moulds	9

1.3.1	In vivo and in vitro effect of fungal spores	9

1.1.2	Epidemiologically studies	10

1.4	Biologically active metabolites from moulds	12

1.4.1	Stachybotrys	13

1.1.2	Aspergillus	17

1.1.3	Penicillium	20

1.1.4	Trichoderma	22

1.1.5	Memnoniella	22

1.1.6	Alternaria	22

1.1.7	Chaetomium	23

1.1.8	Cladosporium	23

1.1.9	Ulocladium	23

1.1.10	Paecilomyces	24

1.5	Biomarkers of mould growth	24

1.1.1	Ergosterol	24

1.6	Detection of fungal metabolites	25

1.6.1	Chromatographic methods for detection of mycotoxins	25

1.1.2	Sample preparation	28

1.1.3	Detection of mycotoxins in air and settled dust	28

3	Overview of experimental work	30

4	Results and discussion	31

4.1	The building associated funga	31

4.1.1	Penicillium and Aspergillus cultures received from Finland	31

4.2	Fungal growth on materials	32

1.1.1	Methods for testing the susceptibility of materials	33

1.1.2	Growth assesment	34

1.3	Growth and metabolite production	36

1.3.1	Stachybotrys	36

1.1.2	Aspergillus	44

1.1.3	Penicillium	49

1.1.4	Trichoderma	51

1.1.5	Memnoniella echinata	51

1.1.6	Alternaria	52

1.1.7	Chaetomium globosum	52

1.1.8	Cladosporium	53

1.1.9	Ulocladium	54

1.1.10	Paecilomyces	54

1.1.11	Eurotium	55

1.4	Overall discussion	55

1.4.1	Growth on materials	55

1.4.2	Metabolites	56

5	Conclusion	58

6	Perspectives and future research	60

References	61

Papers 1-13

Appendix A, list of conference proceedings

Appendix B, Review of metabolite data from the examined species

# Abbreviations and terms

AFB1	Aflatoxin B1

ALK	Alkaloid forming agar

Antibiotic	Activity against microorganisms, usually against bacteria

aw	Water activity

CE	Capillary electrophoresis

CFU	Colony forming unit

Conidia	Asexual production structure from fungi /moulds.

CYA	Czapek yeast extract agar

DAD	Diode array detection

DAS	Diacetoxyscirpentriol, a type A trichothecene

DG18  	Dichloran 18% glycerol agar

DON	Deoxynivalenol, a type B trichothecene

EI+	Positive ion, electron impact ionisation

ESI	Electrospray ionisation, method used extensively in LC-MS

FLD	Fluorescence detection

GC	Gas chromatography

HFB	Heptafluorobuturyl, derivative-group -CO-CF2-CF2-CF3.

HPLC	High performance liquid chromatography, also referred to as LC

IL-1	Interleukin 1, a cytokine

IL-6	Interleukin 6, a cytokine

IPH	Idiopathic pulmonary hemosiderosis

LC	Liquid chromatography

LC50	Concentration lethal to 50% of the test organisms

LD50	Dose lethal to 50% of the test organisms

MEA	Malt extract agar

MS	Mass spectrometry

MS/MS	Tandem mass spectrometry

MTR	Macrocyclic trichothecene

MVOC	Microbial volatile organic compound

NICI 	Negative ion chemical ionisation

NIV	Nivalenol, a type B trichothecene

NO	Nitrogen oxide, as inflammatory mediator

OAT	Oatmeal agar

PCR	Polymerase chain reaction

PFP	Pentafluoropropionyl, derivative group, -CO-CF2-CF3.

PSA	Potato sucrose agar

RE	Roridin E, a macrocyclic trichothecene

RH	Relative humidity (%)

RI	Retention index

RT	Retention time

ROS 	Reactive oxygen species

SG	Satratoxin G, a macrocyclic trichothecene

SH	Satratoxin H, a macrocyclic trichothecene

SPE	Solid phase extraction, chemical clean-up method

Spore	Reproductive structure of fungi/moulds and certain bacteria

ST 	Sterigmatocystin

5ST	5-methoxysterigmatocystin

T-2	T-2 toxin, a type a trichothecene

TA	Type A trichothecene

TB	Type B trichothecene

TFA	Trifluoroacetic acid

TLC	Thin layer chromatography

TMS	Trimethylsilyl, derivative group, -Si(CH3)3

TNF(	Tumor necrosis factor (, a cytokine

TR	Trichothecene

V8	V8 juice agar

VB	Verrucarin B, a macrocyclic trichothecene

VJ	Verrucarin J, a macrocyclic trichothecene

Water-damaged	Floating water present, aw ≈ 1

WP	Wallpaper

YES	Yeast extract sucrose agar

# Papers included in this thesis

- Nielsen KF, Hansen MØ, Larsen TO, Thrane U. 1998. Production of trichothecene mycotoxins on water damaged gypsum boards in Danish buildings.  International Biodeterioration & Biodegradation 42:1-7.

- Nielsen KF, Thrane U, Larsen TO, Nielsen PA, Gravesen S. 1998. Production of mycotoxins on artificially inoculated building materials.  International Biodeterioration & Biodegradation 42:8-17.

- Nielsen, KF, Gravesen S, Nielsen PA, Andersen B, Thrane, Frisvad JC. 1999. Production of mycotoxins on artificially and naturally infested building materials.  Mycopathologia 145:43-56.

- Gravesen S, Nielsen PA, Iversen R, Nielsen KF. 1999. Microfungal contamination of damp buildings - examples of risk constructions and risk materials.  Environmental Health Perspectives 107, Supplement 3:505-508.

- Nielsen, KF, Madsen JØ. 2000. Determination of ergosterol on mouldy building materials using isotope dilution and gas chromatography - tandem mass spectrometry. Journal of Chromatography A 898: 227-234.

- Andersen B, Nielsen, KF, Jarvis BB. Characterization of Stachybotrys from water-damaged buildings based on morphology, growth and metabolite production. Mycologia (submitted).

- Peltola J, Niessen L, Nielsen KF, Jarvis BB, Salkinoja-Salonen M, Möller E. Genetic diversity of Stachybotrys chartarum and relatedness to toxicity (to be submitted).

- Nielsen KF, Thrane U. A fast method for screening of trichothecenes in fungal cultures – using gas chromatography - tandem mass spectrometry. Journal of Chromatography A. (submitted)

- Nielsen KF, Huttunen K, Andersen B, Jarvis BB, Hyvärinen A, Hirvonen M-R. Relationship between metabolite profiles of Stachybotrys isolates from water-damaged buildings and their induction of inflammatory mediators and cytotoxicity in macrophages. Mycopathologia (submitted).

- Nielsen, KF, Nielsen PA, Holm G, Uttrup LP. Mould growth and metabolism on building materials under different humidities and temperatures. (to be submitted)

- Wilkins KC, Nielsen KF, Din SL. Patterns of volatile metabolites and trichothecenes produced by Stachybotrys and other trichothecene producing molds. Environmental Science & Pollution Research. (submitted)

- Reelsev M, Nielsen, KF. Mycometer test and ergosterol for determination of fungal biomass on mouldy building materials. (in prep)

- van Wel G, Nielsen KF, Adan O. Mould growth and metabolism on building materials under constant and transient humidities. (in prep)

Appendix A lists the conference proceedings and non peer-reviewed publications prepared during this Ph.D. thesis.

# Introduction

During the last 10 years several studies have shown that people living and working in damp or mouldy buildings have an increased risk of airways infections, adverse health effects, respiratory problems such as asthma, and CNS symptoms1-9. However concern of mould growth in buildings is not a new problem, already in the Bible (Leviticus Chapter 14, 33-48) it is written that contaminated spots on walls should be removed, and if consistently reappearing the house should be torn down.

The estimated proportion of dwellings with microfungal problems in Northern Europe and North America is perhaps as high as 20-40% based on data from the United Kingdom with 30-45%1,10, the Netherlands with 20-25%6,11,12, Finland with 20-30%9,13, USA with up to 40%2 and Canada with up to 30%3 buildings affected. No data exist for dwellings in Denmark, but the majority of schools and day-care centres build in the late 1960s and 1970s seem to have problems.

Mould growth only occurs in water-damaged and humid constructions. Consequently the major part of the problems in Scandinavia and North America are due to poorly manufactured constructions and inadequate maintenance14-16.

The health problems observed in mouldy or damp buildings can be grouped into three major categories as seen in ¡Error! Argumento de modificador desconocido..

| Table ¡Error! Argumento de modificador desconocido. Health problems associated to mouldy and damp buildings |
| --- |
| General symptoms incl. CNS-symptoms | Mucosal symptoms | Lung symptoms |
| Extreme fatigue7,8,17-20. Lack of concentration and memory7,8,17-20, in extreme cases as cognitive impairment21. Nausea1,7,8,17,18 Lowered immune function due to a misbalance in the lymphocytes sub-populations or chronic stimulation of some of the these22,23. | Blocked nose.1,5,12,19 Itching eyes19,24,25 Burning sensation of the skin7,8,17,18,24,25 Hoarseness.1,7,8,17,18 Recurrent airway infections, especially sinusitis7,8,17,18,24,25. | Wheeze1,2,4 Cough2,3,5,6,8,12 Bronchitis2,3 Asthma2,4,6,8 Pulmonary hemosiderosis in infants26-28. |

To cope effectively with the health problems it is essential to identify the causative agents and the cellular mechanisms as it would lead to:

- Clinically valid analyses documenting the patients' complaints.

- Targeted analysis of causative compounds in buildings suspected of having mould problems

- Consent guidelines for "how much is too much".

- Economically sound cleaning procedures.

However, very little knowledge have been established on peoples' specific exposures and the non-immunologic mechanisms, especially toxic reactions, after exposure to moulds8,29,30. Non-immune mediated chronic activation of immune competent cells22,30,31 have been suggested as the major mechanisms.

From the agricultural occupational environment exposure-effect data exist. Here inhalation of fungal metabolites (mycotoxins) have been shown to cause cancer32,33, premature birth34 and farmers lung25. However the levels of spores and metabolites are magnitudes higher than in indoor air35,36.

A number of potentially causative agents produced by moulds in the water-damaged buildings have been suggested:

- Proteins causing the well-known immediate allergic reactions within minutes of exposure (Type I allergy) 24,25,37 and in rare incidences type III allergy25.

- (-(1,3)-d-glucans triggering inflammatory reactions very similar to symptoms observed on exposure to endotoxin38-40.

- Microbial volatile organic compounds (MVOCs) released from the fungi during growth41-44.

- Mycotoxins released from fungal spores and fragments after inhalation19,41,45-52.

Compounds from other organisms associated with moulds such as mites6,53 and bacteria54-59 should also be considered as they may play an important role in the ecosystem of the infested materials. Additional bacteria growing on building materials also produces a number of very potent bacterial toxins60.

The work carried out during the study and this report, focused on the secondary metabolites and mycotoxins produced by moulds during growth on building materials, as these metabolites are potential risk factors for the adverse health effects observed in mouldy buildings.

Consequently, a major part of the following literature review will focus on fungal growth on materials and the different metabolites produced by moulds during their growth in buildings.

# Moulds in buildings

Viable mould spores and bacteria are ubiquitous in buildings10,61 and are well adapted to inhabit this ecological niche if just sufficient water is available10,61-64.

The moulds growing on a particular material is referred to as the associated funga65, and have been divided into three groups by Grand et al61 following their water requirements on laboratory substrates:

- Primary colonisers capable of growth below a water activity (aw) of 0.8 including species of Wallemia, Penicillium, Aspergillus and Eurotium66.

- Secondary colonisers, with a minimal aw between 0.8 and 0.9 including species of the phylloplanes: Cladosporium, Phoma, Ulocladium and Alternaria.

- Tertiary colonisers, demanding aw of at least 0.9, including genera such as: Stachybotrys, Chaetomium, Trichoderma, Auraeobasidium41,67 as well as actinomycetes and other bacteria64,68. These conditions are generally only met by incoming water and not just high humidity or condensation on indoor surfaces25,61.

### The building associated funga

The associated funga reported from different countries varies considerable for a number of reasons, such as different climates, materials, different isolation procedures and difficulties in identifying the isolates to species level especially in Penicillium, Aspergillus and Cladosporium66,69-71. In Table 1, the most common fungal species isolated in have been compiled.

# In Europe, P. chrysogenum is the most abundant66,70,72, whereas is seems to be Penicillium aurantiogriseum and P. viridicatum in North America. However, this is probably due to misidentification with other species from the P. aurantiogriseum complex.

# For the genus Aspergillus consensus seems to exists with A. versicolor being the absolutely most frequently isolated species, followed by A. sydowii and A. ustus70,71.

| Table ¡Error! Argumento de modificador desconocido. The most common part of the building associated funga* |
| --- |
| Genus | Species | Natural habitat | Common on |
| Water damage moulds |
| Chaetomium | globosum | Soil, straw, wood | Mostly on wood and cellulose containing materials |
| Stachybotrys | chartarum | Hay and straw73, paper, soil | Gypsum boards, pipe insulation |
| Ulocladium | chartarum and atrum | Soil, dung, grasses | Wood, wallpaper, gypsum boards |
| Trichoderma | harzianum, citrinoviride, atroviride and longibrachiatum | Wet wood, soil | Mostly on wood |
| Alternaria | tenuissima | Saprophyte on plants, foods Cereals, leaves | Wallpaper, gypsum |
| Aureobasidium | pullulans | Soil, leaves, cereals | Paint especially in bathrooms, window frames, paint |
| Rhodulotorula | rubra |  | Paints, wood |
| Phoma | sp. | Plant material, soil, | Paints, wood, wall papers, caulkings, especially in bathrooms |
| High relative humidity moulds |
| Aspergillus | versicolor | Cheese, cereals, spices, dried meat products | Most materials, primary coloniser, grows in dust |
| Penicillium | chrysogenum | Various foods, spices, dry cereals | All materials |
| Penicillium | brevicompactum | Soil, nuts, fruits and juices | Especially wooden materials |
| Penicillium | corylophilum | Various foods | Most materials, primary coloniser |
| Aspergillus | Sydowii | Soil, cotton, beans, nuts and straw | Most materials, primary coloniser |
| Aspergillus | ustus | Soil, cereals, groundnuts |  |
| Cladosporium | sphaerospermum | Dead plans | Paints, wood, wall papers, caulkings, especially in bathrooms |
| Cladosporium | herbarum | Dead plans, stored fruits | Paints, wood, wall papers, caulkings, especially in bathrooms |
| Penicillium | palitans | Cheese, wood | Most materials, but especially wooden |
| Eurotium | repens | Cakes, dried food, cereals |  |
| Wallemia | sebi | Dried foods, jam, cakes, dates, salted fish, sugar, chocolate |  |
| Paecilomyces | variotii | Compost |  |
| Penicillium | polonicum | Cereals, meat products |  |
| Aspergillus | niger | Dried food, spices |  |
| Penicillium | expansum | Nuts, fruits (apples) | Wood |

*References14,16,41,52,66,70,72,74,74-79

When measuring viable fungi, as colony-forming units (CFU), the laboratory media will always favour certain genera and species72, thus several media are needed for covering the majority of the building associated funga. Dichloran 18% glycerol agar (DG18) is generally considered the best media for xerophilic fungi (moulds who can grow aw <0.8580), and low nutrient high aw media as V8 juice agar (V8), malt extract agar (MEA) or rose Bengal agar81-83 for the secondary and tertiary colonisers84. However MEA can be supplemented with cellulose agar to enhance detection of Stachybotrys who have difficulties competing with species of Aspergillus and Penicillium as well as having many sterile spores52,85.

#### Air measurements

For investigating moulds associated health problems, air measurements would provide the best exposure data. However, as the causal agents have not been identified, it has not been established what should actually be measured. Four main techniques are used for air measurements: i) cultivation of viable spores; ii) collecting spores and counting them microscopically86; iii) detecting chemical markers87,88; iv) using different molecular-biological (DNA) techniques89. In sections ¡Error! Argumento de modificador desconocido. and ¡Error! Argumento de modificador desconocido. measurements of biomarkers, including mycotoxins, will be dealt with in detail.

A major problem with cultivating techniques is that a major part of the spores may not be viable90. In addition, hyphal and spore fragments are also released from the mouldy materials91. Aggressive air sampling methods are generally preferred over sedimentation plates who are unreliable 41,66,84.

Even in rooms with visible mould growth aggressive sampling may give low counts92-94 although other authors have found clear relationships10. Especially if the ratio between outdoors and indoors is used and speciation of the collected moulds is performed, a clear relationship between infested areas and air measurements can be found14. Determining the ratio of Penicillium and Aspergillus versus outdoors phylloplane moulds as Cladosporium and Alternaria has been successful for indicating a humid environment41,94,95.

A totally different and very elegant approach, is to measures the personal exposure and response by determining inflammatory mediators, such as IL-1, IL-6, TNFα, NO, eosinophil cationic protein and myeloperoxidase in nasal lavage fluid96-98.

Nevertheless interpretation and knowledge of the limitations of the different techniques is crucial85 and generally no single method will provide the full picture of mould exposure and presence in a building76.

## Growth of moulds on building materials

Moulds can grow on laboratory media at temperatures as low as -7(C99 and some wood associated cladosporia and penicillia are able to grow at temperatures as low as -5(C on wood, but seem to require at least 0(C to germinate100. In comparison Aspergillus restrictus101 requires 9(C, and A. versicolor  4°C25 for growth on a high nutrient substrate such as MEA, indicating that temperature cannot be used to avoid fungal growth in buildings.

The associated funga is also selected by aw, light99 and especially the composition of the material, including organic carbon, pH, nutrients like trace metals, nitrogen, phosphor and sulphur10,62-64,99,102, consequently the most important of these factors will be reviewed in the next subchapters.

### "Water - the key factor"11

This is undoubtedly the most important factor for determining if mould growth will start in a building11. Most of the moulds have their optimal aw at 0.96-0.98 even though some are able to grow at much lower aw11,102,103. Some xerophilic fungi like Eurotium spp. and Wallemia will not grow at such high aw72,80.

The germination process requires a slightly (approx. 0.02) higher aw than the critical aw for growth64,101,104-107, older spores also require longer time to germinate105.

In ¡Error! Argumento de modificador desconocido., data on the minimal aw for growth on food products and agar media have been compiled. On agar media the aw was usually regulated by adding glycerol or occasionally sugars to the media.

| Table ¡Error! Argumento de modificador desconocido. Minimal aw for fungal growth of selected species |
| --- |
| Medium | Aspergillus versicolor | Eurotium spp. | Penicillium spp. | Cladosporium spp. | Rhodotorula spp. | Alternaria spp. | Stachybotrys chartarum |
| Food products80 | 0.78 | 0.70-0.72 | 0.78-0.84 |  |  |  |  |
| MEA101 |  | 0.71 | 0.74 |  |  |  |  |
| MEA105 |  |  | 0.81 |  |  |  |  |
| MEA106 |  | 0.71 | 0.79-0.82 |  |  |  | 0.94 |
| MEA108 |  |  |  | 0.81 |  | 0.85 |  |
| Different agars62 | 0.80 | 0.70 | 0.80 |  |  |  |  |
| MEA101 | 0.74 | 0.71 |  |  |  |  |  |
| MEA109 | 0.81 | 0.76 | 0.82 | 0.85 | 0.92 | 0.89 | 0.95 |
| DRBC*109 | 0.81 | 0.77 | 0.83 | 0.86 | 0.93 | 0.89 | 0.95 |

* Dichloran Rose Bengal chloramphenicol agar.

Table ¡Error! Argumento de modificador desconocido. compiles data on selected mould growth on different building related materials, as the minimal aw on these are higher than on the more nutrient rich agar substrates.

| Table ¡Error! Argumento de modificador desconocido. Minimal water activity for fungal growth on materials of selected species and genera |
| --- |
| Medium | Aspergillus versicolor | Eurotium spp. | Penicillium spp. | Trichoderma spp. | Cladosporium spp. | Rhodotorula spp. | Alternaria spp. | Stachybotrys chartarum |
| Ceiling tile110 |  |  | 0.85-0-90 |  |  |  |  |  |
| Fibre glass110 |  |  | 0.85-0-90 |  |  |  |  |  |
| Wood chip paper, 25(C61 | 0.84 |  | 0.84-0.89 |  | 0.96 |  |  | no growth |
| Viscose 111 | 0.80 | 0.80 | 0.80-0.85 | 0.85-0.90 | 0.90 |  |  | 0.90 |
| Woodchip paper at 12(C61 | 0.91 |  | 0.91-0.87 |  | 0.97 |  |  | no growth |
| Painted woodchip paper, 25(C61 | 0.79 |  | 0.84 |  | 0.93 |  |  | 0.97 |
| Painted woodchip paper at 12(C61 | 0.87 |  | 0.87 |  | 0.87-0.91 |  |  | 0.96 |
| Fibre glass earth cont.112 | 0.69-0.72 |  | 0.53-0.60 |  | 0.85-0.87 |  |  |  |
| Fibre glass112 | 0.85-0.87 |  |  |  | 0.96-0.98 |  |  |  |
| Wallpaper and paper113 |  |  |  |  |  |  |  | 0.78-0.81 |
| Gypsum113 |  |  |  |  |  |  |  | 0.84-0.89 |
| Cellulose filter114 |  |  |  |  |  |  |  | 0.84-0.89 |
| Woodchip wallpaper109 | 0.85 | 0.77 | 0.86 |  | 0.89 | 0.93 | 0.90 | 0.97 |

Table ¡Error! Argumento de modificador desconocido. shows data on building materials, where the moulds were applied as a mixture, the natural contamination was used or where moulds growing were not identified, often referred to as mildew.

| Table ¡Error! Argumento de modificador desconocido. Minimal water activity for fungal growth of mixtures or unidentified fungi (mildew) |
| --- |
| Medium | Mixture |
| Pinewood , planned115 | 0.80 |
| Painted wood115 | 0.80 |
| Hardened pain115 | No growth |
| Distempered wood115 | 0.80 |
| Brick115 | 0.88 |
| Cement rendered brick115 | 0.80 (but almost no growth) |
| OSB, MDF, Particle board, Fibre board, wood116 | Growth at 0.70 (after 8 weeks) |
| Glass wool and cotton117 | 0.92-0.96 |
| Cotton fabrics118 | 0.70 |
| Wood and wool117 | 0.85 |
| Leather117 | 0.76 |
| Different wood119 | 0.80, 0.90 when temp < 5(C |
| White brick115,115 | 0.80 |

It is clear from Tables 4 and 5 that no consensus exists on the minimal aw for fungal growth on materials. It is however generally known that the humidity calibrations in many studies are not correct11. Hence studies are needed with more precisely controlled humidity and other environmental conditions.

#### Humidity - some definitions

Figure ¡Error! Argumento de modificador desconocido.. Relations between air temperature, relative humidity and absolute humidity.

The water activity is called equilibrated relative humidity in some papers109 and is the same as the RH/100 (at steady state). Aw is considered a better descriptor of available water64,120 than the absolute water contents in the material62,64,111. This is perhaps seen more clear when the aw relation to the osmotic pressure is shown62,64,120, as it is the difference between this pressure and the osmotic pressure in their own cytoplasma the moulds have to maintain:

Where T is the absolute temperature, R the gas

constant, and V the partial molal volume of water.

Large local differences in ventilation and surface temperatures, especially on thermal bridges, can generate micro climates with very high aw, even in rooms with low RH. This is due to the large temperature dependency of RH and the water contents of air as illustrated in Figure ¡Error! Argumento de modificador desconocido.. For example, if the indoor air temperature is 22(C and the RH is 50%. The RH at a cold wall of 15(C can be estimated to about 80% RH, which is at the RH point where moulds starts to grow.

Precise measurements of the humidity in materials and the air is difficult especially at RH > 90%. Especially the measurements are calibrated against sulfuric acid gives inaccurate determinations11,64.

#### Transient conditions

Physical parameters including humidity and temperature are not constant in buildings, and greatly influences the mould growth11,121-123. A bathroom in one of the extreme examples of this, and in this environment the funga is different than in environments with more constant environmental conditions72,124 as it is being dominated by phylloplane fungi such as Phoma, Aureobasidium, and Cladosporium. This field observation is explained by data of Park125 who showed that after drying for one week, phylloplane fungi were able to re-attain growth from the hyphal tip within 60 min whereas storage moulds (Penicillium spp.) and soil fungi (Fusarium spp., Verticillium, and Trichoderma) needed 1-2 days, meaning that the phylloplanes can cope with a few hours of humid environment in the bathroom.

Adan11, who worked with mould growth on plaster and painted materials, introduced the term Time-of-wetness (TOW) defined as the ratio between the wet period (RH ( 80%) and the total period, and the term f, for the number of cycles per day. It was shown that using air dryer than 65% during the dry period did not affect the growth, and that growth increased slowly with TOW from TOW=0.17 to 0.5, with a dramatic increase of higher TOWs. The parameter f had only very limited effect on growth, unless very high values were used (f>4). Viitanen122,126 also showed that when short time fluctuations were applied (0.25 days) the growth occurred more slowly compared with longer periods (1, 2, 7 and 14 days).

### The impact of the material on the mould growth

Moulds are able to degrade almost all natural and many man made materials25,72, especially if they are hygroscopic11,117. Even totally inorganic materials will still get mouldy as they over time absorb dust which is a good medium for especially A. fumigatus25 and A. versicolor127,128.

Wood is still one of the most commonly used materials, and is highly susceptible to mould growth122,129,130. It may become infested with Cladosporium, P. brevicompactum and P. expansum, already at the sawmill100. Kiln drying makes the surface of the wood more susceptible to mould growth122,126, as the surface will get a higher content of nitrogen and low molecular carbonhydrates131. A number of modified wood materials are commonly used, and materials such as OSB, plywood and MDF are more susceptible to growth of Aspergillus, Trichoderma and Penicillium than solid wood, particleboard116, acylated wood132 and wood-polyethylene composites133.

Prefabricated gypsum board is the most commonly used inner-wall material in new Danish buildings. However due to the paper, used to reinforce the material, the boards are highly susceptible to growth of moulds especially the cellulytic S. chartarum14,25,79,113,134. The gypsum itself (used to plaster walls) can also support fungal growth and the susceptibility is then correlated to the relative nutrient content of gypsum11 and additives who make it more hygroscopic at lower humidities135.

Many indoor surfaces are wallpapered and this increases the susceptibility of the walls, as paper and the glue are very good media for most indoor moulds61,71,79.

Plastic materials are being increasingly used, and polyethylene and PVC are vulnerable to mould growth, as the moulds utilise most plasticizers136. Already in 1957, Berk, et al137 showed that 90 of 127 different plasticizers could be degraded by moulds commonly found on indoor surfaces. Even fibre glass insulation112,138 and fibre glass ceiling tiles (10% urea phenol-formaldehyde resin)110 support fungal growth of especially A. versicolor and Penicillium sp. Polyurethanes has been used in many composites as well as insulation materials, and some of them are highly susceptible to mould attack139 and they should be routinely tested for microbial degradation. Especially Paecilomyces variotii, T. harzianum, and Penicillium spp. are frequently growing on urea-formaldehyde foam insulation materials79.

Paints can both increase and decrease the susceptibility of a given base material. Waterborne paints, which are the most commonly used in Europe due to occupational health problems with organic solvents, are highly susceptible to mould growth and should be routinely tested11,140. However the base material for paint is also important for the mould growth11,61. Aureobasidium pullulans is the absolutely most common mould on paints which it deteriorates in contrast to Penicillium and Aspergillus species who grows superficially on the paints141, actually A. pullulans is often succeeding Aspergillus, Alternaria and Cladosporium on acrylic paints142.

Mould growth in air filters143 and in ventilation ducts144 is of special concern, as the ventilation system will act as an effective carrier of the spores. In the ventilation ducts growth generally occurs on painted surfaces and especially in dust145, although certain fibre glass insulation materials may support growth16,146.

### Modelling mould growth on materials

Validated models which can predict fungal growth under different environmental conditions on building materials are extremely important as they can be interfaced with many of the current PC programs which can model humidity conditions on materials, and simulate real buildings. However only a very few models for growth on materials have been published:

- Rowan109 predicted RH limit for growth of S. chartarum, A. versicolor and Eurotium herbariorum, as a function of temperature (3rd order polynomial), and interfaced this simple model for transient temperature and humidity conditions in buildings.

- Hukka & Viitanen147 have an almost identical model, and have improved it126,147 to include also growth under transient temperature and humidity conditions.

However, none of these models have been validated on a large number of real buildings with and without mould problems, which is the only way to validate these models.

Adan11 have developed several models for comparing the susceptibility with building materials to both constant and transient humidity conditions. These are however more sophisticated and they are based on a non-linear logistic model, which is able to cope with the non-linear, 6-point scale, used to compare the susceptibility of different materials.

## Health problems associated with airborne moulds

A number of different approaches exist for studying the health effects associated with mouldy buildings. The two major approaches are: i) comparing the toxicity or biological activity, based on in vitro and in vivo data, with the actual exposures in the buildings; ii) epidemiological studies where symptoms in a large population are correlated to exposure in normal and mouldy buildings.

In the first studies of health problems related to mouldy buildings it was believed that people were type I allergic25,148, meaning that IgE antibodies are formed against specific proteins, called allergens, from the fungal spores 25. Type I allergy can be precisely diagnosed by the classic skin prick testing (SPT) or in serum if extracts of the appropriate allergens exist25.  SPT panels and antibody-allergen-kits for the outdoor air moulds, Alternaria and Cladosporium, as well as some penicillia and aspergillii have been commercially available for a number of years, but are not available for many of the building associated moulds. Allergic persons are often genetically predisposed25 and may develop asthma due to the inflammation of the lung due to the large quantities of inflammatory mediators released from the different lung granocytes. However, as type I allergy is not the main cause of the health problems observed in mouldy buildings22,30, the use of SPT or specific IgE in serum has a very limited diagnostic value when working with mouldy buildings.

A number of other types of antibodies, including the IgG antibodies, are naturally produced against most "non-self" proteins and help clearing these from the body. Detection of specific IgG antibodies against these "non-self" proteins can hence be used do determine if a person have actually been exposed to a specific mould. However only positive results can be used, as not all people will develop detectable quantities of IgG antibodies23.

High exposures to protein dust may result in so high level of antibodies and the specific protein in the blood stream that these are deposited in such quantities in the blood stream that they trigger a immune response (called type III allergy or farmer's lung) seen as malaise, elevated temperature, pains in joints and even astma25,149.

### In vivo and in vitro effect of fungal spores

As earlier mentioned, the vehicle for exposure to mycotoxins in the indoor environment seems to be the fungal spores47 and fragments of these and the mycelia91. Hence, studies of the effects of whole spores are important as they contain the whole "mixture" of metabolites and structural components as well as the particle effect of the spores150.

An interesting study showed that rats exposed to naturally released spores of A. versicolor (up to 10×106 CFU/m3) originating from growth on the walls, during one month developed severe lung damages including granulomatous lesions, partly due to high production of IL-1 from the macrophages151.

Instillation of P. chrysogenum spores in mice152 revealed similar results, and in addition showed that 104 spores instilled twice a week increased total IgE in serum and IL-4 in the lung bronchoalveolar lavage, interestingly this was not seen when the spores were treated with methanol to kill them or extract metabolites.

Shahan et al153 showed that spores from different fungal species induced very different responses in rat macrophages, measured as mRNA induction of TNF( and other inflammatory mediators. Spores from A. terreus and P. spinulosum did not stimulate any inflammatory response, in contrast to A. fumigatus, A. candidus, A. niger, Eurotium amstelodami, and C. cladosporioides which stimulated production of several inflammatory mediators.

Ruotsalainen154 showed that Stachybotrys isolates (21 different) induced either strong inflammation, by releasing NO, TNFα, IL-6 and reactive oxygen species (ROS), or cytotoxicity (induced by satratoxins producing isolates) in macrophages. In vitro studies with instilled Stachybotrys spores in mice have showed similar results 46,46 and will be dealt with in details in section ¡Error! Argumento de modificador desconocido..

The cytotoxicity of Penicillium and Aspergillus isolates from damp buildings in Scotland cultured on MEA was studied at it was found that about 50% of the investigated isolates were cytotoxic to the fibroblasts155,156. Such cytotoxicity may cause severe lung damage, especially if the fibroblasts and perhaps also macrophages die by necrosis, as the latter subsequently will liberate high quantities of inflammatory mediators.

However there seems to be many different mechanisms associated with the effects in cell cultures, especially when both cytotoxicity and inflammatory potential are tested simultaneously 157. Generally many mould spores will kill macrophages before they are able to respond with an inflammatory response.

These studies indicate that the lung damage induced by fungal spores may be partly or fully due to the inflammation induced by the macrophages as it has been shown that excess induction of some cytokines, NO and ROS may play an important role in the pathogenesis of inflammatory diseases such as asthma 158-160. It is also notable, that isolates/species specific metabolites are involved. However, except for the first, they have all used spores from agar culture, which is seriously biased as moulds usually produces much higher quantities of metabolites on these media71.

Literature on in vitro and in vivo studies of specific metabolites will be found under the producing mould species in section ¡Error! Argumento de modificador desconocido..

### Epidemiologically studies

Epidemiologically studies have been widely used to study health effects in mouldy buildings6,9,161, especially combined with questionnaires to determine symptoms and/or if the home or workplace has been damp or mouldy. However several studies have concluded that objective measures is needed to obtain statistical significant results6,30,93,95.

A large number of studies on general health problems and the association dampness and mould growth have been published (see ¡Error! Argumento de modificador desconocido. p. 1), however reviewing these is outside the scope of this work, and only case studies of specific moulds will be further dealt with, as they may be correlated to specific fungal metabolites.

Johanning et al23,162 studied an office building heavily infested with S. chartarum. Only two persons were IgE positive to S. chartarum, these persons worked in the same area and some had abnormal complement function and composition of T and B lymphocytes, CD3+ T cell (CD3 is a protein found on both Tcytotoxic and Thelper cells149) concentrations were lower among the employees than among controls. IgG measurements showed only small differences between exposed and non-exposed employees and were not significant correlated with symptoms. In a later paper20,163, they reported several more cases from the clinic with corresponding surveys of their homes for mould occurrence. Specific IgG antibodies could only be used as exposure markers but was only positive in 25% of the cases of actual exposure.

In a 10 years old building with severe water damages Hodgson et al19 found that the occupants had significantly more pulmonary problems, as eye irritations, stuffy nose, and especially flue like symptoms, than normal. Air samples in one of the rooms revealed up to 8000 CFU/m3 of especially A. versicolor, and in an other room up to 129 CFU/m3 but with up to 50% of the colonies being S. chartarum.

#### Idiopathic pulmonary hemosiderosis cases

A dramatic escalation in the symptoms observed in mouldy buildings has been reported from the Cleveland, Ohio, area164,165. Here idiopathic pulmonary hemosiderosis (IPH) in infants (< 6 months old) was associated with growth of S. chartarum in the homes. It should be noted that IPH is extremely rare in infants, with a general prevalence of 0.2-1.2 per 106 children per year in the Western world166. Reports of such life threatening conditions including fatal cases has great legal implications, especially in the USA, as well as economically importance for the rest of the world as it could lead to guidelines not accepting growth of S. chartarum in buildings.

The first 10 IPH cases from Cleveland reported in December 1994 by the US CDC167 whoever with no plausible reason. Later CDC reported additional 27 cases from Cleveland164,165, and at this time it was concluded that IPH was associated with growth of S. chartarum. Additional 7-9 cases were identified in Chicago168 and 6 from Detroit169, however no mould investigation of the houses have been published.

An overview over the IPH cases in the USA has been made by Dearborn et al26, who found 138 IPH cases in the USA the period 1993-1995, and that the IPH incident rate in Cleveland was 1.5 IPH per 103 infants per year in the period. The association between IPH and Stachybotrys exposure has been questioned by the CDC170, after a anonymous review to which the investigators have not been able to respond to.

An additional case has been reported from Kansas city171,172 in a home with a mould infested ventilation system, yielding 420 Stachybotrys spores/m3 (counted by microscopy) from the in bedroom of the infant, however also extremely high counts of Penicillium and Aspergillus (11250 spores/m3 counted by microscopy) in the air was detected.

From Houston a case has also be describes28, and here Stachybotrys (= Houston strain173) was isolated from the lung of a 7 years old white boy with IPH, chronic cough, and chronic fatigue.

From Cleveland and additional case have been reported174 with no abnormal clinical tests except from the hemosiderin laden macrophages (showing that the bleedings had been occurring over some time) recovered from the lung. The bedroom of the child was heavily infested with S. chartarum and air samples revealed 6(104 CFU/m3 of the fungus.

From St. Louis there is also a report27 on a case of IPH in an infant, who was exposed to fungi during a 2 weeks holiday. On the return trip the infant developed the hemorrhage upon exposure to tobacco smoke. Low quantities of hemosiderin in macrophages in the lung indicated no preceding bleedings. During the vacation (14 days) the infant had resided in a room with visible mould growth of Trichoderma, Penicillium, Cladosporium and Ulocladium.

Recently a fatal IPA case have been discovered in Belgium (N. Nolard, personal communication), in this case airborne spores were detected, they were released in high numbers due to constructional work in the bathroom.

## Biologically active metabolites from moulds

Microfungi have the ability to produce a high number of secondary metabolites, which they for various reasons need in their natural habitat175. M176ost of these are produced as a response to other organisms especially other fungi177. Some of these metabolites can cause a toxic response "when introduced by a natural route in low concentrations to higher vertebrates and animals" and are referred to as mycotoxins178.

Sorenson179 and Miller76 were some of the first to realise the implications of mycotoxins in the indoor environment. The latter emphasises that moulds generally produce several mycotoxins and synergizers, which are not toxic themselves, but enhance the toxicity of some mycotoxins180. It is also stressed that chronic low concentration exposure of airborne mycotoxins would be very difficult to diagnose.

When trying to predict which biologically active compounds of microfungal origin may be present in water-damaged buildings - at least five problems have to be addressed:

- Most secondary metabolites and mycotoxins are species specific making identification of isolates to the species level extremely important. Changes in taxonomy including introduction of new species and synonomisation of others has further complicated this work69,181.

- False positive findings of mycotoxins are often common from laboratories which use insufficiently specific methods, or which are not experienced in mycotoxin analysis and the large number of interfering compounds produced by moulds69.

- Even in fungal extracts of species, which have been extensively studied for their metabolites as e.g. Aspergillus flavus and A. fumigatus, Fusarium graminearum, unknown biologically active metabolites are still present76.

- A large number of the secondary metabolites described in the literature have been tested in a very few assays, and extremely few compounds have been tested in full animal studies.  The latter method is unfortunately often the only way of finding defects in the offspring or reveal metabolites which are activated in special organs such as liver or kidney150,182. For exposure assessment even fewer metabolites have been tested in inhalation studies where some metabolites have been magnitudes more potent183.

- The produced metabolites varies considerably between media, so the moulds may produce very different metabolites when growing on building materials70,184.

It should be considered that on naturally infested materials the moulds do not grown in pure cultures, but in mixed cultures with other moulds and often also bacteria. These conditions may induce production of other metabolites than in pure cultures54.

The following review will target the potential fungal metabolites produced in buildings by the building associated funga, and may have a varying detailing level. This reflects where most of the experimental work has been concentrated and where less known species and genera have been reviewed.

The tables of the metabolites reported from the reviewed species have been moved to Appendix B, as many of them run over several pages, and hence will diminish the readability of this thesis.

### Stachybotrys

# Stachybotrys chartarum (Ehrenberg ex Link) Hughes (= S. atra Corda, and S. alternans Bonord.) is the only species from this genus which has been found in buildings.

Jong & Davis185 made a revision of the genus in 1976 based on available cultures and found that the genus comprised additional ten species: S. albipes, S. bisbyi, S. cylindrospora, S. dichroa, S. kampalensis, S. microspora, S. nephrospora, S. parvispora, S. oenanthes and S. theobromae. Later McKenzie186 described three new species from decaying leaves, and Dorai & Vittal 187 and Hua-zhong188, Miyazaki  et al189 additional species.

Most interest of S. chartarum has been due to its capacity to deteriorate organic fabric fibres185 and its ability to produce the highly cytotoxic macrocyclic trichothecenes190,191 which have given significant problems in mouldy straw in Eastern and Northern Europe190,192-194.

Stachybotryotoxicosis was first described in the 1930s by Russian researchers195, and later by Forgacs in the English written literature193,196. He assisted Russian veterinarians during World War II, where stachybotrystoxicosis in horses was a severe problem for the Russian army197. Russian researchers showed that horses were very susceptible to Stachybotrys infested straws198. Forgacs describes two types of toxicosis: i) A typical form with inflammation of the stomach, and the mouth as well as necrosis some places, followed by a decreasing number of thrombocytes and a decreases in the blood clotting, followed by a decreasing number of leukocytes and an almost total absence of blood clotting198; ii) An atypical form, characterised by nervous disorders, as loss of reflexes, elevated body temperatures, and altered cardiac action198.

The link to indoor air appeared in 1986, when Croft et al48 described a household in Chicago, where the occupants suffered from symptoms similar to stachybotryotoxicosis. Filters from air sampling in this home was black after sampling due to the many Stachybotrys spores (B. B. Jarvis, personal communication).

#### Trichothecenes

In 1973, Eppley & Bailey190 were the first to isolate trichothecenes from S. chartarum, they found the known components, trichodermol and roridin E (RE) and three novel components, named satratoxins H, G and F199. These three components were first structure elucidated 4-7 years later191,200. All trichothecenes produced by Stachybotrys species have been compiled in Table 1 in Appendix B.

The trichothecenes (TR) are divided into the following four groups201.

- Type A trichothecenes (TA), easily described as the trichothecenes (TR) not included in the following three groups. These trichothecenes have been isolated from species within the fungal genera Memnoniella, Trichoderma, Trichothecium, Myrothecium, Stachybotrys, and Fusarium, are highly cytotoxic.

- Type B trichothecenes (TB) are characterised by the C8-keto group. This group is approximately only 10% as toxic as the TA182,202 and is only produced by Fusarium species.

- Type C trichothecenes are characterised by the ring from R2 to the R3 alcohol group and are generally referred to as macrocyclic trichothecenes (MTR). These are at least 10 times more cytotoxic than the type A, and are produced by species of Stachybotrys and Myrothecium.

- The very rare type D trichothecenes are characterised by a C-7,8 or C-9,10 epoxy group.

Figure ¡Error! Argumento de modificador desconocido.. Purposed biosynthesis of the macrocyclic trichothecenes.

The sesquiterpenoid pathway of the trichothecenes produced by Fusarium has been examined in detail (see Figure ¡Error! Argumento de modificador desconocido.) due to the economical importance of this genus203. An important step in the biosynthesis is the then cyclization to trichodiene by trichodiene synthase, encoded by the TRI5 gene203-205, which has been characterised in Fusarium, Myrothecium and Stachybotrys203,206,207. Trichodiene is volatile and can be used as an indicator for the synthesis of trichothecenes208,209. The MTR is the synthesised over trichodermin and the trichoverroids as seen in Figure ¡Error! Argumento de modificador desconocido.203,210.

Several studies have shown that S. chartarum strains isolated from cereals can produce MTR113,114,211 when grown on building materials and air filters. In naturally infested materials MTR have been detected by Croft et al48 who found, satratoxin H (SH), verrucarin B (VB), verrucarin J (VJ), and the trichoverrins. Several later studies have verified these findings54,171,212. From an exposure point of view, Sorenson47 have shown that the spores from MTR producing isolates contained approx. 10-40 ppm of the MTR ≈ 40 fg MTR per spore, whereas Nikulin et al 46 found 140 fg/spore.

Not all S. chartarum strains produces satratoxins, Korpinen & Uoti194, showed that 67% of the S. chartarum strains isolated from toxic feed in Finland were cytotoxic to fibroblasts (presumably producing satratoxins). Andrienko & Zaichenko213, showed that Russian S. chartarum isolates grown on seeds, could be grouped in four: i) 19% with highly dermatoxic properties (presumable being satratoxin produces); ii) 4% with only antifungal activities; iii) 47% strains with antifungal and antibacterial activity also being dermatoxic; iv) 26% with no biological activity. Jarvis et al214 found that 80% of the strains isolated from stachybotrytoxicosis cases in farm animals from Eastern Europe produced MTR. This is significantly different from the strains isolated in water-damaged buildings in the USA where only 30-40%, of the isolates from the IPH case homes produced MTR45,215 and from Finland154 where about 50% of the strains were highly cytotoxic to murine macrophages, resembling the biological activity of MTR producing strains.

Toxicology of the trichothecenes

It has long been known that the TR generally inhibited the protein synthesis202, where some inhibited the ribosomal termination or the elongation of the translation process. Later both TR and MTR have been shown also to induce apoptosis in cells, by activating SAPK/JNK and p38 MARK kinases by ribosome binding inhibiting the protein synthesis202,216. Interestingly trichodermol and trichodermin are the only TR that are non-cytotoxic202.

Parent-Massin & Parchment217 grouped haematoxicity, abnormal blood cell grouping or malfunction, of mycotoxins in three groups:

- Haematoxicity not described in literature: patuline, verrucosidin, and fumonisins.

- Compounds able to cause adverse haematoxic effects, but with the principal mechanism not being haematoxic: ochratoxin, aflatoxin and zeralenone

- Compounds giving severe haematoxic effects, with minor symptoms, like the trichothecenes.

At high concentrations (10-20 mM) T-2 (the most toxic TA) induces heamolysis of red blood cells of rodents, pigs, dogs, horses and humans. Single doses of DAS (a TA) given to humans as anti-cancer drug (Phase I test), resulted in vomiting and central nervous toxification. TR have a significantly lower LD50 value in new borne animals (mice, lowered by approx. 100 () in which the pathologists found severe lesions of bone marrow, thymus and spleen.

As only few MTR are commercially available, only few studies on these components exist. However Hughes et al218 studied the effect of 11 different MTR on the immune system of mice. They were administered, once, with half the LD50 dose and sacrificed after 4 days. White blood cell concentration decrease upon exposure to VJ and RE, but some of the others MTR had the opposite effects. This might be due to more circulating white blood cells at the start. ELISA showed a decreased production of antibodies against sheep red blood cells for some components.

Pestka & Bondy219 who showed that mice exposed to TR had up to a 10 000 lower LD50 to Salmonella typhimurium exposure. This is presumably due to the fact that leukocytes (white blood cells) are affected at far lower concentrations than the acute ones217. Especially TA, are cytotoxic to granulocyte, monocyte and erythroblast progenitors217 at concentrations higher than 5(10-8 M.  Effects at this level includes inhibition of antibody production, delayed skin graft rejection, and inhibiting phagocytosis of murine macrophages150.

These symptoms resemble the ones observed in humans from Stachybotrys infested buildings reported by Johanning et al23,162 (see section ¡Error! Argumento de modificador desconocido.), especially when combined with the data of Creasia et al183,220 who showed that the acute effects of the TR T-2 toxin in rodents was 10-20 time stronger when it was inhaled than when it was administrated through the feed. However Pang et al221 was not able to verify this effect in pigs.

Animal studies on the inhalation of Stachybotrys spores

The association of IPH cases with S. chartarum26 has of course triggered a number of projects on the influence of S. chartarum spores on cell cultures and whole animals.

Lung mycotoxicosis in mice was demonstrated by Nikulin et. al.46 who used two S. chartarum strains, isolates #72(=CBS 414.95 = IBT 9460) and #29 (=CBS 413.95 = IBT9472). It was shown that #72 induced much more severe haemorrhage in the mice than #29. The first isolate produced satratoxins and high quantities of stachybotrylacetones and the later strain produced only minor quantities of the latter type. The same group222 also instilled mice with 103 and 105 spores of the same two S. chartarum isolates 6 times during 3 weeks. In the mice instilled with the highest dose, severe inflammatory changes were observed in the lungs. The mice administered with spores from #72 developed much more severe inflammations than the mice instilled with spores from #29. At the lowest level only the mice instilled with the spores from the satratoxin producing isolate, #72, developed inflammatory changes in the lungs. However due to the few isolates used and the variation in both MTR and stachybotrylacetone production the study remains partly inconclusive on the responsible components.

This is the same for the study of Mason et al223,224 who instilled S. chartarum spores and iso-satratoxin F in the lungs of mice, and observed that both obstructed the lung homeostasis whereas Cladosporium spores did not. However the S. chartarum spores and the pure toxin induced very different surfactant production (P60 and P100 phosphor lipids), but no chemical analyses were performed on the strain so it is unknown if it produced MTR.

Rao et al225 instilled spores in rat lungs, and showed that when spores from a highly cytotoxic (presumably a MTR producer) of S. chartarum was methanol extracted, the toxicity of the spores almost disappeared compared with unextracted spores. This clearly shows that the pulmonary toxicity is due to extractable metabolites as MTR or most of the metabolites described in the following subchapter.

The conclusion drawn from these studies is that S. chartarum spores indeed contains a number of metabolites which can induce severe inflammation, haemorrhage and death in animals. However there is no evidence that these effects are only caused by the MTR.

#### Non trichothecene metabolites

Figure ¡Error! Argumento de modificador desconocido..  Left, the spiriocyclic drimanes, stachybotrylactone (X=O) and stachybotrylactam (X=NH). Right, SMTP-1, one of their precursors.

Most species in Stachybotrys and especially S. chartarum produces high quantities of a number of spiriocyclic drimanes189,226 as shown in Figure ¡Error! Argumento de modificador desconocido.. These components have a number of biological properties, inter alia inhibition of TNFα liberation from human macrophages227, complement inhibition189,228 and  antiviral activity229. When considering that one of the most common symptoms in mouldy buildings is recurrent airways infections, metabolites which inhibits the complement system are interesting, as the complemet system is an important part of our defence against bacteria149. A number of triprenyl phenol metabolites (see Figure ¡Error! Argumento de modificador desconocido.) have been described from several Stachybotrys species. They are precursors of the spiriocyclic drimanes, as the triprenyl can be cyclizied into the drimane part. These metabolites can activate and enhance the plasminogen-mediated fibrinolysis (at levels down to 100 µM)230-232  and could in that way be plausible components responsible for IPH, as this could account for the brittle blood vessels in the lungs.

Both the triprenyl phenols and the spiriocyclic drimanes are produced by two mixed biosynthetic pathways, partly by the sesquiterpenoid pathway (shown in blue on Figure 3) and partly by the polyketide pathway. Reviewing the literature on these components has been troublesome as Russian groups have published known structures under new names, data on the stereochemistry is often not available, and a significant number of the publications have been Japanese patents and patent applications. Chemical and biological data on the spiriocyclic drimanes and other non-trichotehcene metabolites are given in Table 2, Appendix B.

A new type of metabolites has been isolated from non-satratoxin producing isolates of S. chartarum, and has been named atranones215. They are 233 biosynthetically related to the dolabellanes234 and altogether 8 atranones and two dolabellanes have been isolated from the S. chartarum cultures215,233. Three of these metabolites (6β-hydroxydolabella-3E,8E,12-trien-14-one, atranones B and C) have also been detected in material samples from a IPH case home in Cleveland235. However the biological activity revealed until now on these components has been rather limited, but with number of enzymatic steps used to synthesise such complicated components234 they must have a biological activity.

A component belonging to the immunosuppressing cyclosporin family has also been isolated from a Stachybotrys sp.236, and is of course interesting due to many infections experienced by people living in mouldy buildings. Also components, shown not to be TR, damaging the cell membrane of boar sperm cells has also been described237 from S. chartarum, however it has not been cleaned up and characterised.

Vesper et al238 tested the haemolytic activity235 of S. chartarum isolates from the Cleveland IPH cases, grown on gypsum boards. Heamolysis was correlated to growth at 35(C and not at 23(C, and a higher percentage of the spores from IPH case homes were haemolytic. The responsible component have just been partly charecterised239 as novel haemolytic protein, stachylysin. Additionally the group have showed that the S. chartarum strains from the IPH case homes produces higher quantities of siderophores than strains from non-IPH case homes173.  As iron is a key component for pathogens240-243 iron binding proteins and peptides excreted from pathogenic bacteria241 and fungi244 are well known. The authors seem to indicate that a mechanism might be partly due to actual growth of Stachybotrys in the lung tissue of the infants.

All these findings clearly show that the biologically active components from S. chartarum are far from known, and even when they are all known there will still be much left to do in determining the actual exposure to these in mouldy buildings.

### Aspergillus

As the genus of Aspergillus Mich. ex Fr. is one of the anamorph genera placed in the family Trichocomaceae, where it is associated with 8 holomorph genera. This is new in comparison with the last monograph by Raper & Fennell245, which is still extensively used, although is should only be used in combination with "Integration of modern taxonomic methods from Penicillium and Aspergillus classification" and Modern concepts in Penicillium and Aspergillus classification from 2000246 and 1990247 respectively.

The following sub chapter has been divided into subsections on the most important species.

#### A. versicolor

A. versicolor  (Vuillemin) Tiraboschi belong to the subgenus »Nidulantes« section »Versicolores«, with no known teleomorphs. This species is common in many dry environments and is one of the few aspergillii, which are also common in temperate and cold environments25. It is the absolutely most common Aspergillus in damp and water-damaged buildings.

Together with several streptomycetes248 and Chaetomium globosum249 it may be one of the major producers of the mouldy smelling component, geosmin, in buildings250.

Fragments which are significantly smaller than the spores are liberated from A. versicolor infested building materials91 and may account for the health problems in buildings where it is the predominant species on the materials without being so in cultivation based air-samples.

Prolonged exposure may lead to significant lung damage, maybe as a secondary effect of IL-1 liberation151, as discussed earlier in the report.

Sterigmatocystin

Sterigmatocystin (ST) is considered the most important toxic metabolite of A. versicolor and as seen in Table 3 in Appendix B, a number of analogues have been isolated including a number of precursors that are also biologically active.

The biosynthesis of ST has been studied in detail, as ST is only two enzymatic steps from aflatoxin B1 (AFB1) which is of great economical importance for the agriculture industry. ST is deca polyketide synthesised over a C20 precursor, which is then transformed to norsoloric acid, averatin, 1'hydroxyversicolorone, versiconal hemiacetate acetate, versicolorin A and finally ST251, meaning that findings of ST would also imply the presence of a significant number biologically active precursors.

ST is cytotoxic by itself, but the major problem is the carcinogenic properties after activation in the liver by the cytochrome P450 mono-oxidase system, to the 8,9-epoxide analogue which then preferable reacts with guanine as seen in ¡Error! Argumento de modificador desconocido., just as for AFB1 182,252.

ST has been shown to be a very strong inhibitor of the of chicken tracheal cilia253,254, and as this is one of the important ways we clean our upper airways, inhibition of this system may increase the risk of upper airways infections.

Figure ¡Error! Argumento de modificador desconocido.. Activation of sterigmatocystin and formation of the guanine adduct.

No studies of airborne ST have been found. However several exist for AFB1, which in rats and mice (one dose 17 mg/kg) suppressed the macrophage phagocytosis for 2 weeks as well as their release of TNF( upon exposure to endotoxin. Airborne dust containing AFB1 has been shown to increase the risk of liver cancer in workers handling ABF1 infected animal feed by two- to threefold with a 10 years latency32,33. Later studies have shown that the AFB1-guanine-adduct is an important exposure biomarker252.

ST production is influenced by the humidity on cereals, as was only detected at RH over 88.5% and the maximum production of the toxin as well as biomass occurred at 93% RH255, and hence the same phenomena may be found in buildings.

Other metabolites

A. versicolor produces a number of other metabolites shown in Appendix B, table 4, but their toxicity is generally not very well described. The production of cyclopiazonic acid by A. versicolor reported by Ohmomo et al256 was due to misidentification with A. oryzae69 and isolation of griseofulvin, dechlorogriseofulvin, and 3,8-dihydroxy-6-methoxy-1-methylxanthone from A. versicolor reported by Kingston et al257 must be due to a misidentification or contamination with a griseofulvin producing Penicillium (J. C. Frisvad, personal communication).

#### A. ustus

Aspergillus ustus (Bainer) Thom & Church, also belongs to the subgenus »Nidulantes« but is placed in the section »Usti«, and has no known teleomorphs.

The most extensive work on A. ustus metabolites have been done in South Africa by the group of Steyn and Vleggaar, due to problems with mycotoxicosis in cattle caused by A. ustus infections of grains258-260. And as seen in Appendix B, Table 5 the austamides and austdiols261,262 are acute toxic and the austocystins both toxic and carcinogenic263. The later group is also deca polyketides and closely related to AFB1 and ST both in structure and biological activity251 also notable is the production of versicolorin C264 which is one of the precursors to ST.

Aspergillus ustus var. pseudodeflectus is very different from A. ustus sensu strictu and produces pergillins, the TMC-120's and the ophibolins all showing various biological activities265 (Appendix 5, Table 5)264,266,267.

However no studies of airborne A. ustus spores or metabolites have been published, and hence the data on airborne AFB1 found in the A. versicolor section is the best when concerning the austocystins.

#### A. niger complex

The Aspergillus section Nigri, found in the subgenus Circumdati, is also called the Black Aspergilli, and contains 9 species: A. heteromorphus, A. ellipticus, A. carbonarious, A. niger, A. bubingensis, A. brasiliensis, A. japonicus, A. carbonarious and A. aculeatus268.

The literature review on metabolites deals with the first 6 species, as they are very difficult to differentiate and seem to produce very similar metabolites (J.C. Frisvad, personal communication), and can be seen in Appendix B, Table 6.

When a Niger is found in buildings, there are usually significant quantities of biomass but it is not that common that a full overview of its preferred materials has been established.

Extracts of A. niger generally contains significant quantities of the low toxic269 tetra-cyclic compounds and naphtho-γ-pyrones 72, but the distribution of strains producing the highly cytotoxic malformins270 not known. This together with the low number of isolates which actually produces the highly nephrotoxic component ochratoxin A, makes a this a species which could pose a significant indoor problems if these two latter types of metabolites are produced in buildings.

#### Other aspergillii

A number of other aspergillii are also found in buildings especially the teleomorph Eurotium repens de Bary (A. glaucus group in Raper & Fennell245), often isolated from wood containing products and in roof construction which are getting very hot during the day. Eurotium is not recognised as a mycotoxin-producing genus72, but has however never been tested for their inhalation toxicity. Many of them can grow at 37°C and may cause infections in immunosuppressed persons.

A. ochraceus is relatively rare in buildings, but in a household with indoor air problems, growth of A. ochraceus was found, and subsequently ochratoxin A was detected in dust using several highly selective analytical methods271. This means that growth of this species in a building should be considered a very serious problem.

Two studies272 have both shown that A. flavus does not produce aflatoxins when growing on different building materials.  The isolates used with both studies were capable of producing theses toxins on laboratory media272,273. However this species produces a number of other metabolites which many pose a health risk.

A. fumigatus, is commonly found in dust and thus isolated frequently on dusty materials, but rarely found growing on materials25. When cultivated on wood pieces, it produces tremorgenic components274, but the responsible components were not detected. Later, Ren et al272 showed that two isolates capable of producing verruculogen and helvolic acid, failed to produce these when growing on different materials. This species is the most common infectious moulds, growing in the lungs of immunosuppressed persons.

### Penicillium

The genus of Penicillium Link ex Fr. is one of the anamorph genera placed in the family Trichocomaceae. It is associated to the holomorph genera, Eupenicillium and Talaromyces275. In the last 10-15 years, the use of secondary metabolite profiles, isoenzyme patterns, and genetic approaches have drastically altered the taxonomy of this genus, previously classified on the basis of morphology. At present 225 accepted species exist in Penicillium. These include approx. 3 times as many synonymisized species275, reflecting the difficulties experienced when identifying and classifying Penicillium species.

Especially the terverticillate penicillia are difficult to identify to species level as they are very closely related, and secondary metabolite profiling seems to be most precies276. Unfortunately misidentification of production cultures has obscured the connection between species and secondary metabolites69,277,278.

#### P. chrysogenum

Penicillium chrysogenum Thom, is placed the series Chrysogena Raper & Thom ex Stolk & Samson279 in the subgenus Penicillium.

P. chrysogenum has 16 synonomised species279:

| P. griseoroseum Dierckx P. brunneorubrum Dierckx P. citreoroseum Dierckx, P. baculatum Westling P. notatum Westling P. meleagrinum Biourge P. flavidomarginatum Biourge | P. cyaneofulvum Biourge P. roseocitreum Biourge P. rubens Biourge P. camerunense Heim apud Heim P. chrysogenum var. brevisterigma Romankova P. harmonense Baghdadi P. verrucosum var. cyclopium strain ananas-olens Ramire |
| --- | --- |

P. chrysogenum is found in dry habitats and can grow at temperatures as low as 5°C280. It is known to produce a large number of metabolites especially antibacterial as shown in Table 7 in Appendix B. However, this also reflects the many screening projects including this species due to its original production of penicillin. The most toxic metabolites isolated have been the neurotoxic roquefortine C but it may also produced Secalonic acid D182,281-283 which is produced by the closely related P. oxalicum, (J.C. Frisvad, personal communication).

PR-toxin have been reported from this species by Frisvad & Filtenborg284 and by Dai et al285, but these findings are still discussed (J.C. Frisvad, personal communication).

An inflammatory mediator may be present in the spores, as methanol extracted spores were non active compared with non-extracted spores152.

#### P. brevicompactum

Penicillium brevicompactum Dierckx275 is now placed in the series Olsonii279 in the subgenus Penicillium. It is common on wood, some fruits, tropical soil and can grow at a lower aw than other penicillia130,279.

P. brevicompactum has 9 synonomised species279:

| P. griseobrunneum Dierckx P. stolenifererum Thom P. tabescens Westling P. szaferi K.M. Zalessky P. hagemiii K.M. Zalessky | P. biolowiezense K.M. Zalessky P. patris-meii K.M. Zalessky P. brunneostoloiferum Abe P. brunneostoloiferum Abe ex Ramirez |
| --- | --- |

As seen from Table 8 in Appendix B, this fungus is capable of producing a high number of biologically active metabolites, from which mycophenolic acid is the most well known and most consistently produced278,286. This component was the first mould metabolite to be purified and crystallised, as early as in 1893287. It is being used as both an antibacterial and immunosuppressant drug. The most toxic component is the genotoxic botryodiploidin288-290, but it has not been proofed it this has been the principle component for a number of mycotoxicosis cases where this species has been the primary contaminant (J.C. Frisvad, personal communication). However most of the biologically active components seem to be able to interact with the growth of plants291-293.

#### P. polonicum

Penicillium polonicum K.M. Zalessky also found in the subgenus Penicillium, but the series Viridicata, some times refereed to as the Penicillium aurantiogriseum complex. The series are generally found on cereals and produces a high number of secondary metabolites279.

P. polonium has 2 synonomised species:

| P. aurantigriseum var. polonicum (K.M. Zalessky) Frisvad | P. carneolutescens G. Smidth |
| --- | --- |

Some of the most toxic Penicillium species are found in the aurantiogriseum complex, but it is extremely difficult to distinguish the individual species by other means than metabolite profiling. Consequently literature has been obscured especially in this complex and the literature review will mostly be based on the paper of Frisvad & Lund294,295, and can be seen in Table 9, Appendix B.

P. polonicum produces at least the groups of highly toxic components, the verrucosidins296 who are tremorgenic, the cytotoxic penicillic acid, which is extremely active against rodent lung macrophages (in vitro)297, and nephrotoxic glycopeptides which may be involved in the Balkan nephropathy endemic 298.

#### P. expansum

P. expansum is occupationally isolated in buildings, where it is often isolated from wood70. On this substrate, Land and Hult299 showed that some P. expansum could produce patulin. This mycotoxin is one of the most toxic Penicillium metabolites, being very highly cytotoxic and has a high inhibitory effect on the activity of mouse peritoneal macrophages300, as well as increases the susceptibility of fungal and bacterial infections219.

However on agar substrates this species produces patulin, citrinin, chaetoglobosin C, roquefortine C, and the communisins A and B, one of the most toxic mixtures in this genus72.

### Trichoderma

Trichoderma Pers. ex Fr. is common on water-damaged wood containing materials, and from Danish buildings six different species have been isolated: T. longibrachiatum, T. harzianum, T. citrinoviride, T. atroviride, T. viride and T. harmatum78.

Trichoderma was originally known for producing trichodermin and trichodermol which was originally isolated from a T. viride strain, and crystallised for the X-ray structure determination as the first TR by Godtfredsen & Vangedal301,302. Later another ester, Harzianum A, of trichodermol has been isolated303. As trichodermol and esters of it are not commercially available, very few surveys for these metabolites have been performed, probably also due to its very low toxicity.

Cvetnic & Pepelnjak304 have reported the production of DAS from T. viride using TLC, but it has not been possible to obtain any of the strains, for verification of this very unlikely finding.

As seen in Appendix B, Table 10, the majority of the non-peptabol metabolites seems to be antibiotic and especially antifungal, and a large number of these seem to be small pyrones and lactones (<300 g/mol) often being volatile. Production of gliotoxin and viridin have also been reported from several Trichoderma species, but these have always been shown to be T. virens305 which has not been found in mouldy buildings72.

The major group of biologically active metabolites are the peptabols, and cyclic peptides, Appendix B, Table 11, who often works by making pores in the cell membranes of the target organisms giving free passage of ions over the cell membrane. These metabolites have both antibacterial, and antifungal properties, but few reports exists of their effect on mammalian cells as most of the work on Trichoderma has been done to identify new antibacterial, and antifungal components. A number of proteins with severe biological properties ribosome inactivation306 and high toxicity307,308 have also been described.

No studies on the inhalation toxicity of these species or their peptabols exist, but they may be significantly more potent when inhaled.

### Memnoniella

Only one species from the genus Memnoniella Höhnel has been identified in buildings and that is M. echinata Galloway, which is closely related to Stachybotrys185,309. As seen in Appendix B, Table 12, a number of biosynthetic groups are produced by this species. The griseofulvins which is a known type of antibiotics45 and are commercially used as such, can inhibit the polymerisation of turbulin in mammalian cells182.

Two mycophenolic acid analogues; memnoconol and memnoconone310 have also been isolated along with a number of spiriocyclic drimanes very similar to the ones produced by S. chartarum229,310-313 also the production of the simple trichothecenes; trichodermol and trichodermin are common with Stachybotrys314.

### Alternaria

The genus of Alternaria Nees ex Fr. comprises more than 40 species280 and is very common in soil and the phylloplane species A. alternata and A. tenuissima are found in very high numbers in the outdoors air during the summer25.  The toxicology of the Alternaria toxins have been reviewed thoroughly by Woody & Chu315. The acute toxicity (LD50) in rodents of alternariols seems to be in the range of 400 mg/kg, which is quite low even though they are reported teratogenic at 10 lower levels. They are mutagenic in the Ames test, but only few data in higher animals exists. Tenuazonic acid (LD50 10-200 mg/kg in rodents) is more toxic and the altertoxins are about 1000 more toxic (LD50, 200 µg/kg in rodents). In Appendix B, Table 13 the biologically active metabolites of this groups have been compiled. It should be noted that A. alternata in grains may to be associated to esophageal-canser in China.

The most potent mycotoxins produced by this genus, are the AAL toxins which are related to the fumonisins316-321 Alternaria alternata f.sp. lycopersici infecting tomato plants, but these strains have not been linked to buildings.

Ren et al 322 showed that only alternariols were produced on various building materials, whereas the altertoxins were not produced in detectable quantities.

However if species of this genus should be the cause of the health problems observed in mouldy buildings, very different metabolites should be produced selectively in buildings,

### Chaetomium

The teleomorph genus of Chaetomium Kunze ex Fr. comprises about 160-180 species280 and has the genus of Acremonium Link ex Fr. as anamorph genus.

The genus one of the most important deteriorators of cotton and cellulose containing materials280 and in buildings C. globosum Kunze ex Steud. is the most common species16.

C. globosum is  known from the cytohalasin mycotoxins, which are also produced by several Penicillium species, and who inhibit cytoplasmatic cleavage, and inhibit glucose transport in the tissue182. However the knowledge of toxicity of these components during inhalation is not known.

The major work done on the metabolites has been performed in Japan323, but as seen in Tabel 14 from Appendix B, many other metabolites are produced by species of the genus, especially the highly cytotoxic chaetomin which inhibits protein synthesis, the cytotoxic chaetocins, the mutagenic mollicellins and the chaetochromins who are cytotoxic, teratogenic and induces liver injuries324.

Interestingly some species also produce sterigmatocystins325 but these species have not been found in buildings.

### Cladosporium

Cladosporium Link ex Fr. is a phylloplane genus and during the summer there can be as many as 10 000 spores per. m3 air of C. cladosporioides and C. herbarum25, and both contains many of the same allergenic proteins326.

On indoor surfaces C. sphaerospermum Penz. and some times also C. herbarum (Pers.) Link ex Gray is frequently isolated from bathrooms and silicone caulkings11,25.

As seen in Appendix B, Table 15 no papers on real mycotoxins have been found from this genus, but a number of antifungal metabolites have been isolated along with a few plant growth inhibitors.

### Ulocladium

The genus of Ulocladium (Thüm.) Simmons is often isolated from water-damaged materials together with Stachybotrys, and generally it is Ulocladium chartarum and U. atrum which are two commonly species of this genus in buildings16,70.

Although this genus is morphologically similar to Alternaria and share the same major-allergen, almost no secondary metabolites have been isolated as seen in Table 16 in Appendix B.

### Paecilomyces

From the genus Paecilomyces Bain. two species are found in water damaged buildings, P. variotii Bain. and P. lilacinus (Thom) Samson, with the first being the most abundant.

P. variotii is capable of growing on very low nutrient substrates as optical lenses, whereas P. lilacinus seems to prefer protein rich media280.

P. variotii can produce the strongly cytotoxic mycotoxins patulin and viriditoxin72 as well the metabolites: ferrirubin, variotin, fusigen and indole-3-acetic acid25.

## Biomarkers of mould growth

As earlier mentioned, not all spores are viable and hence a number of methods for measuring chemical and molecular biological markers are needed. These methods can also provide much faster measurements for mould determination and significantly better quantification. For determination of moulds, four different principles can be used for material samples or air filters:

- Determination of the activity of fungal enzymes. Here two methods have been used: i) Fluorescein diacetate hydrolytic activity (by determining fluorescein) will both detect the presence of bacteria and/or moulds in wooden samples131,327; ii) Determination of the activity of (-N-acetylglucosaminidase328 which is now commercially available as the Mycometer TestTM. Both methods have the advantage that the samples can be incubated for as long time as wanted, and hence a very high sensitivity can be obtained as many molecules of reactant can be obtained from each enzyme molecule. However these methods only detect functional enzymes.

- Chemical markers, which can be genus, species, or isolate specific. These include: i) extracellular polysaccharides from Penicillium and Aspergillus30,329;ii) 18:2(-phosphorlipid fatty acids328;iii) β-glucan from the cell wall, also being an important inflammatory marker38,40; iv) mycotoxins or secondary metabolites who are species specific48; v) MVOC's in the air42,330; vi) chitin from the cell wall 331; and finally the cell membrane material ergosterol 332,333. All these metabolites can principally be detected using various analytical methods as described for metabolites in section 2.6.

- PCR-based methods, detecting specific parts of the fungal DNA, enabling even isolate recondition if needed, and also recently quantitation235. These methods will undoubtedly be very important in the future especially when the DNA-chip technology comes down in price.

- Bioassay detection, either by detection cytotoxicity334,335 or more specific mode of action, as the protein translation inhibition which is highly selective against trichothecenes336. Such methods give health relevant data but do not give any information on the producing mould.

All these methods are significantly faster than cultivation techniques and can also detect dead spores and mycelia, and will be the predominant methods in the future.

### Ergosterol

# Ergosterol (Erg) is the predominant compound in the fungal cell membrane, making it a suitable indicator for fungal growth, although it should be noted that also some amoebae and green algae are capable of producing Erg337.

Erg is partially bound as different esters338, and thus three different extractions can be performed: Free Erg, extracted without saponification; Total free Erg by saponification of the esters after extraction; and Total Erg by saponification of the sample during extraction339-341,341-344. In plant tissue extraction has shown some matrix dependency due to instability of Erg under various conditions, as exposure to sunlight or low pH341,342,345.

Extraction has included reflux in methanol- water with or without NaOH/KOH for 30-90 min, generally being labour intensive compared with the microwave-assisted extraction for total Erg developed by Young344 and the extraction method of Larsson and co-workers332,346,347. These methods have been able to detect quantities down to 500 pg, corresponding to 200 spores88,95.

Erg is an excellent marker for quantification of fungal biomass on building materials332,348 and can also be used as exposure marker in air or dust, where especially Larsson et al 346,349 and Miller et al22,88,95,350 have used it. However here it was found not to correlate with questionnaire data on mould in the home and not with as self-reported symptoms88.

## Detection of fungal metabolites

Although perhaps more than half the time of the present work has been spent on developing analytical methods and trouble shooting on instruments, this subchapter will only give an overview of the analytical methods, as a more detailed literature review can be found in the papers 1-13.

### Chromatographic methods for detection of mycotoxins

Fungal metabolites can be detected by various methods, often combined with chromatographic methods351,352.

#### Thin layer chromatography

Thin layer chromatography (TLC) is the oldest of the chromatographic method, and requires less expensive and advanced equipment than the other chromatographic methods284 and a considerable sample speed can be achieved compared with other methods, unless 2-D TLC is used351,353.

Target components can after separation be detected visually or instrumentally under light or under UV-light, the latter being very sensitive to fluorescent components. Usually the target components can be more or less selectively coloured by spraying with various reagents284,351. Biologically active components can be found by spraying the plate with a suspension of microorganisms in a growth substrate and after incubation for some days spots with no growth can be detected.

Mass spectrometric methods such as MALDI-TOF and FAB-MS can also be used as detection methods of TLC353 although it seems more troublesome and slower than LC-MS and will probably only be used for very special applications.

TLC is not specific enough for detection of TR354 although a number of "selective" colouring methods have been published355-359.

For sterigmatocystins, spraying with AlCl3 is considered quite specific when combined with sample preparation methods removing quinones and related components360.

#### Gas chromatography

As previously mentioned, mycotoxins are generally not volatile and hence gas chromatographic detection of them will always have to face instability problems during injection and chromatography361. On the other hand capillary GC gives 10-100 times higher separation power362 than LC (packed column) and runs very stable with flame ionisation, electron capture detection (ECD), and MS, which are significantly more sensitive than UV and refraction index detectors used in LC.

Almost all GC methods for mycotoxins start with derivatisation of free OH and N-H groups363 to decrease the thermal lability. Acid groups are usually methylated, and alcohol groups are reacted to their TMS ether or esterficied to their acetyl or pentafluoropropionyl esters354,361.

GC methods on most mycotoxins have been published, inter alia AFB1 and ST363, Alternaria mycotoxins364, penicillic acid365, patulin366,  and especially the TR354. The latter, is the only group where GC-MS or GC-ECD has been the primary analytical method.367-381.

##### GC-MS for trichothecenes

The use of MS detection of the pentafluoropropionyl- (PFP) or heptafluorobuturyl (HPB) esters will give the highest sensitivity if the MS has a mass range > m/z 800354. These derivatives can be formed by the imidazoles PFPI and HFBI respectively or acid anhydrides PFPA and HFBA respectively, although the latter needs a nucleophilic catalyst such as triethylamine, dimethylaminopyridin or imidazole354. Unfortunately the TB react slowly with both types of reagents and can undergo isomerisation giving more than one peak368.  The fluorinated derivatives can be detected selectively to very low levels using negative ion chemical ionisation (NICI)-MS or ECD, but also positive electron impact ionisation (EI+)-MS or positive chemical ionisation (PCI)-MS can been used370,376,382-385.

TR lacking free OH groups cannot be detected using NICI and ECD unless they are hydrolysed to their parent alcohols prior to derivatisation369,376.

##### GC-MS for sterols

GC-MS has also been used, usually based on an internal standard, such as cholesterol or dehydrocholesterol349,386, as a isotope substituted standard is not commercially available. Erg has usually been derivatised to its tertiary-butyldimethylsilyl or trimethylsilyl (TMS) ether to reduce decomposition during injection and chromatography. On-column injection can also be used to further reduce decomposition344, but this method requires cleaner samples and is not as robust as splitless injection386.

#### High performance liquid chromatography

Since the late 1980s and the start of the 1990s HPLC have been the most important analytical method for mycotoxins351,387-391.

The success of HPLC compared with the other methods have several reasons. Firstly the instruments have decreased in price as well as getting easier to maintain. They are easily automated and PCs can sample and do automated detection of target compounds. Many column materials are available from many different manufactures, and significantly larger samples can be injected than in a GC. More over samples do generally not demand derivatisation as GC does.

From the mid 1990s the use of HPLC with MS detection employing atmospheric pressure ionisation techniques (API)392 such as electrospray393-395 and atmospheric pressure chemical ionisation (APCI) have greatly expanded the use of HPLC for mycotoxins393,396-398. As toxins previously transparent to UV detectors can now be detected, e.g. the fumonisins which previously needed OPA derivatisation394,399, small peptides400,401,  and especially the TR396.

#### Capillary electrophoresis

Capillary electrophoresis (CE) has been used for detection of mycotoxins and low molecular-mass compounds since the late 1990s, due to the extreme separation power exceeding capillary GC by several magnitudes, as well as providing very fast separation395,402,403.

The method has, however, a number of limitations as uncharged components cannot be separated unless micellar CE is being used which greatly lowers its separation power404. The very small sample volume (<<1 µl) which can be loaded on to the column gives detection-limit problems even though several pre-concentration methods exists403,405. This means that CE is still generally used with very sensitive detectors such as Laser-Induced Fluorescence detection406,407. CE-MS methods have been used for low molecular-mass compounds but it has not yet been possible to use it in combination with micellar CE392,392,395.

#### Immunochemical methods

For routine analysis, enzyme linked immunoassay (ELISA) is used for detection of AFB1, the TB DON, ochratoxin A and zeralenone in cereals408-410.

An increasingly important and very specific technique is to combine chromatographic detection methods with immunoaffinity clean-up411.

Monoclonal antibodies have also been prepared for the TB 3- and 15-acetyl-DON412,413, sporidesmin A414, the MTR roridin A415, the TA DAS416 417 and presumable a number of other mycotoxins.

A roridin A ELISA has been used to detect SG and SH in building material samples334, as the assay cross-reacts with SG (4-7%) and SH (15-19%)415,417. Also the MTR hydrolysis product verrucarol, was detected in serum using DAS-ELISA samples after it was derivatised to diacetyl-verrucarol which is structurally similar to DAS.

#### Bioassay for detection of mycotoxins

The first assays for measuring Stachybotrys toxins, were rabbit skin test which later have been shown to be highly sensitive for TR73,194,418. However due to ethical reasons this method is not used any more, as in vitro cultivated cell lines of human or animal origin can provide the same sensitivity and specificity335. Cell cultures are the most common assay for cytotoxicity testing, and have been very successful for detection of the cytotoxic trichothecenes20,335,419 and cytotoxic indoor air organisms154,155. It should be noted that great differences in sensitivity and specificity of different cell types exist335. Most of the methods are used in combination with the MTT test, which measures if the mitochondria are functioning using a simple colormetric detection335,420. The cell assays can also be used for measuring other reactions than cytotoxicity, e.g. induction of inflammatory mediators such as NO and different interleukins158,421.

The major problem with mammalian cell cultures is the need for cultivation in highly sterile environments and frequent sub-cultivation which is very time and material-consuming. Hence a more simple solution can be used, e.g. sperm cells54,422-424 who are available from local insemination centres, blood cells which can assayed for heamolysis235 and/or rings from chicken trachea where the movement of the cilia can be monitored425. A very simples assays is the brine shrimp Arthemia salina190,426 which has been extensively used for TR and other mycotoxins as the aflatoxins426. Engler et al427 used the yeast Kluyveromyces marxianus grown in microtitre plates for detection of TR by monitoring its expression of β-galactosidase.

An assay measuring protein translation inhibition have been reported by Yike et al336. This assay has detection limits 20-400 times lower than cell cultures.

### Sample preparation

The most time-consuming part of analysing for mycotoxins and other fungal metabolites, is extraction and especially the sample clean-up.

#### Trichothecenes

TR range from polar compounds like nivalenol (NIV) extracted with methanol-water or acetonitril-water mixtures to apolar compounds such as diacetoxyscirpentriol (DAS) and T-2 toxin (T-2) extracted with mixtures of chloroform, dichloromethane and ethyl acetate. Thus no method can provide full extraction (≈ > 80%) of all TR unless multiple extractions are performed 354.

The MTR can be extracted using water-methanol to dichloromethane-methanol mixtures, but the first mixture should extract fewer interfering components428.

At least one solid phase extraction (SPE) step has to be included before the TR can be detected. Most successful are normal phases, such as silica gel, florisil, charcoal-alumina or MycoSep columns354,375. Reversed phase has also been published367,429 but due to the large difference in polarity of the TR and the time-consuming evaporation of water these methods have not been as popular as the normal phase ones. For the MTR the PEI silica has proven to be superior, as it selectively removes the spiriocyclic drimanes, phenolic compounds and the brownish gum always present in extracts from Stachybotrys428,430.

For the polar TB immunoaffinity clean-up is also widely used, as they are soluble in the water-acetonitrile mixtures used for loading immunoaffinity columns354,413, and can be detected using HPLC with UV detection.

### Detection of mycotoxins in air and settled dust

To estimate the human exposure to mycotoxins, these have to be measured and quantified directly in air samples or in settled dust. But as spores and airborne dust contain interfering components and the spore concentration is very low 431(usually << 5000 m-3), detection of airborne mycotoxins will be very difficult due to the very low quantities. Until now, airborne mycotoxins have only been detected in environments with high concentrations of airborne spores, such as the agricultural industry and the feed-handling industry. Here several studies have demonstrated airborne AFB1 when handling materials infested with A. flavus32,432.

Richard et al271 detected ochratoxin A in dust from a dwelling with growth of A. ochraceus, using LC-MS and HPLC-FLD from samples cleaned up using immunoaffinity clean-up.

Sorenson47 showed that spores released from a S. chartarum isolates growing on rice, contained ≈ 4×10-14 g MTR per spore, meaning that about 1500 spores (450 spores using the data of Nikulin et al46) should be collected, if assuming 80% extraction efficiency and 50 pg detection limit in sample, however as there are different MTR present (unless they are hydrolysed to verrucarol) and rice and MEA are good substrate for MTR production significant more spores may be needed.

Smoragiewicz et al433,434 reported that dust from a ventilation system contained the TR roridin A, T-2 tetraol, T-2 toxin, and DAS. They also reported TR from cultures of the non-TR producing genera Penicillium, Aspergillus, Alternaria, and Ulocladium, which demonstrates that all their results must be false positives.

Yike et al235,336 demonstrated that dust and air samples from houses infested with S. chartarum inhibited their protein translation assay, which strongly suggested the presence of trichothecenes in the air.

To conclude it should be possible to detect mycotoxins in air samples, but no validated sampling and clean-up procedures exist, meaning that this major problem has to be addressed first.

# Overview of experimental work

The details of the experiments performed during this study can be found in the papers 1-13. However results of a number of small experiments not included in the papers can be found in the discussion part and identification of components initially reported as unknown.

Figure ¡Error! Argumento de modificador desconocido.. Overview of experimental work.

# Results and discussion

## The building associated funga

As mentioned in paragraph ¡Error! Argumento de modificador desconocido. the associated funga reported from different countries varies considerably. Unfortunately this study has not analysed field samples enough to make definite conclusions on this issue. However a number of observations are still interesting:

- It was not possible to get any material samples with Alternaria infestation, all were instead infested with Ulocladium. Although > 15 field samples which should contain Alternaria were received).

- Almost all (>50%) of the material samples received were at least partly infested with P. chrysogenum and A. versicolor, although the presence of the latter could only be revealed by chemical detection of sterigmatocystin (ST), see section 4.3.2.1, page 45.

- When Trichoderma spp. or Chaetomium spp. were present on a material they grew in almost pure culture and with significant biomass.

### Penicillium and Aspergillus cultures received from Finland

A number of Aspergillus and Penicillium isolates collected from both material and air samples were received from National Public Health Institute, Kuopio, Finland (KTL). They were cultivated on YES, CYA, CREA and MEA and identified by colony diameter and morphology. Isolates that could not be unquestionably identified were metabolite-profiled by HPLC-DAD (YEA and CYA).

| Table ¡Error! Argumento de modificador desconocido. Aspergillus and Penicillium isolates (n=131) received from KTL1 |
| --- |
| Species | Frequency (%) | Species | Frequency (%) | Species | Frequency (%) |
| Aspergillus versicolor | 23 | P. citreonigrum | 3 | Penicillium charlesii | 1 |
| Penicillium brevicompactum | 11 | Aspergillus ustus2 | 2 | Penicillium commune | 1 |
| Aspergillus fumigatus | 10 | Penicillium crustosum | 2 | Penicillium echnilatum | 1 |
| Penicillium corylophilum | 5 | Penicillium solitum | 2 | Penicillium janczewskii | 1 |
| Aspergillus sydowii | 5 | Aspergillus niger3 | 2 | Penicillium manginii | 1 |
| Eurotium repens | 5 | Penicillium decumbens | 2 | Penicillium purpugenum | 1 |
| Penicillium chrysogenum | 5 | Penicillium expansum | 2 | Penicillium rosepurureum | 1 |
| Penicillium palitans | 5 | Penicillium rugulosum | 2 | Penicillium variabel | 1 |
| Penicillium glabrum | 4 | Aspergillus flavus | 1 | Penicillium vinaceum | 1 |
| Penicillium italicum | 4 | Penicillium albocoremium | 1 |  |  |

1From Anne Hyvärinen, National Public Health Institute, Kuopio, Finland. 2Not a classic A. ustus but Aspergillus ustus var. pseudodeflectus. 3Did not produce detectable quantities (HPLC-FLD) ochratoxin A on CYA or YES agar.

As seen in ¡Error! Argumento de modificador desconocido., A. versicolor was the most predominant mould almost contributing with 25% of the isolates and more than 50% of all aspergillii. Surprisingly A. fumigatus was very frequently isolated (10%) which might be due to sampling on dusty surfaces, as A. fumigatus is frequently recorded in Danish house dust (S. Gravesen, personal communication).

P. brevicompactum was the most frequently isolated Penicillium, confirming results from the on-going Danish School study, where P. brevicompactum, P. corylophilum and P. chrysogenum were the most common penicillia.

# These results contradict results from North America, reporting P. aurantiogriseum and P. viridicatum as the most abundant Penicillium species. This might be due to misidentification with P. palitans and other species from the aurantiogriseum-complex (J.C. Frisvad, personal communication), but unfortunately it has not been possible to obtain any of these Penicillium isolates to verify the identification.

## Fungal growth on materials

In papers 2 and 3, material samples were water-damaged (aw ≈ 1) and significantly higher number of spores were applied to the materials than naturally found in buildings. The moulds were usually able to cover the materials where they occur "naturally" within 4-10 days, clearly demonstrating that when water damages occur, action should be taken the same day if materials should be saved. This also complies with observations by several consultant engineers (M. Ø. Hansen, personal communication), who report complains from the inhabitants within 10-30 days after a single water damage, and complaints within 2-4 days in buildings with a known water damage history.

When using lower aw (papers 10 and 13) the growth rate decreased dramatically and with very few exceptions only the primary and secondary colonisers were observed growing on the materials. At stationary conditions (paper 10), only Penicillium and Aspergillus species grew, with P. chrysogenum and A. versicolor being the most common species. However on wooden materials A. flavus and Eurotium spp. were observed quite frequently and always with significant biomass. At 5°C only P. chrysogenum and A. versicolor grew, with the latter producing conidiophores with very few conidia.

Figure ¡Error! Argumento de modificador desconocido.. Concrete after 4 months at 95% RH and 10°C, at #1 can A. versicolor conidiophores be seen and at #2 sterile mycelia.

Wooden and wallpapered materials supported growth down to 78% RH (paper 10), which was lower than the other materials. It was seen that the planned pinewood  was usually not infested on as much of the surface as the rough materials, but on the areas where growth occurred there was not significant difference in the produced biomass. At 5°C this limit was about 90% RH, whereas the results only indicates a limit between 80 and 90% RH. These results comply perfectly with the results of Hukka & Viitanen147 and Grant et al61, when the uncertainties of the RH measurements of both studies (±2%) are taken into account.

Interestingly, the gypsum boards did not support growth <90% RH, but did support production of significant quantities of biomass at 95% RH, it is also clear that the fibre-gypsum was less susceptible than the cardboard-gypsum, which is the most common type in Denmark. Paper insulation material did not support fungal growth at all due to the high contents of borates, although it should be noted that this material when damaged supports growth of several moulds including Stachybotrys (unpublished results). The almost totally inorganic concrete materials partly supported germination of especially A. versicolor and sterilia mycelia at RH >90% and growth at 95%, as seen in Figure ¡Error! Argumento de modificador desconocido.. This must be due to trace quantities of organic components in the concrete. As the concrete materials were cleaner than the ones used in buildings concrete based materials will probably support more growth under field conditions (paper 10).

When comparing Tables 2 and 3, it is clear that the temperature drop from 10 to 5°C had a dramatic effect on the fungal growth, showing no growth at 90% RH and 5°C, and that also here was wooden and the wallpapered materials the most susceptible (paper 10).

### Methods for testing the susceptibility of materials

Figure ¡Error! Argumento de modificador desconocido.. The fungal growth assesment set-up used in Paper 10.

Figure ¡Error! Argumento de modificador desconocido.. The TNO set-up, 10 material in each row. In this case infested with P. chrysogenum.

As mentioned in the literature part, testing materials for their susceptibility is difficult, even just controlling the humidity is difficult. As this was the first time such a test was performed at the Danish Building Research Institute, it was tried to keep the set-up as simple as possible (paper 10), and regard the study as a pilot project which should explore difficulties such as humidity range, inoculation, and especially assessment of the materials. This set-up is shown in Figure ¡Error! Argumento de modificador desconocido., and was primarily built by Gunnar Holm. Initial conditions may play an important role for the surface aw of the materials, and as it was desired to use steel chamber and take the materials out for assesment, it was necessary to use the sample boxes for reasons occupational health. This meant that the surface aw would be controlled by the RH of the incoming air to the sample box and primarily by the absorbance of water by the material until equilibrium, which small experiments had showed would take months. This meant that we had to add the quantity of liquid water to the materials, assuming that it would be equally distributed within a few days. Although this should tested in future experiments.

I paper 13, the set-up at TNO Bouw was used, and the initial humidity was controlled by a high continuous airflow over the materials (see Figure ¡Error! Argumento de modificador desconocido.). This means that the absorption of water from the airflow was so little that the change in humidity over the 10 materials in each channel could be neglected. However this approach created another problem as the air speed itself can inhibits growth if the speed is too high. This is illustrated in Figure ¡Error! Argumento de modificador desconocido., where the air speed was higher in one side of the channel than in the other.

The TNO approach (paper 13) had another advantage, as it is possible to work with transient humidity conditions, and here it was seen that the stress of using periods of high and low humidity during a day, trying to mimic a bathroom. This had a strong selectivity stress towards the phylloplane, Cladosporium, which under transient conditions was able to outgrow P. chrysogenum.

Figure ¡Error! Argumento de modificador desconocido.. The influence of to high air velocity on A. versicolor growth in one side of the set-up.

The instationary conditions, with and without surface condensation (paper 13), can cope with conditions which keeps the storage moulds away and still be too dry for the phylloplane. It can also cope with water accumulation in the surface of materials, especially when working with two to three layer systems, like a painted piece of cardboard gypsum (3-layer system)11.

Hence, the total growth behaviour of materials is extremely complicated, and to characterise a material well, the performance and associated funga under at least three different environmental conditions is needed:

- The lowest RH which supports growth.

- The performance under transient conditions.

- The performance under water damage.

### Growth assesment

In paper 10, the materials had to be taken out of the set-up for assesment. This was very time consuming and obscured the environmental conditions for the samples. Using the approach of Adan11 as in Paper 13 (see Figure ¡Error! Argumento de modificador desconocido.), the materials can be assessed several times a day if required. The time resolution of this process describes the susceptibility - as how fast growth started - better than endpoint determinations of biomass. The latter parameter seems to describes how much of the substrate could be utilised (papers 10 and 13).

Visual inspection (paper 13) has a major problem, especially using the 5 point scale described by British Standard435, as the assessed coverage area is the output parameter. This does not take the concentration of fungal biomass into account. Thus a material with very light coverage over all of the material will be assessed to have a higher value than a material with heavy growth over only a part of the material.

Figure ¡Error! Argumento de modificador desconocido.. Mixture of A. flavus, A. versicolor and P. chrysogenum, growing on pinewood.

The use of image analysis was partly explored at the stay at TNO Bouw (unpublished), and this technique will undoubtedly help in future studies, as images for assessing the materials can be taken automatically several times a day. It can also cope with the high growth rate observed on some paints (where the materials had to be assessed 2-3 times per day, paper 13). Also a more standardized assessment including the fungal "concentration" can be made. However this will require that the image-analysis is calibrated carefully against very well-described samples. Here chemical markers could help to compare the appearance of different moulds.

The use of dissection microscopy showed that the moulds often grew in mixtures (see Figure ¡Error! Argumento de modificador desconocido.). Looking at materials with scarce growth and a fibrous surface was very difficult, and only sporulation could be detected. However it was possible to distinguish A. versicolor, often seen as white to olive conidiophores with very few spores and P. chrysogenum, often as light bluish or white conidiophores with very long chains of spores attached.

When no sporulation occurred on fibrous materials such as the pinewood or gypsum boards it was only the chemical markers which could detect growth, but in no case significant biomass overlooked.

#### Biological markers

One or both the biological markers ergosterol (Erg) and the Mycometer TestTM were used in papers 5, 10, 12 and 13.

Qualitative determination or Erg was easily performed by the standard HPLC and TLC methods already used at the department, but quantitative determination proved to be painstaking process. External standard quantitation using HPLC or GC-MS proved unreliable, especially using GC-MS where both splitless injection, various ion-trap phenomena, and the breakdown of the GCQ followed by it being rebuilt in USA, complicates things further (paper 5).

All the sterol standards obtained were almost transparent to the HPLC-DAD, leaving GC-MS with internal standard as the only possibility. LC-MS was not available at that time, and will probably not be an alternative, as the low-polar solvents used to elute it will give problems with the ionization process. Several sterols were tried as internal standard for GC-MS, but the high dynamics of the external ionisation ion-trap system did not give better standard deviations (SD) than 25% when working on standards. When using 4-D2-ergosterol as internal standard, synthesised by Dr. J.Ø. Madsen, Erg could be determined with a SD of < 5%, as variation in the ionization and the dynamics of the gate lens is no longer interfering with the analysis.

In paper 5 it was shown that no SPE clean-up step was needed when using GC-MS/MS and that the sample did not need to be neutralised after the saponification when splitless injections was used. Microwave assisted extraction was proven to be a very powerful and fast technique but very dangerous, as the vials occasionally exploded and ripped open the microwave oven door.

As many samples could be hydrolysed in standard laboratory vials at the same time - this method was preferred. It was possible to reach 120 samples per day, although the GC-MS/MS can only analyse 60-65 samples per day. The SD ranged from 1-4% in spiked samples and in real samples SD ranged from 4-12%, with detection limits in the sample of 2-10 ng, which is fully sufficient as the variation of fungal growth on surfaces is much higher.

However during analyses of samples described in papers 10 and 13, this detection limits was difficult to reach and the general limit was 10-30 ng, which is significantly higher than reported in paper 5, which was already higher than reported elsewhere 332,344. One of the major problems was the daughter ion-yield (number of daughter ions / number of the parent ion in the full scan chromatogram), decreased to 4-8% for unknown reasons, compared with a yield of > 50% of the PFP or HFB-trichothecene derivatives. The water and oxygen levels in the system was extremely low, and various q-values, ion-source temperatures and CID voltages were explored as well as alternative tuning of the lenses, but with no increased sensitivity.

Sample decomposition during injection was a particular problem while running the sample described in paper 13, where the painted materials had a dramatic impact on the sensitivity due to deposits in the liner (not visible). In the future such samples should probably, after hydrolysis, be loaded (cold) onto a C18 cartridge which can be cleaned with water-methanol mixtures, before the sterols can be eluted with methanol/dichloromethane, but would compromise sample preparation speed.

In paper 12, the m/ 363 and 365 were used as parent ions and m/z 157 and 159 as daughter ions for Erg and 4-D2-Erg respectively, this combined with newly cleaned ion source assemble and new liners in the GC every 60 injections lowered the detection limit to 1 ng (20 pg injected).

In paper 10, both Erg and the Mycometer Test™ showed growth or no growth, but the correlation was obscured by the high variability of the fungal growth. This problem was overcome in paper 12, where it was shown that the (-N-acetylglucosaminidase activity increases faster than Erg during the initial growth phase, and it decreases slightly (indsæt figur !).

Compared with visual inspection, paper 10, the chemical markers generally showed the same, but were a nice alternative on very fibrous surfaces where even the use of a stereomicroscope gave problems with distinguishing fungal growth from fibres. Erg has the advance of being an absolute method, which can be good for comparing different ratings of mould growth.

The secondary metabolites were very useful species-specific biomarkers, and in papers 3 and 10, significant growth of A. versicolor (see also section ¡Error! Argumento de modificador desconocido., page 45) was hidden by P. chrysogenum.

Metabolites may also indicate how wet the materials have been, e.g. does the presence of the A. versicolor metabolites PE1, XOO and ROQ but not ST, indicates 0.95 > aw > 0.90, whereas ST indicates aw > 0.95 (see section ¡Error! Argumento de modificador desconocido., page 45).

## Growth and metabolite production

In this chapter the most important results of the different moulds and their growth and metabolites production will be discussed.

### Stachybotrys

Figure ¡Error! Argumento de modificador desconocido.. Scarce growth of S. chartarum on a gypsumboard at 95% RH and 10°C after 4 months.

Experimental growth of S. chartarum IBT 7711 could be recognised after 5 days of incubation (paper 2) on new water-damaged (aw ≈ 1) gypsum boards, which is partly due to the high dose of spores (4×103 spores/cm2), but still surprisingly fast. Growth of the other 4 isolates was not as fast, but the gypsum boards were still totally covered with the fungus after 14 days. None of the 5 isolates could grow on chipboard, acoustic ceiling tiles or pinewood pieces.

These findings are in accordance with field observations14 and paper 4 where consistently wet gypsum boards seem to be the main substrate of Stachybotrys in buildings25.

In paper 10 where mixtures of common moulds were inoculated under regulated humidities and temperatures (95-70% RH) Stachybotrys was only found on the three types of gypsum boards when RH ≥95, and here only with very limited production of biomass had occurred, as shown in Figure ¡Error! Argumento de modificador desconocido.. This demonstrates that this species generally require water-damaged materials to produce significant quantities of biomass and compete with the penicillia and aspergillii. This is in accordance with the literature (see Table ¡Error! Argumento de modificador desconocido., p.5) where Stachybotrys is seen to require aw 0.95 or more for growth, although Pasanen et al113,114 have reported growth as low as aw 0.78-0.81 which is highly unlikely. This is presumable due to the 1 ml spore suspension added to very small samples (down to 0.25 g), meaning that aw of the samples would be higher than the RH in the air controlled by the saturated salt solutions for an unknown period.

In paper 10 it was also able to grow at 10°C and 95% RH at gypsum boards, meaning that it should also be able to grow in colder constructions.

#### Analysis for trichothecenes

In papers 1 and 2, GC-MS negative ion chemical ionisation (NICI) was used successfully for detection of the trichothecenes (TR) as it gave excellent matrix suppression compared with EI+ ionization, as illustrated i Figure 2 in paper 2. However, the matrix suppression could also be obtained with more polar extraction mixtures (methanol-water) and more effective removal of acid residues from the derivatised samples. Combined with a number of problems with NICI compared with EI+ (paper 1, 2 and 8) the latter became the preferred as NICI gave the following problems:

- A decrease in sensitivity after 10-15 samples was observed. This could be avoided by changing the ion volume.

- After changing to the turbo pump, it took 1-2 hr to stabilise the ionisation gas.

- The MS got very dirty much quicker and needed to be cleaned every 2-3 months, which is very time consuming.

- Very short lifetime of the filament (1-2 months)

- The high pressure of methane, which was necessary to obtain a high sensitivity and high m/z ions, gave a poor mass resolution of approx. m/z 0.5-1 (10% valley), making automatic data processing very difficult.

- If the method should also be used on the TA from Fusarium, the ion volume temperature should be raised to 120°C to avoid condensation. However this gave almost no high-mass ions (<m/z 300) especially not for the TB.

Figure ¡Error! Argumento de modificador desconocido.. Derivatisation of the trichothecenes.

- The number of ionised molecules is about 10 times as low in NICI as in EI+, meaning than when MS/MS (which looses 10-90% of the ions) was used a significant drop in sensitivity was observed.

In EI+ the daughter ion spectra were significantly more reproducible than the full scan spectra. Thus EI+ ionisation combined with MS/MS (paper 8) was used in all other studies except papers 1 and 2.

In the study of TR produced by Fusarium (paper 8) it was observed that the methods used in papers 1 and 2, could not fully derivatise the type B trichothecenes (TB) and that a number of artefacts were produced. A number of methods using imidazole or acid anhydride based reagents and mixtures of these were tried but none were successful, until the method of Langseth et al419 was applied. This method worked both with PFP and HFB esters, but the PFP was chosen as the HFB gives molecular masses exceeding the upper mass range of the GCQ (m/z 1000).

However this derivatisation method did not work for trichodermol and verrucarol as partly facilitated apotrichothecene rearrangements (ring breakage of the epoxy group)436, so the original method (papers 1 and 2) using HFBI was not changed for these trichothecenes (¡Error! Argumento de modificador desconocido.).

To speed up the hydrolysis step it was tried to pass the hydrolysed sample through a strong cat-ion exchanger for neutralisation of the NaOH428, which worked fine on standards. However with fungal extracts huge quantities of interfering peaks and irreproducible derivatisation were observed, hence the liquid-liquid extraction seems to be a powerful clean-up step.

Figure ¡Error! Argumento de modificador desconocido.. HPLC-DAD chromatograms (260 nm) of Stachybotrys chartarum extracts from PSA agar: a) crude extract (IBT 7711); b) PEI cleaned up extract from a satratoxin producing strain (IBT 7711); c) PEI cleaned up extract from an atranone producer (IBT 9466).

Parallel to changing the GC-MS method to EI+, a clean-up method for HPLC detection was developed to detect the unhydrolysed macrocyclic trichothecenes (MTR). It was clear that reversed phase clean-up was not effective due to the polarity difference between the MTR a problem well known from the simple trichothecenes where normal phase clean-up is the most effective354. Silica and PEI silica (provided by B.B. Jarvis430) were tested, but it was clear that the latter was significantly better to remove the spiriocyclic drimanes. By dry-packing the PEI in syringes between two pieces of filter-support material stamped out by a sharp steel cylinder a SPE-PEI module could be manufactured on less than 30 sec. The dichloromethane sufficient to elute the macrocyclic trichothecenes could then be placed in the RVC (takes 24 vial) and evaporated in 2 hr giving a much higher sample throughput compared with the method of Hinkley & Jarvis428. The effect of cleaning up the extract on the PEI columns is illustrated in Figure ¡Error! Argumento de modificador desconocido., where the HPLC profiles of crude extract is compared with the cleaned up extracts on a MTR and an non-MTR producing S. chartarum on PSA agar.

It was noted that the sample should be totally dry before redissolving it in dichloromethane, as water or methanol traces facilitated the breakthrough of the spiriocyclic drimanes in the dichloromethane fraction.

When trying to fractionate Stachybotrys extracts it was also noted that the dry solvent blanks from the PEI-columns were toxic to the boar sperm used by Peltola et al237 and the human bronchoalveolar cells used by Norn et al437.

To study the ratio between trichodermol and trichodermin in the crude extracts, unhydrolysed crude and PEI cleaned extracts was derivatised and analysed using GC-MS/MS. The PEI clean-up step was necessary to avoid huge quantities of interfering peaks and unreproducible derivatisation. It was also shown that the trichodermol trichothecenes are predominantly present as trichodermin (paper 6-8).

#### Metabolites produced by Stachybotrys

During the first part of study (papers 1 and 2) it was believed that most isolates would produce MTR214. This was, however later shown not to be true, papers 6-9 and Jarvis et al45, as only 30-40% of the isolates produces MTR.

The samples collected in a school and a dwelling (paper 1) both yielded verrucarol upon hydrolysis (up to 15 ng/cm2 SH equivalents) as well as trichodermol (not quantified). When incubating different strains on water-damaged new and old gypsum boards (paper 2), only 2 of 5 isolates yielded high quantities of verrucarol upon hydrolysis (up to 120 ng/cm2 SH equivalents), one isolate produced significantly less MTR. In extracts from the last two isolates verrucarol was perhaps present, but detection could only be performed on the non-specific m/z 213 ion, [HFB-O]-, which was observed from many peaks of the chromatogram.

The satratoxin levels detected (15-120 ng/cm2) are the same as reported by Johanning et al23 who found 33 ng cm-2 satratoxin H in biomass scraped off from a infested building material, but lower than found by Nikulin et al113 who detected 2-3.5 µg/cm2 satratoxins from a highly toxic strain of S. chartarum (isolate #72 = IBT 9460).

Temperature and humidity did not seem to influence the production of the spiriocyclic drimanes (paper 10) when growing on gypsum boards, as these were detected in substantial quantities at 10°C and 95% RH at gypsum boards.

In papers 6, only S. chartarum produced satratoxins G, H and iso-F whereas S. dichroa stopped at roridin E. S. oenanthes produced trichodermol type TR. S. bisbyi, S. albipes, S. microspora S. nilagrica S. parvispora, S. theobromae, and S. cylindrospora did not produce any detectable quantities of TR. The latter species has been reported to produce trichodermol and trichodermin438 and El-Maghraby et al439 have reported that S. albipes, S. kampalensis and S. microspora produced MTR. Unfortunately these strains are not available in any culture collection. However as only 1-3 strains of each species were tested, the study is not big enough for major conclusions on these rare species, as it should also be noted that only ALK and PSA were used for these species.

In paper 6 and 8 it was observed that the strains capable of producing MTR did this on all solid substrates tested (CMA, V8, YES, PSA, OAT, PSA, DRYES, ALK, CYA and rice extracts agar), with PSA and ALK agar yielding the highest quantities. On the latter agar, enhanced production of stachybotrylactone and lactams was observed, often more than 20 different components with the UV spectra illustrated in Figure ¡Error! Argumento de modificador desconocido., A. As these components are the main interfering components (removed by the PEI silica SPE clean-up), PSA agar was chosen as the standard substrate for chemotaxonomic studies of S. chartarum.

The rich substrates CYA and YES, where high quantities of biomass was produced, yielded surprisingly low quantities of MTR together with CMA, V8, OAT and rice extract agar. The low quantities of MTR produced on the latter substrate is surprising since whole rice is a very good substrate used extensively by Jarvis and co-workers45,210,314.

The construction cardboard used in study 12 gave approx. as much of the MTR per area as PSA agar.

Three taxa was found among the isolates from buildings (paper 6): i) the MTR producing S. chartarum isolates; ii) the non MTR producing S. chartarum isolates; iii) a new undescribed species, referred to as Stachybotrys sp. type A.

The latter taxa did not show PCR amplification of the TR5 gene (paper 7) and did not produce detectable quantities of trichodermol. However this was not the same in paper 6, where 25% of the Type A isolates produced trichodermol or esters of it, which was also confirmed in paper 8, where trichodermol and trichodiene was detected from the type A isolate.

Figure ¡Error! Argumento de modificador desconocido.. Positive ESI spectra of Epoxydolabellane A and 6β-hydroxydolabella-3E,8E,12-trien-14-one.

Study paper 6, 7 and 9 showed that and the non-MTR producing S. chartarum taxa and the Type A taxa consistently produced 6β-hydroxy-dolabella-3E,8E,12-trien-14-one and often also epoxydolabellane A (se Figure ¡Error! Argumento de modificador desconocido. C), both precursors to the atranones233. Due to the lack of pure reference standards the identity of these had to be confirmed using LC-MS. This was kindly performed by Hanne Jakobsen, on the new Micromass LCT system using electrospray ionization (ESI) with the same or similar eluents as the general LC method391. In ¡Error! Argumento de modificador desconocido.) the ESI spectra of these two dolabellanes can be seen.

When growing on PSA agar, S. chartarum rarely produced the atranones themselves, which is different to growth on rice233. However, most of the isolates tested in the spring of 2001 also produced the atranones, indicating that the PSA agar had changed.

Two extracts of atranone producing isolates on rice (Jarvis, B.B., Hinkley, S.F., Nielsen, K.F. et al, to be published) contained trace levels of verrucarol upon hydrolysis (GC-MS) and also were significant more toxic that the other atranone producing isolates although still being magnitudes less toxic than the MTR producers. Trace level of verrucarol was also detected in the material sample from the Belgium IPH case home from which none of 6 isolates were MTR producers. When IBT 14915 (an atranone producer) in paper 2 was inoculated on gypsum boards trace level of verrucarol was also detected. Altogether these observations indicate that the atranone producers may be able to synthesise the verrucarol type TR. Hopefully a more sensitive LC-MS method can reveal if MTR are produced by these strains.

The very clear distinction of atranone producers and MTR-producers on agar substrates (paper 6-9) suggests that the genes from the atranone biosynthesis perhaps in inserted in, or near the genes coding for the enzymes used for synthesising trichodermin into verrucarol-type TR or epi-genetic changes (rearrangements in the 3D structure of the genes), so that only of these pathways is expressed.

The isolates studied by Ruotsalainen et al154 were retrieved from Public Health Institute, Kuopio Finland (KTL). Originally two large groups of isolates were observed, one which was highly cytotoxic and one which induced inflammatory responses in the murine macrophages. When analysing (paper 9) the chemical profiles of the 20 isolates, it was shown that all the 11 isolates being cytotoxic, except one which was probably contaminated or confused by another isolate, belonged to the MTR producing taxa. All the isolates inducing inflammatory responses belonged to the atranone producing S. chartarum taxa. In the original study154 it was also observed that as the only isolate HT16, did not induce the strong inflammatory response as well as not being cytotoxic at 105 spores/ml. This isolate was the only Stachybotrys sp. type A, suggesting that this taxa is not producing the inflammatory inducing substance(s) and that the effects is not due to the particle effects, as the spores are almost identical in size and shape (paper 6). The pure atranones B and D were did not induce any inflammatory response in the macrophages. Thus, the specific agent triggering the inflammatory response in the macrophages is still unidentified. The inflammatory agent(s) may be present in the MTR-producing isolates, but due to the extremely potent cytotoxins the macrophages are killed before they can respond or they may produce components inhibiting the induction of TNFα as such components have been isolated from this genus227.

Identification of the component inducing the inflammatory response is of special interest since high induction of TNFα is known to be a significant factor of the induction for lung damage159. Nikulin et al46,222 suggested that the MTR were the main reason of the lung tissue inflammation they observed when installing mice with S. chartarum spores from a MTR producer (#72) and a non-MTR producer (#29, later shown to produce atranones, paper 6). However #29 also produced significantly smaller quantities of the spiriocyclic drimanes, making these components an alternative agent.

When looking at the number of papers dealing with possible causative agents to the IPH, it is surprising how little effort has been put into the spiriocyclic drimanes, which are produced at considerably higher levels than the atranones and trichothecenes, presumable 10-500 times more, based on their extension coefficient.

Especially the spiriocyclic drimanes isolated from S. microspora232,440 which enhances the plasminogen-mediated fibrinolysis should be taken into consideration as they might be produced by the S. chartarum isolates in buildings. The neurotoxic symptoms reported by Johanning et al21,23 could be due to the neurotoxic as well as the nerve activator compounds441,442.

Figure ¡Error! Argumento de modificador desconocido.. UV and ESI spectra of two MER-NF500 analogues.

It the present work attempts were not made to differentiate between the different spiriocyclic drimanes as their UV spectra are very similar. Furthermore there was only very limited time to run LC-MS analyses. A single subclass, including 5-7 analogues of the spiriocyclic drimanes was, however, tentatively identified (paper 6), by their distinct UV-spectra seen in ¡Error! Argumento de modificador desconocido., as the Mer-NF5003227 components. LC-MS analyses pointed at molecular masses (MW) of 470 Da of three analogues, two analogues of 412 Da, one with 368 Da. All with slightly higher MW than the reported B and E analogue227, however one minor analogue also fitted MW, 386 Da, with the F analogue227. The attention was drawn to these components, as B.B. Jarvis had never seen these in the extracts from rice. These components are produced on most agar substrates, especially DRYES and PSA, as well as on hay (unpublished) and in crude extracts from the building materials (paper 1, 2, 10 and 11). In paper 10, it was shown that the spiriocyclic drimanes and atranones were produced at 10°C and 95% RH on several types of gypsum boards indicating that these metabolites are produced under most environmental conditions.

Airborne Stachybotrys metabolites

Figure ¡Error! Argumento de modificador desconocido.. HPLC chromatogram (260nm) of air sample from a stachybotrys infested house. With the UV spectra of peaks corresponding to metabolites.

Late in the study a number of air samples (24 hr, 60 m3/min) and material samples were received from E. Johanning. The filters and materials had already been shown to be highly cytotoxic in the pig kidney cell line used by Gareis et al335, which indicated the presence of MTR. Analysis of these samples revealed that two air samples contained several spiriocyclic drimanes including Mer-NF5003 analogues as seen on ¡Error! Argumento de modificador desconocido., and probably also satratoxins G and H (the UV spectra were very weak), which were confirmed by the presence of verrucarol in the two hydrolysed samples, detected by GC-MS and GC-MS/MS (¡Error! Argumento de modificador desconocido.).

Based on HPLC-DAD detection of satratoxins G and H, the total MTR contents were estimated to 75 and 100 ng (± 50%), whereas GC-MS showed 130 and 150 ng (± 50%) respectively.

Figure ¡Error! Argumento de modificador desconocido.. Chromatograms of HBF-derivatised hydrolysed air sample, from above: Total ion chromatogram; extracted ion (m/z 444) from the full scan event; extracted ion (m/z 231) from the MS/MS scan event on m/z 444. In the right side is the full scan and MS/MS spectra inserted.

These quantities correspond to about 100 and 116 pg/m3, as about 1.5% of the filter area was extracted, using the MTR contents of Sorenson et al47 of 40 ppm in the spores from rice cultures which corresponds to about 0.04 pg/spore (assuming a density of 1 g/cm3, and ellipsoidal shape of 11 x 4 µm) which correspond to about 2700 spores/m3. Based on data of Nikulin et al46 who found 0.14 pg/spore from MEA culture, this corresponds to 770 spores/m3, which are high but realistic concentrations.

Several of the material samples (vacuum cleaned onto the ALK filters) from the same building contained significantly higher quantities of the same drimanes as well as satratoxins G and H.

When working with these filters as well as samples from non problem buildings it was clear a significant quantities of black sticky material was also collected on the filters, and more method development is needed to clean-up these samples more efficiently.

When comparing exposure data to animal studies, it seems for the non-toxicologist to be very high quantities that have been instilled in rats and mice. Often 105 to 106 spores in single doses46,223-225,443 and down to 103 spores in several doses222, and with the concentrations of Stachybotrys spores even in highly infested buildings generally <<1000 spores/m3.

As seen in the literature part, many data on the toxicity of trichothecenes exist, however only af few studies take lung toxicity, particle effects, and other metabolites into account.

Using the data of Nikulin et al46 who used 106 spores (containing 140 ng MTR) as a single dose, the death of 2 of 4 animals, resembles the LD50 value (not taking the statistical uncertainty into account). Directly transferred to a human (70 k) assuming the same susceptibility per weight, corresponds to about 750 µg MTR or 3×109 spores.

As concentrations of Stachybotrys spores even in highly infested buildings, is generally below 1000 per m3 (Hunter et al10 have reported 20 times higher values) and with a human respiratory rate of 1.5 m3/hr, about 36 000 spores can inhaled per day.  This is so much lower than the LD50 value, that there is no reason to suspect lethal mycotoxicoses even if a 1000x lower LD50 is used, to cope with individual and species susceptibility as well as more toxic strains into account.

Workers handling infested materials, and not using the prescribed respiratory filters may be exposed to very high levels. Assuming up to 0.1-1 µg/cm2 MTR and a LD50 of 750 µg MTR this corresponds to dust from 0.15-1.5 m2, and it is not likely that any persons will inhale so much biomass even if working in a small unventilated room. But significant inflammation in the lungs and decrease in platelet concentration, as well as changes in the lymphocyte sub-populations may be possible. Such effects were observed in mice when instilling 6 dose over 3 weeks using 103 spores each time222. This corresponds to the dust from 2-15 cm2 infested material per day. However these data does not take the higher metabolism and shorter life span of the mice into account.

To asses the risk of people living in mouldy homes repetitive exposures of small doses is needed to estimate the No observed adverse effect level (NOAEL)444. This is especially important for the MTR, as they have immunosuppressing effects at far lower levels than the acute ones and should be combined with the other metabolites.

To conclude on this species, which is the far most investigated indoor contaminants, and still not been established any causal relationship to IPH, although is seems that the MTR are not the principle components. The general immunosuppression of people exposed to stachybotrys may also be explained by the spirocyclic drimanes, although exposure to MTR producing strains must be considered to be worse.

Significant is needed to characterise the health effects of spiriocyclic drimanes as they are the primary metabolites of S. chartarum when growing on building materials. More over they are also produced in its natural habitat, hay, and have been proven pharmacologically active in many assays (Appendix B, Table 2).

### Aspergillus

#### A. versicolor

Figure ¡Error! Argumento de modificador desconocido.. A "hotspot" of A. versicolor conidiophores on low density concrete.

In paper 2, it was shown that this species was capable of growing on almost all the water-damaged materials, and that chipboard and wallpaper supported production of the most visible biomass. Furthermore (paper 13), it was observed that A. versicolor grew especially fast on paints, and transient humidity conditions greatly slowed its growth.

Two different growth patterns were seen: either low biomass production and heavy sporulation or high biomass production (white-red mycelia) with very low sporulation (paper 2, 3 and 10).

In paper 10, A. versicolor was one of the most frequently observed mould growing on the materials, even capable of growing at 5°C. This is contradictory to Smith & Hill101, who observed that A. versicolor requires 9(C for growth on a high nutrient substrate such as MEA.

It was capable to grow on the three types of concrete at RH > 0.90 (paper 10), although the produced quantities of biomass were very low, except for a few hotspots (illustrated in Figure ¡Error! Argumento de modificador desconocido.). It was notable, that it always was A. versicolor that grew on the concretes and never P. chrysogenum, which indicates that A. versicolor may require less nutrients or is better grow at high pH. This is confirmed by private consultants who often see A. versicolor growing in plaster (M. Ø. Hansen, personal communication).

Figure ¡Error! Argumento de modificador desconocido.. UV spectrum and positive ESI spectrum of 5-methoxysterigmatocystin.

In paper 2, it was shown that all the 5 isolates of A. versicolor from buildings produced, very high quantities of sterigmatocystins (ST) and 5-methoxysterigmatocystin (5ST), up to 30 µg/cm2 on the material samples. In addition other ST analogues, versicolorins and other components from this biosynthetic pathway were usually also present in lower quantities estimated on the peak areas and the molar absorptivities. The amounts of biomass scraped from the materials were estimated to less than 100 mg, which means that the total contents of sterigmatocystins may have been more than 1% of the biomass. All the materials, especially wallpaper supported production of ST, which was positively correlated to the amount of visible biomass and negative correlated with sporulation. This is quite obvious, as substantial energy is put into sporulation.

In the study on naturally infested materials (paper 3) it was observed that red coloured areas infested with non- or poorly sporulating A. versicolor isolates contained the largest quantities of ST, whereas areas with many of A. versicolor conidia contained very small quantities of ST. This is important for exposure assesment, as the spores are considered the source of exposure to ST, although new studies have shown than smaller fragments than the spores are liberated from its mycelium91.

Figure ¡Error! Argumento de modificador desconocido.. UV spectra of two peaks resembling versicolin.

In both paper 2 and 3, the investigated materials were soakingley wet (aw > 0.99) and compared with paper 10 and 13 where different humidities were applied, it was apparent that ST production was correlated with RH, and that ST production was not detectable at aw < 0.90. This complies with findings on cereals255, where sterigmatocystin production started at aw 0.89 with a maximum production and biomass at aw 0.93.

In paper 2 and 3, 5ST was tentative detected based on its UV spectrum, especially the shoulder at 270-280 nm (Figure ¡Error! Argumento de modificador desconocido.) not seen in the UC-spectra of other sterigmatocystins. Later it was shown by positive electrospray LC-MS, that the molecular weight was 354 Da. This is seen as the [M+H]+ ion in ¡Error! Argumento de modificador desconocido.. The M+64 adduct could not be accounted for but it was also observed for ST.

A number of A. versicolor isolates produced one to five components resembling the known component versicolin445-447 (J.C. Frisvad, personal communication). Two of the UV spectra are shown in Figure ¡Error! Argumento de modificador desconocido.. Al least one of these was produced in substantial quantities on wallpapered gypsum boards (paper 2).

Figure ¡Error! Argumento de modificador desconocido.. UV spectra 3,4,5-trihydroxytoluene and 2,4,6-trihydroxy toluene.

It was tried to clean up 5 of these components by growing a particular good producer on YES agar, where they often are produced in very high quantities. But as the components seem to be unstable when cleaned-up, and as time was short the project (2 weeks) it was abandoned. Later it was tried to tentative identify the analogues by LC-MS as a literature review showed that it might be 2,3,6-trihydroxytoluene447 and esters hereof. However this analogues was not commercially available, but the two analogues to isomers 3,4,5-trihydroxytoluene, and 2,4,6-trihydroxy toluene of were purchased. Especially the 3,5,6 analogue, had a similar UV-spectrum (¡Error! Argumento de modificador desconocido.) and a retention time similar to several of the "versicolins".

LC-MS of extracts containing the "versicolins" indicated molecular masses of 260 and 262 Da, and several with 242 Da. However other, less abounded, unexplained ions were also present, meaning that these molecular masses may not be correct. This was further complicated, as LC-MS of the two commercial analogues indicated the 2,4,6-analogue was not ionised at all, and that the 3,4,5 analogue showed 6 major ions at m/z 253, 294, 311 and 481, with no apparent ionization mechanism. Thus the ionisation conditions, including ion-polarity, have to be optimized for this type of components before any definite molecular mass determinations can be made.

Figure ¡Error! Argumento de modificador desconocido.. From above, UV spectra of the structurally unknown ROQ, XXO, and PE1.

In paper 10 and 13, where the sterigmatocystins and their analogues were almost never detected, and number of other metabolites were detected. These have previously been detected in extracts of A. ochraceus (J.C. Frisvad, personal communication), and are named ROQ, PE1 and XXO until their structure is known, their UV spectra can be seen in Fig. 11. Especially the latter component was often detected in material extracts. Looking at some of the very small peaks in the chromatograms from both agar and material extracts (paper 2 and 3) revealed that these metabolites were present in many A. versicolor extracts.

LC-MS analysis indicated that XXO had a MW of 431 Da, and an analogue eluting at 1-2 min. before a MW of 447 Da. Three analogues of ROQ were detected, however the MW as only determined for on of them as 393 Da. It is interesting that these presumable nitrogen-containing metabolites (nitrogen rule) are still biosynthesised at RH < 90% while the polyketide pathway that produced ST, is shut down. However at 86% RH they were not biosynthesised by the still growing A. versicolor.

Four other types of metabolites, eluting between 3 and 10 min, seemed to be strongly associated with growth of this species under low RH, and their UV spectra can be seen in ¡Error! Argumento de modificador desconocido., all has several analogues often also seen. A few of the metabolites have been seen in agar culture extracts.

Figure ¡Error! Argumento de modificador desconocido.. UV spectra of four unknown metabolites presumable produced by A. versicolor

The HPLC-DAD analyses of the samples of paper 10 and 13, also revealed a ERG analogue eluting approx. 2 min after having identical UV spectra, it was only detected in samples infested with A. versicolor. Inspection of the full scan segments of the GC-MS analyses indicated no other sterols, which together with the retention time and same UV spectrum strongly indicates that it was an ester of ergosterol.

It is obvious that the metabolism of this species is very diverse, and needs much more attention, as most of the metabolites produced at aw < 0.95 are unknown. These metabolites may be important for the adverse health effects associated to growth of A. versicolor, especially because they were liberated from the materials by a light vacuum, and hence have the capability of becoming airborne.

Animal tests have also shown that A. versicolor induces inflammatory responses in rats and mice151,157. These things combined with the small liberated fragments from the spores or hyphae91, means that the growth of A. versicolor poses a health risk even if air measurements does not show elevated concentrations of spores.

#### A. ustus

Figure ¡Error! Argumento de modificador desconocido.. Common UV-spectra from Aspergillus ustus var. pseudodeflectus.

In paper 3, A. ustus were incubated on a number of materials, they grew very slowly on pure gypsum boards and chipboard whereas growth was much faster on the wallpapered ones, which it covered the surface after 2 weeks. On the gypsum boards solid structures, 1-2 mm in diameter, containing up to 100 Hülle cells were observed. The A. ustus isolates studied in paper 3, were all isolated from mouldy buildings, and produced no detectable quantities of any known mycotoxins from this species. The highly toxic austamides, austdiols, and the austocystins who are consistently found in cereal isolates (J.C. Frisvad, personal communication) were not produced in detectable quantities on the materials or in agar cultures. Instead a number of metabolites with UV spectra resembling the ones seen in ¡Error! Argumento de modificador desconocido., with varying UV-max, all eluting between from 14 min to 35 min, were observed. The low toxic kotanines, also seen from isolates of A. niger was the only known metabolites produced on the materials.

The indoor isolates appears to be Aspergillus ustus var. pseudodeflectus, which should be described as a new species, as varieties are not accepted any more175.

In agar culture extracts of the indoor air type, components resembling the drimane sesquiterpenes, the TMC's, pergillins and ophibolins seem to be present (Appendix B, Table 5). These metabolites are not described as toxic, and have been isolated from Aspergillus ustus var. pseudodeflectus, but a definitive identification of these metabolites was not possible due to the lack of reference standards and LC-MS analyses.

The general conclusion on the indoor air A. ustus isolates, is that studies on their in vitro and in vitro pulmonary toxicity and inflammatory potential is needed (grown on relevant materials), as well as knowledge on what is actually liberated from materials infested by these isolates.

#### A. niger complex

Figure ¡Error! Argumento de modificador desconocido.. UV spectra of a tetracyclic compound (upper) and naphtho-(-pyrones.

Growth of especially A. niger was extremely fast on all artificially infested materials except on gypsum board and the wallpapered gypsum boards where almost no biomass were produced (paper 3). The other materials were covered by black Aspergillus heads in one to two weeks, and substantial quantities of biomass could be scraped off the material. This indicates that the gypsum boards contains components inhibiting the growth of this species. All isolates (paper 3) produced high quantities (>20 different) naphtho-(-pyrones and tetracyclic compounds eluting from 6 to 35 min (UV spectra, see ¡Error! Argumento de modificador desconocido.) and the known compounds orlandin and nigragillin (Appendix B, Table 6). The quantities of these components made detection of the malformins and other end-absorption components impossible, and if the spores are later shown to be highly cytotoxic a more selective method against these small cyclic peptides should be developed.

After the study (paper 3) the samples were reanalysed using HPLC-FLD for the presence of ochratoxins, but these analyses were also negative.

When observing the spores on the media it is clear that they contains a high number of other metabolites, but as for A. ustus, studies on their in vitro and in vitro pulmonary toxicity and inflammatory potential is needed.

#### A. flavus

In paper 10, A. flavus contaminated a number of the wooden materials, presumable due to ineffective X- ray sterilisation (25 kGy), as A. flavus growth was seen on a piece of pinewood  returned from the sterilisation plant. It should be noted that all boxes were marked with small X-ray indicators to assure that they were x-rayed.

However as A. flavus usually produces aflatoxins, extracts from materials where it grew were also analysed with HPLC-FLD, where the samples had been derivatised using trifluoroacetic acid to produce the stronger fluorescent hemiacetals448, which had a 52 times lower detection limit (≈100 pg) for the B1 analogue than the underivatised had.

No aflatoxin was detected in of these samples, which complies with the results of Ren et al272 and by Rao et al273. Surprisingly, the isolate recovered from one of the materials did not produce aflatoxins on CYA or YES agar.

However the in vitro and in vivo toxic and inflammatory potential of material cultures should still be investigated, as it may still be the source of indoor air problems.

### Penicillium

In papers 3 and 10, it was observed that the penicillia produced significant less biomass than the aspergillii, based on visual observations, what could be scraped off the materials and the size ergosterol peak in the HPLC chromatograms.

It has been a problem to obtain materials with other penicillia than P. chrysogenum, as identification to the species level is not done by the consultant engineers we collaborates with, and who have a good source of naturally infested materials.

#### P. chrysogenum

In paper 3 it was observed that this species grew very fast on the wallpapered gypsum boards and chipboard, seen as grey to light green discolouring patches. The materials were overgrown in two to three weeks.

On the naturally infested materials investigated it was present in almost all samples, with more substantial amount of biomass than on the artificially infested materials. Isolation often also revealed an additional but limited number of A. versicolor colonies, indicating that it often grows in mixed cultures, which was also observed in paper 10. The mixed cultures may be due to a lower quantities of antifungal metabolites, or perhaps that the metabolites does not diffuse in these solid materials.

Figure ¡Error! Argumento de modificador desconocido.. A MDF plate (20(14 cm) from paper 10, after 4 months at 95%RH and 10°C. # 1 and 2 are P. chrysogenum growth (2 mm high) and #3 is a Eurotium Sp., #4 is Ulocladium sp., and the rest of the material is partly covered with a mixture of A. versicolor and P. chrysogenum.

In paper 13, P. chrysogenum (CBS 401.92) was surprisingly fast on the painted samples, where it grew faster than A. versicolor, and was visible after 2 weeks, here i appeared light blue, but changed colour to grey over time.

P. chrysogenum produced (paper 3, 10 and 13) very low quantities of secondary metabolites compared with Aspergillus species, e.g. were no P. chrysogenum metabolites detected in any of the large areas seen on ¡Error! Argumento de modificador desconocido., except for occasional detection of chrysogine, and  2-pyrovoylaminobenzamide no metabolites could be associated to growth of this species under non water damage conditions. A considerable number of the P. chrysogenum infested samples in paper 13 were contaminated with an unknown Aspergillus, producing totally unknown metabolites perhaps related to A. ustus and/or A. versicolor.

On water-damaged wallpapered gypsum boards it produced chrysogine (paper 3) whereas this metabolite was not detected on chipboard. The natural samples, meleagrin was detected as the only metabolite, which is interesting as it is a predecessor of the neurotoxic roquefortine C (paper 3). TLC analyses284 showed that all isolates produced an unknown metabolite appearing as dark blue spots after spraying with anis aldehyde. This metabolite was only detected from P. chrysogenum and had approximately 10% higher Rf-value than griseofulvin.

Recently it was shown that double blinded exposure of 8 "sensitive" humans to 6×105 spores/m3 of P. chrysogenum, grown on wallpapered gypsum boards, during 6 min, did not induce any significant self reported or clinical measured symptoms (Meyer, H.W., Kildesø, J., Nielsen, K.F. et al, to be published).

As for most of the other moulds, no data no the long term toxic potential of this species exists, and hence it may produce toxic metabolites, not detectable with HPLC-DAD. However on the other hand, it may be one of the moulds that obscure detection of more toxic species.

#### P. brevicompactum

All isolates grew well on water-damaged wallpapered chipboard and chipboard (paper 3) whereas the growth was slower on the wallpapered gypsum-boards, and no growth was observed on gypsumboards. This observation suggest that growth it is stimulated by components present in wood, which corresponds well to field observations where it is frequently isolated from wooden materials130.

On chipboard (paper 3), 1/3 of the isolates produced mycophenolic acid, and 1/2 of the stains also produces asperphenamate, a tanzawaid acid analogue449(UV in ¡Error! Argumento de modificador desconocido.), and the structurally unknown metabolite O.

Figure ¡Error! Argumento de modificador desconocido.. UV spectra of unknown tanzawaid acid analogue (RI 649).

In paper 10, this species was not isolated from any of the materials, indicating that it has difficulties with competing with P. chrysogenum and A. versicolor. However the dust from one MDF plate (10°C, 95% RH) contained another tanzawaid acid analogue indication the presence of P. brevicompactum on the material, and other possible analogue was detected from a beech wood piece (90% RH, 20°C), also indicating the presence of P. brevicompactum.

Especially the presence of the immunosuppressing mycophenolic acid, a number of metabolites with unknown biologically activities, and the anecdotal mycotoxicoses after ingestion of infected food, suggests that may have strong in vitro and in vivo toxic and inflammatory potential, which of needs further investigation, as it is the second most common penicillia.

#### P. polonicum

Only two indoor strains were available, and they grew on all the materials, although usually with not very much biomass (paper 3). They both produced 3-methoxy-viridicatin, verrucofortine, and the tremorgenic verrucosidin.

However as it is not clear how common this species is in the indoor environment, there are other species which need to have their in vitro and in vivo toxic and inflammatory potential determined before this species.

#### Penicillium expansum

The only indoor isolate of indoor origin was available (paper 3) and it grew very poor on all the four materials, and no metabolites were detected in any of these samples. This is contradictory to Land and Hult299 who saw production of the patulin, when their strains were inoculated on wood and wood chips.

As this species can produce some of the most toxic components found in this genus, it is necessary to know if it presence in buildings is due to growth on materials or introduced from mouldy fruits.

### Trichoderma

In paper 2, where the materials were inoculated at aw ≈ 1, growth of Trichoderma could be detected after 3-4 days on wooden materials whereas it was much more slow on other materials and did not occur on the new gypsum boards. These observations are fully in accordance with field observations (paper 4) where Trichoderma is generally found on wood products25,78.

In paper 10, where the humidity was lower, Trichoderma was only found growing on a very small fraction at the wooden materials and here not even as the dominating mould. This further demonstrates that this genus requires water-damaged materials to grow.

None of the T. atroviride, T. harzianum, T. longibrachiatum and T. viride infested materials from, paper 2, revealed trichodermol upon hydrolysis, which was also the case for the YES extracts from the 36 isolated investigated by Lübeck et al78.

In a later paper 8, 150 additional agar extract from U. Thrane's collection were screened for trichodermol, however only one isolate (IBT 9471 = ATCC 90237) was able to produce trichodermol as also found by Corley et al303. It was not been possible to obtain other known trichodermol producing isolates, as the isolate used produce the first trichodermin by Godtfredsen & Vangedal301 at LEO pharmaceuticals, Denmark, is not available.

The literature review on Trichoderma clearly showed that the peptides are some of the dominating biologically active metabolites (Appendix B, Table 11), but they were not targeted in this work due to lack of LC-MS facilities.

Recently it was shown that double blinded exposure of 8 "sensitive" humans to 6×105 spores/m3 of T. Harzianum, grown on wallpapered gypsum boards, during 6 min, did not induce any significant self reported or clinical measured symptoms (Meyer, H.W., Kildesø, J., Nielsen, K.F. et al, to be published). The set-up was (economic reasons) partly build in plastic, and during characterization of the set-up it was shown that particles smaller than the spores were absorbed to the walls of the set-up. As T. harzianum as A. versicolor, also produces smaller particles (Kildesø, J.K., Würtz, H., Nielsen, K.F. et al, to be published) than the spores the people were not exposed to these fine particles.

To conclude on this genus, it is important that their in vitro and in vitro pulmonary toxicity and inflammatory potential is investigated (grown on relevant materials), as well as knowledge on what is actually liberated from materials infested.

### Memnoniella echinata

No growth tests were performed with this species on materials, but an infested piece of Memnoniella infested gypsum board received from Dr. E. Johanning. Dust, sampled by the ALK mouthpiece, from this sample contained griseofulvin and its two dechlorinated derivatives.

Chemical analysis (unpublished) were performed on the following 11 isolates, grown on ALK, PSA, SYES, CYA and V8 agar: Results showed that the three griseofulvins where consistently produced on all media and in significant in quantities compared to other metabolites, and combined with data from rice cultures45, it must concluded that these components seems to be produced on all solid substrates. Spiriocyclic drimanes, similar to the ones produced by S. chartarum, were also consistent produced, however in significant (ca. 10×) lower quantities than the griseofulvins, based on the UV molecular absorptivities.

The production of trichodermol or esters of it, varied considerable even in the same isolates on the same media (papers 8 and 11)

To conclude on this species, it seems to be isolated the same places as S. chartarum although less frequently, which may be due to difficulties of distinguishing it from S. chartarum. However studies on its in vitro and in vitro pulmonary toxicity and inflammatory potential is needed (grown on relevant materials), as well as knowledge on what is actually liberated from infested materials.

### Alternaria

All the isolates, except of the A. infectoria group isolate, inoculated on different materials (paper 3) grew well and produces alternariol, it's mono methyl ether and three to five unknown analogues with identical UV-spectra, metabolites which are very low toxic and should not be considered mycotoxins. No altertoxins, tentoxin or tenuazonic acid was detected in any of the extracts, confirming results of Ren et al322.

It was tried to find naturally infested material with growth of Alternaria, but all samples (>15) brought to the department was infested with Ulocladium sp. and not Alternaria. This may indicate that actual Alternaria growth on materials may not be that common, and that the many findings of Alternaria in the indoor air environment may originate from out door sources.

However it has still not been shown if the AAL toxins are produced by Alternaria in buildings, although this is very unlikely, as this type of strains are only known as endophytes in plants319,320. These metabolites are the only really mycotoxins known from this species, but need LC-MS detection or the unspecific OPA derivatisation also used for fumonisins. An alternative would be to hydrolyse them and detect the backbone using GC-MS320. Thus, the presence of this fungus in buildings only seems to pose a very limited risk, especially as the main source of exposure comes from outdoors, where the air concentrations are magnitudes higher than indoors.

### Chaetomium globosum

Being an ascomycete this genus has a very characteristic appearance (paper 3) due to its distinct black or dark green, hairy perithecia visible to the naked eye. Field samples were all very wet wallpaper, gypsum board and wood products (paper 3 and 4). On the artificially infested water-damaged material growth was very fast covering the surface with substantial amounts of biomass after two weeks (paper 3).

In paper 10 where mixtures of common moulds were inoculated under controlled humidities Chaetomium was only found growing at one material clearly showing that this genus generally requires water-damaged materials for growth.

Figure ¡Error! Argumento de modificador desconocido.. Unknown metabolite from C. globosum.

When growing on building materials (paper 3) C. globosum consistently produced high quantities of biomass (up to 10 mg/cm2). Very high quantities of secondary metabolites, especially chaetoglobosins A, C and analogues were produced in very similar quantities, 28-50 and 5-7 µg/cm2 respectively, by six isolates incubated on wallpapered gypsum. An unknown metabolite, was detected in all Chaetomium extracts except in IBT 7029, which had visible smaller peritricia than the other isolates. Hence this component may be a species-specific marker. Its UV data (see ¡Error! Argumento de modificador desconocido.) did not seem to match any of the components found in Table 15 in Appendix B.

The naturally infested materials was very similar to the artificially infested materials, chaetoglobosin A and C production in quantities up to 3 µg/cm2. Besides these, three other chaetoglobosins and approximately 10 unknown metabolites were also detected. Analyses of two old (2-3 years) heavily black-stained materials did not reveal chaetoglobosins A or C, but a number more polar analogues, which are probably hydrolysis or oxidation products of the original metabolites, however these extracts have not yet been subjected to LC-MS analyses.

The consistent production of the chaetoglobosins and lack of detectable quantities of chaetocin, sterigmatocystines and chaetomin, which should not be produced by C. globosum, shows that the connections species names and produced metabolites has not been obscured as in Penicillium and Aspergillus69.

C. globosum grew very well together with gram negative bacteria on various building materials without it was possible to se this in the stereo microscope. However when determining the inflammatory potential of this mixture in mice macrophages huge quantities of TNFα and NO was liberated due to endotoxin from the bacteria. This observation may point against more studies on the interaction between bacteria and moulds as the bacteria may need the moulds powerful enzyme-systems (unpublished). However spores from the pure cultures did not induce any inflammatory response in macrophages, but was cytotoxic to the cells (unpublished).

When concerning risk assessment of this fungus in buildings, it is clear the cytotoxic and cytoplasmatic cleavage inhibiting chaetoglobosins is the main concern, as no data on inhalation of the spores have been found in the literature. However as the spores of this fungus is packed in the Peritrecia the exposure to airborne spores may be rather limited and smaller particles released from dry mycelia, as it has been shown for A. versicolor, must be studied before any attempt on risk assesment is being tried.

### Cladosporium

C. sphaerospermum seems to be the most predominant species growing in buildings, and was able to out grow P. chrysogenum even in a ratio of 1 to 100 (paper 13). This is a result of their ability to re-attain growth from the hyphal tip much faster than penicillia125, which is presumable why this and other phylloplanes are so common in bathrooms and on silicon caulkings in windows, environments which often have very different humidities during the day.

No secondary metabolites were detected in any of the samples in paper 13, and this genus is known for the very few metabolites it produces, and it ability to grow under these special conditions may account for this.

The high number of spores of C. cladosporioides (up to 15000m-3) found out doors during the summer and the apparent lack of metabolite production on materials, and no inflammatory response when in instilled mice lungs223, suggests that this genus should generally not be considered more than a humidity indicator.

### Ulocladium

All four isolates inoculated on materials (paper 3) grew well, but did not produce any detectable quantities of secondary metabolites, which is in accordance with the literature where extremely few metabolites from this genus have been described. Analyses of natural samples with excessive growth have not either revealed any metabolites in the polarity range we look at using present HPLC-DAD method.

In Study 10, it was only isolates at RH ≈ 0.95, indication that is also requires very high RH, and not metabolite seemed to be associated to it.

To conclude on this genus, it seems to be isolated the same places as S. chartarum although more frequently, as it is presumable able to grow under the same humidities as Alternaria, but the low production of metabolites no known knowledge of mycotoxicoses indicates that it is not a major problem. However this should be confirmed by testing its in vitro and in vitro pulmonary toxicity and inflammatory potential.

It is a good indicator for wet environments and hence water-damage, but requires significant microscopic training if it should be differentiated from Alternaria.

### Paecilomyces

P. lilacinus was found to grow poorly on all the artificially infested materials except on gypsum boards, where the characteristic pink cotton-like mycelium was produced, but only in modest amounts, and no metabolites were detected in the extract (paper 3).

P. variotii grew well on the artificially infested chipboards and wallpapered chipboard, but the quantities of biomass were very limited, however at the chipboard did support production of seven components with totally unknown UV-spectra.

These two species, both needs to have their in vitro and in vitro pulmonary toxicity and inflammatory potential determined (grown on relevant materials) besides determining the size of particles liberated from materials infested with them.

### Eurotium

Figure ¡Error! Argumento de modificador desconocido.. The ascoma from Eurotium sp. on a piece of pinewood  after 4 months at 10°C and 95% RH.

In study 10, Eurotium sp. was isolated from several of the wooden materials (see Figure ¡Error! Argumento de modificador desconocido.) inoculated at 25, 20 and 10°C (materials were not sterilised prior to inoculation at 10°C). The HPLC analyses revealed the presence of very high quantities of metabolites compared with A. versicolor and P. chrysogenum. These metabolites were probably present in the ascoma (see ¡Error! Argumento de modificador desconocido.) as these structures were very predominant. Echinulin and several derivatives were detected along with a high number of antraquinones, including questin and questinol, several benzoquinones, including flavoglausin, metabolites produced by many Eurotium species450. Also two isochromane toxin analogues449,451 were detected.

The high quantities of metabolites sampled on the filters indicates that this genus may be important, and the in vitro and in vitro pulmonary toxicity and inflammatory potential of dust from infested materials s needed.

## Overall discussion

### Growth on materials

It has been demonstrated that the tertiary colonisers in practise require almost liquid water to grow on the materials. Hence the name water-damage moulds is very appropriate. To avoid growth of these is theoretically very simple, as it just requires dry constructions, however due to insufficient quality assurance in the building industry and partly also insufficient maintenance, these five problems are observed:

- The climate screen, especially the roof, should be watertight, which should not pose any problem. However this is actually a major problem in Denmark, as seen in paper 4, especially due to leaking flat roofs.

- Leaking pipes, especially when they are hidden in the constructions, constitutes a substantial part of the severe water damages (papers 3 and 4).

- Rising damp from the ground, due to lack of drainage or capillary breaking layer.

- Water build into the construction either from hardening concrete, which had not had the time to dry out. Also materials which have been placed on the ground or out in the rain is becoming an increasing problem and a number of these cases have been reported in the press.

- When parts of the building is exposed to rain during the building process, this an engineering or planning problem which demand that the partly finish construction is shielded during the building process.

Solving these problems is a not a matter of choosing or developing other materials, as almost all materials was able to support fungal growth (paper 4 and 10). Instead it is a matter of creating new quality assurance systems, which can be practically implemented during the building process.

### Metabolites

The water-damage moulds produced very high quantities of secondary metabolites, and as secondary metabolites are signal components175, these metabolites must be very important for the fungi, as they must use significant energy and internal resources on producing them.

In contrast Trichoderma spp. produced very low quantities of detected metabolites, which is probably due to the poor extraction and UV-absorption of the peptabols which this genus is so known for, at it is known to out-grow most other moulds.

When comparing the quantities and number of metabolites produced the aspergillii and penicillia on agar substrates with the metabolites produced on building materials, it was clear that the rich agar substrates short circuits the metabolism of these genera. It appeared that the aspergillii produced significant higher quantities on moisture saturated materials, whereas the penicillia seemed to need the many nutrients found in the rich agar media.

When comparing the metabolism of aspergillii and penicillia with Stachybotrys, it is seems like this short circuiting is correlated to the extensively mycelia production, which seemed to be negatively correlated the sporulation. Thus, when trying to predict the production of metabolites on various matrixes such as building materials, by using agar substrates, media enhancing sporulation and decreasing pure mycelia growth should be used.

Especially when working with A. versicolor, it was frustrating to see the numbers of unknown metabolites in the extracts. Hopefully accurate-mass LC-MS, will make identification of some metabolites known in literature possible.

It is essential to investigate the toxicity and inflammatory responses of all appropriate moulds as function of the humidity, as it may only under certain humidities that they are toxic or inflammagenious. Perhaps it is also isolate depended or perhaps loses some of the strains the ability of producing important metabolites when held in the lab, as it observed when working on the membrane-toxin (paper 7).

The funga has still not been characterised enough, as there is still considerable confusion on especially the speciation of Cladosporium and Penicillium species found in buildings.

The total microbial flora still needs to be established, at bacteria presumable means a lot under certain conditions and there may be several types of bacteria present at the materials which have not been determined. The bacteria may need the moulds to degrade the materials, and especially genera as Stachybotrys, Chaetomium and Trichoderma that are very well known producers of cellulases and as they requires almost saturated conditions they will have to compete with bacteria which can also grow at these aw.

#### Analytical methods

Extraction of the metabolites was the most important step, and it was clear that extracting whole the material in organic solvents is not a suitable technique as: i) very huge quantities of interfering material was also extracted from the material (paper 1-3) which may obscure detection or even react with the target components; ii) mycotoxins as ST and TR, could only be extracted from the material-matrix in very limited quantities, <1% of spiked quantities could be extracted from materials (paper 2); iii) the detected metabolites may not become airborne, especially if they are excreted into the material. It is important to evade interfering components, as it will require a number of different solid phase extracting (SPE) techniques for each or a group of components. This makes screening impossible, as it perhaps needed to 2-6 different SPE steps per analysis, which is very time and resource consuming.

Scraping off the material using a blade worked better (paper 3) but material is easily lost if it is dry and if the material is very wet then significant quantities of interfering material may still be present from the material. Hence the vacuum sampling technique used in paper 10 and 13, is much better as it only samples metabolites that may become airborne and samples a minimum of matrix.

The used detection methods have unfortunately only worked on medium to apolar substances, which could be detected using HPLC-UV, except for the trichothecenes, which were targeted by GC-MS. However important substances as the nephrotoxic glycopeptides, AAL toxins, malformins, cyclosporin analogues, and many peptides would have evaded detection, this also includes unknown toxins and of course metabolites present below the detection limits.

Appropriate bioassays would cope with these problems as these, but it would still need a lot of assays for the different activities, so it would have been perfect to combine this study with a lot of assay tests, unfortunately this was not possible.

#### Exposure

This study and several others have clearly shown, that mould damaged buildings around the world contains many different extremely toxic substances23,48,54,212,235, however only one study have successfully been able to determine indoor mycotoxins indirect in air samples336. Here this study is the first with direct determination of several Stachybotrys toxins in air samples, although both Yike et al336 and Dietrich et al416 have shown the presence of MTR in air indirectly.

It is clear that Stachybotrys is special as the spores actually contains significant higher quantities metabolites than other spores, and this probably is the reason for the much more serious health effects associated to this mould.

Stachybotrys is also an example of the importance that the spores are dry. However recurrent drying and rewetting may facilitate the development of smaller particles, and may extract especially water-soluble components from the mycelia which may become airborne on dust or water particles.

# Conclusion

Moulds growing on water-damaged materials produce a high number of very toxic metabolites. The production of these metabolites is very depended on the humidity of and for some moulds also the substrate.

Three taxa of Stachybotrys are found in buildings, of these only one taxa, approx. 35% of the isolates, actually produced satratoxins whereas most other strains stop the trichotehcene biosynthesis at trichodermin. All three taxa produced high quantities of the pharmacologically active spiriocyclic drimanes and their precursors. These two groups of metabolites and the atranones, which are produced by the two non-satratoxin producing taxa, are produced on building materials under field conditions. Idiopathic pulmonary hemasiderosis in infants did not seem to be associated with satratoxin production. Stachybotrys biomass collected on filters from naturally infested materials samples, contained significant higher quantities of metabolites than any other fungal species investigated during this study.

This study has showed that spiriocyclic drimanes and satratoxins was present on filters from air-samplings in a building with severe health problems due to growth of S. chartarum.

Aspergillus versicolor, which is perhaps the most common species found in mouldy buildings, had a very diverse metabolism where many of its biosynthetic pathways was only occasionally expressed. When growing on materials under high water activity > 0.95% most isolates produced high quantities of the carcinogenic mycotoxin, sterigmatocystin, whereas aw < 0.90 a number of structurally unknown metabolites, presumable alkaloids, also know from A. ochraceus were produced. A. versicolor grew often in mixed cultures with others moulds where it sporulated poor, meaning that it may evade detection by cultivating based methods.

Penicillium chrysogenum is the most frequently detected species, but it produces surprisingly few detectable metabolites and often none. Combined with the no observed effects in humans experimentally exposed to high quantities of the spores this implies that it may not be important for a heath point of view and is actually obscuring the detection of more toxic genera and species.

On water-damaged materials Chaetomium globosum produces high quantities of chaetoglobosins, whereas P. brevicompactum produces mycophenolic acid and P. polonicum the tremorgenic verrucosidin. The A. ustus isolates from buildings are macro-morphologically and chemically very different than cereal isolates, and should be described as a new species.

Trichoderma longibrachiatum, T. harzianum, T. citrinoviride, T. atroviride and T. viride does not produce detectable quantities of trichothecenes when growing on materials, and even on laboratory media do <1% of the isolates produce trichodermol or esters of it.

When mouldy material are investigated for mycotoxins they should vacuum sampled onto filters, as it dramatically decreases the number of interfering substances from the materials and gives a more precise description of what people may be exposed.

Except from Stachybotrys, almost no data on the pulmonary toxicity and inflammatory potential of the spores and fragments exists from indoor moulds grown on appropriate materials and not just agar media where the secondary metabolism is often short circuited.

The minimal RH for growth on wood based materials and material containing starch is just below 80% at room temperature, and increases to about 90% at 5°C. On paper-mineral composites such as gypsumboard the min RH is approx. 90% RH from room temperature to 5°C. Pure mineral based materials with few organic additives seems to be able to support growth at RH ≥ 0.90, although 95% RH was needed to generate chemical detectable quantities of biomass. S. chartarum requires RH ≥ 95% to grow on gypsum boards.

When applying transient humidities to material samples during a day, the phylloplane Cladosporium was able to outgrow P. chrysogenum, even though it can grow under lower RH than Cladosporium under constant humidity. This is presumably why phylloplanes like Cladosporium, Ulocladium, Phoma and Aureobasidium are very common i bathrooms and other places with instationary humidity conditions.

Ergosterol content of building materials could be very precisely be quantified and quickly analysed (60-100 samples per day) by isotope dilution GC-MS/MS, although not being as sensitive as other GC-MS based methods due to interference from the isotope marked standard and instrumental problems on the ion-trap used. Visual assessment, especially supported by dissection microscopy, was however just a sensitive and is able to cope with the high variation in mould biomass on materials, but should occasionally be supplemented with chemical markers for comparison with other studies.

# Perspectives and future research

Although excellent research is being done on this field is being done all over the world, especially in northern Europe and North America, it still seems like we are far away from a major breakthrough, and hence much more research is needed.

Smaller projects

Studies on the inhalative toxicity of the spiriocyclic drimanes fund in the spores of Stachybotrys is needed. This should be followed by development of specialised methods for detecting these metabolites as they are present in substantial quantity in the spores and hence probably will become good biomarkers.

Studies on the three different Stachybotrys taxa are needed, to se if atranone and satratoxin producing isolates coexists, and/or also to see if the atranone producing taxa over long time also can produce low quantities of satratoxins.

It would also nice to produce antibodies against the sterigmatocystin-guanine adduct to see if people are exposed to the toxin through the air or only through the food.

The unknown A. versicolor metabolites needs to be structure elucidated and produced in sufficient quantities for a toxicological evaluation.

It is also necessary determine if these particles can be sampled on filters or if they should be collected on adsorption materials, and the clean-up methods used for screening of mycotoxins is needed.

Major projects

General microbiological work is needed so the total funga can be established in the individual countries, especially for Penicillium where a lot of confusion exists. But also the performance days under dynamic conditions is needed to know, e.g. what if the moulds gets periods of humidities close to their critical RH. Also species succession and the growth in mixed cultures needs to be investigated.

Co-ordinated tests of the inflammatory potential and the toxicity of particles released from appropriate materials, including materials from problem buildings and materials incubated at realistic conditions should be performed from a representative number of isolates from all relevant species. These results should be compared with the activity observed from field samples from buildings with health problems. In this way better ratings to the health impact of the moulds could be developed for the individual moulds which is needed in epidemiological studies and risk handling in mouldy buildings. The responsible components should also be structurally elucidated and specific methods for the determination of the most important ones should be developed, as they are good candidates as exposure-markers.

Nobody have tried inhalation experiment where the cognitive performance on mice or rats or their off-spring are measured. This was very successful for low concentration exposure xylene452, and if combined with exposures to known areas of naturally infested materials and perhaps artificially infested materials under well characterised ventilation in the boxes, this may be the way to force a major breakthrough.

There is a great need to develop methods for measuring the exposure to particles, and to determine if exposure to mycotoxins occurs only through spores. The metabolites may also be found on dust and in small fragments.

# References

1. 	Platt, SD, Martin, CJ, Hunt, SM, Lewis, CW. 1989. Damp Housing, Mold Growth and Symptomatic Health State. Brit.Med.J 298: 1673-1678.

2. 	Brunekreef, B, Dockery, DW, Speizer, FE, Ware, JH, Spengler, JD, Ferris, BG. 1989. Home dampness and respiratory morbidity in children. Am.Rev.Resp.Dis. 140: 1363-1367.

3. 	Dales, RE, Zwanenburg, H, Burnett, R, Franklin, CA. 1991. Respiratory health effects of home dampness and moulds among Canadian children. Am.J.Epidem. 134: 196-203.

4. 	Dekker, C, Dales, RE, Bartlett, S, Brunekreef, B, Zwanenburg, H. 1991. Childhood asthma and the indoor environment. Chest 100: 922-926.

5. 	Brunekreef, B. 1992. Association between questionnaire reports of home dampness and childhood respiratory symptoms. Sci.Tot.Env. 127: 79-89.

6. 	Verhoeff, AP, Strien, RT, Wijnen, JTM, Brunekreef, B. 1995. Damp Housing and Childhood Respiratory Symptoms: The role of sensitization to dust mites and moulds. Am.J.Epidem. 141: 103-110.

7. 	Koskinen, O, Husman, T, Hyvärinen, A, Reponen, T, Nevalainen, A. 1997. Two Moldy Day-care Centers: a Follow up study of respiratory symptoms and infections. Indoor Air 7: 262-268.

8. 	Koskinen, O. 1999. Moisture, Mold and Health. Ph.D. dissertation, KTL National Public Health Institute, Kuopio, Finland.

9. 	Koskinen, O, Husman, T, Meklin, T, Nevalainen, A. 1999. Adverse health effects in children associated with moisture and mold observations in houses. International Journal of Environmental Health Research (United Kingdom) 9: 143-156.

10. 	Hunter, CA, Grant, C, Flannigan, B, Bravery, AF. 1988. Moulds in buildings: the air spora of domestic dwellings. Int.Biodet. 24: 81-101.

11. 	Adan, OCG. 1994. On the fungal defacement of interior finishes. Dr. Dissertation, Eindhoven University, The Netherlands.

12. 	Brunekreef, B. 1992. Damp housing and adult respiratory symptoms. Allergy 47: 498-502.

13. 	Nevalainen, A, Partanen, P, Jääskeläinen, E, Hyvärinen, A, Koskinen, O, Meklin, T, Vahteristo, M, Koivisto, J, Husman, T. 1998. Prevalence of moisture problems in Finnish houses. Indoor Air Suppl. 4: 45-49.

14. 	Miller, JD, Haisley, PD, Reinhardt, JH. 2000. Air sampling result in relation to extend of fungal colonization of building materials in some water-damaged buildings. Indoor Air 10: 146-151.

15. 	Hilling, R. 1998. 220 Schools. Damage and defects in school buildings. SP Swedish National Testing and Research Institute [In Swedish], Borås.

16. 	Gravesen, S, Nielsen, PA, Nielsen, KF. 1997. Skimmelsvampe i vandskadede bygninger. SBI rapport 282.  Statens Byggeforskningsinstitut, Hørsholm.

17. 	Koskinen, O, Husman T, Hyvärinen A, Reponen T, Ruuskanen J, Nevalainen A. 1994. Respiratory Symptoms and Infections in Mouldy Dwellings and Day-care Centers. In Samson RA, Flannigan B, Flannigan ME, Verhoeff AP, Adan OCG, Hoekstra ES. (eds.), Health Implications of Fungi in Indoor Environments. p. 211-214. Elsevier, Amsterdam.

18. 	Koskinen, O, Husman, T, Hyvärinen, A. 1995. Respiratory symptoms and infections among children in a day-care center with mould problems. Indoor Air 5: 3-9.

19. 	Hodgson, MJ, Morey, PR, Leung, WY, Morrow, L, Miller, JD, Jarvis, BB, Robbins, H, Halsey, JF, Storey, E. 1998. Building-associated pulmonary disease from exposure to Stachybotrys chartarum and Aspergillus versicolor. J.Occup.Env.Med. 40: 241-249.

20. 	Johanning, E, Landsbergis, P, Gareis, M, Yang, CS, Olmsted, E. 1999. Clinical experience and results of a sentinel health investigation related to indoor fungal exposure. Env.Health Persp. 107: 489-494.

21. 	Gordon, WA, Johanning, E, Haddad, L. 1999. Cognitive impairment associated with exposure to toxigenic fungi. In Johanning E (Ed.), Bioaerosols, Fungi and Mycotoxins: Health effects, Assessment, Prevention and Control. Eastern New York Occupational & Environmental Health Center, New York,  p. 94-98.

22. 	Dales, RE, Miller, JD, White, J, Dulberg, C, Lazarovits, AI. 1998. Influence of residential fungal contamination on peripheral blood lymphocyte population in children. Arch.Env.Health 53: 190-195.

23. 	Johanning, E, Biagini, RE, Hull, D, Morey, PR, Jarvis, BB, Landsbergis, P. 1996. Health and immunology study following exposure to toxigenic fungi (Stachybotrys chartarum) in a water-damaged office environment. Int.Arch.Occup.Health 68: 207-218.

24. 	Gravesen, S. 1994. Allergic and non-allergic manifestations related to indoor fungal exposure - management of cases. In Samson RA, Flannigan B, Flannigan ME, Verhoeff AP. (eds.), Health implications of fungi in indoor air environment. p. 241-248. Elsevier, Amsterdam.

25. 	Gravesen, S, Frisvad, JC, Samson, RA. 1994. Microfungi.  Munksgaard, Copenhagen.

26. 	Dearborn, DG, Yike, I, Sorenson, WG, Miller, MJ, Etzel, RA. 1999. Overview of investigations into pulmonary hemorrhage among infants in Cleveland, Ohio. Env.Health Persp. 107: S495-S499

27. 	Novotny, WE, Dixit, A. 2000. Pulmonary hemorrhage in an infant following 2 weeks exposure of fungal exposure. Arc.Ped.Adol.Med. 154: 271-275.

28. 	Elidermir, O, Colasurdo, GN, Rossmann, SN, Fan, LL. 1999. EXPERIENCE AND REASON - Stachybotrys and Pulmonary Hemorrhage. Isolation of Stachybotrys from the lung of a child with pulmonary hemosiderosis. Pediatrics 104: 964-966.

29. 	Gravesen, S. 2000. Microbiology on Indoor Air '99- what is new and interesting? An overview of selected papers presented in Edinburgh August, 1999. Indoor Air 10: 74-80.

30. 	Douwes, J. 1998. Respiratory health effects of indoor microbial exposure. A contribution to the development of exposure assesment methods. Dr. Dissertation, Landbouwuniversiteit Wageningen, Holland.

31. 	Larsen, FO, Christensen, G, Clementsen, P, Gravesen, S, Skov, P, Norn, S. 1996. Microfungi in indoor air are able to trigger histamine release by non-IgE-mediated mechanisms. Inflammation Research 45: S23-S24

32. 	Olsen, JH, Dragstead, L, Autrup, H. 1988. Cancer risk and occupational exposure to aflatoxins in Denmark. Brit.J Cancer 58: 392-396.

33. 	Autrup, JL, Schmidt, J, Seremet, T, Autrup, H. 1991. Determination of exposure to aflatoxins among Danish worker in animal-feed production through the analysis of aflatoxin B1 adducts to serum albumin. Scand.J.Work.Env.Health 17: 436-440.

34. 	Kristensen, P, Irgens, LM, Andersen, A, Bye, AS, Sundheim, L. 1997. Gestational age, birth weight and perinatal deaths amongst births to Norwegian  farmers 1967-1981. Am.J.Epidem. 146: 329-338.

35. 	Lappalainen, S, Pasanen, A-L, Pasanen, P, Kalliokoski, P. 1997. Production of fungal volatile compounds in bedding material. Agric.Food Sci.Finland 6: 219-227.

36. 	Lappalainen, S, Nikulin, M, Berg, S, Parikka, P, Hintikka, E-L, Pasanen, A-L. 1996. Fusarium toxins and fungi associated with handling of grains on eight Finnish farms. Atmos.Env. 17: 3059-3065.

37. 	Gravesen, S. 1979. Fungi as a cause of allergic disease. Allergy 34: 135-154.

38. 	Rylander, R, Northall, M, Engdal, U, Tunsäter, A, Holt, PG. 1998. Airways inflammation, atopy, and (1-3)--D-glucan exposure in two schools. Am.J.Resp.Crit.Care Med. 158: 1685

39. 	Rylander, R. 1997. Investigation of the relationship between disease and airborne (1-3)--D-glucan in buildings. Mediators of Inflammation 6: 275-277.

40. 	Goto, H, Yuasa, K, Rylander, R. 1994. (1-3)--Glucans in indoor air, Its measurements and In Vitro activity. Am J Ind.Med. 25: 81-83.

41. 	Miller, JD, Laflamme, AM, Sobol, Y, Lafontaine, P, Greenhalgh, R. 1988. Fungi and Fungal products in Canadian houses. Int.Biodet. 24: 103-120.

42. 	Ström, G, West J, Wessen B, Palmgren U. 1994. Quantitative analysis of microbial Volatiles in damp Swedish houses. In Samson RA, Flannigan B, Flannigan ME, Verhoeff AP. (eds.), Health implications of fungi in indoor air environment. p. 291-305. Elsevier, Amsterdam.

43. 	Wilkins, CK, Nielsen, EM, Wolkoff, P. 1997. Patterns in volatiles organic compounds in dust from mouldy buildings. Indoor Air 7: 128-134.

44. 	Bock, R, Schleibinger, HW, Ruden, H. 1998. Volatile secondary metabolites as indicators for fungal growth indoors. Umweltmed.Forsch.Prax 3: 359-364.

45. 	Jarvis, BB, Sorenson, WG, Hintikka, E-L, Nikulin, M, Zhou, Y, Jiang, J, Wang, S, Hinkley, SF, Etzel, RA, Dearborn, DG. 1998. Study of Toxin Production by Isolates of Stachybotrys chartarum and Memnoniella echinata isolated during a study of pulmonary hemosiderosis in infants. Appl.Env.Microb. 64: 3620-3625.

46. 	Nikulin, M, Reijula, K, Jarvis, BB, Hintikka, E-L. 1997. Experimental lung mycotoxicosis induced by Stachybotrys atra. Int.J.Experim.Pathol. 77: 213-218.

47. 	Sorenson, WG, Frazer, DG, Jarvis, BB, Simpson, J, Robinson, VA. 1987. Trichothecene Mycotoxins in Aerosolized Conidia of Stachybotrys atra. Appl.Env.Microb. 53: 1370-1375.

48. 	Croft, WA, Jarvis, BB, Yatawara, CS. 1986. Airborne outbreak of Trichothecene Mycotoxicosis. Atmos.Env. 20: 549-552.

49. 	Miller, JD, Greenhalgh, R, Wang, Y, Lu, M. 1991. Trichothecene chemotypes of three Fusarium species. Mycologia 83: 121-130.

50. 	Flannigan, B, McCabe, EL, McGarry, F. 1991. Allergenic and toxigenic micro-organisms in houses. J.Appl.Bacter. 70: 61-73.

51. 	Tiffany, JA, Bader, HA. 2000. Detection of Stachybotrys chartarum: The effectiveness of culturable-air sampling and other methods. Env.Health 9-11.

52. 	Flannigan, B, Miller JD. 1994. Health implications of fungi in indoor environments - An overview. In Samson RA, Flannigan B, Flannigan ME, Verhoeff AP, Adan OCG. (eds.), Health implications of fungi in indoor air environment. p. 3-26. Elsevier, Amsterdam.

53. 	Brunekreef, B, Verhoeff AP, van Strein RT, Van Wijnen JH. 1994. Home Dampness and Childhood Respiratory Symptoms: The Role of Sensitisation to Dust and Mites. In Samson RA, Flannigan B, Flannigan ME, Verhoeff AP, Adan OCG, Hoekstra ES. (eds.), Health Implications of Fungi in Indoor Environments. p. 189-199. Elsevier, Amsterdam.

54. 	Anderson, MA, Nikulin, M, Köljalg, U, Anderson, MC, Rainey, F, Reijula, K, Hintikka, E-L, Salkinoja-Salonen, M. 1997. Bacteria, Moulds, and Toxins in Water-Damaged Building Materials. Appl.Env.Microb. 63: 387-393.

55. 	Hirvonen, M-R, Nevalainen, A, Makkonen, N, Mönkkönen, J, Salvolainen, K. 1997. Strecptomyces spores from mouldy houses induce nitric oxide, TNF- and IL-6 secretion from RAW264.7 macrophage cell line without causing subsequent cell death. Env.Tox.Pharm. 3: 57-63.

56. 	Nevalainen, A, Hyvärinen A, Pasanen A-L, Reponen T. 1994. Fungi and Bacteria in normal and mouldy dwellings. In Samson RA, Flannigan B, Flannigan ME, Verhoeff AP. (eds.), Health implications of fungi in indoor air environment. p. 163-167. Elsevier, Amsterdam.

57. 	Reponen, T, Nevalainen, A, Jantunen, MJ, Pellikka, M, Kalliokoski, P. 1992. Normal Range Criteria for indoor air bacteria and fungal spores in a subartic climate. Indoor Air 2: 26-31.

58. 	Räty, K, Raatikainen, O, Holmalahti, J, Wright, A, Joki, S, Pitkaenen, A, Saano, V, Hyvärinen, A, Nevalainen, A, Buti, I. 1994. Biological activities of actinomycetes and fungi isolated from indoor air of problem houses. Int.Biodet.Biodegr. 34: 143-154.

59. 	Brunekreef, B, Douwes, J, Doekes, G, van Strien, R. 1999. Health effects of mould and bacterial components in the home environment. Proceedings of the 8th International Conference on Indoor Air Quality and Climate, Indoor Air `99.   p. 897-898.

60. 	Andersson, M. 1999. Bacterial diversity and toxicity in air, indoor environments and food. Ph.D. Thesis, Department of Applied Chemistry and Microbiology, Dicision of Microbiology, University of Helsinki.

61. 	Grant, C, Hunter, CA, Flannigan, B, Bravery, AF. 1989. The Moisture Requirements of Moulds Isolated from Domestic Dwelling. Int.Biodet. 25: 259-284.

62. 	Ayerst, G. 1966. Influence of physical factors on the deterioration by moulds. Soc.Chem.Indust.Monograph. 23: 14-20.

63. 	Joffe, AZ. 1962. Mycopath.Mycl.Appl. 16: 201

64. 	Scott, WJ. 1957. Water relations of food spoilage micro-organisms. Adv.Food.Res. 7: 83-127.

65. 	Filtenborg, O, Frisvad, JC, Thrane, U. 1996. Moulds in food spoilage. Int.J Food Microbiol 33: 85-102.

66. 	Samson, RA. 1985. Occurrence  of moulds in modern living and working environments. Eur.J Epidemiol. 1: 54-61.

67. 	Nielsen, KF, Thrane, U, Larsen, TO, Nielsen, PA, Gravesen, S. 1998. Production of mycotoxins on artificially inoculated  building materials. Int.Biodet.Biodegr. 42: 8-17.

68. 	Gaylarde, CC, Morton, LHG. 1999. Deteriogenic biofilms on buildings and their control: a review. Biofouling 14: 59-74.

69. 	Frisvad, JC. 1989. The connection between the penicillia and aspergilli and mycotoxins with special emphasis on misidentified isolates. Arch.Env.Contam.Tox. 18: 452-467.

70. 	Frisvad, JC, Gravesen S. 1994. Penicillium and Aspergillus from Danish homes and working places with indoor air Problems: Identification and mycotoxin determination. In Samson RA, Flannigan B, Flannigan ME, Verhoeff AP. (eds.), Health implications of fungi in indoor air environment. p. 281-290. Elsevier, Amsterdam.

71. 	Larsen, TO, Frisvad JC. 1994. Production of volatiles and presence of mycotoxins in conidia of common indoor Penicilia and Aspergillii. In Samson RA, Flannigan B, Flannigan ME, Verhoeff AP. (eds.), Health implications of fungi in indoor air environment. p. 251-279. Elsevier, Amsterdam.

72. 	Samson, RA, Hoekstra, ES, Frisvad, JC, Filtenborg, O. 2000. Introduction to Food- and Air Borne Fungi. 6th Edition. In Samson RA, Hoekstra ES, Frisvad JC, Filtenborg O(Eds.). Centraalbureau voor Schimmelcultures, Utrecht.

73. 	Korpinen, E-L. 1973. Studies on Stachybotrys alternans. I. Isolation of toxigenic strains from Finnish grains and feeds. Acta.Pathol.Microbiol.Scand.Sect.B 81: 191-197.

74. 	Hansen, MØ. 2000. Database on moulds and the materials they grow on. Østergaard Miljø, Copenhagen.

75. 	Gravesen, S. 1972. Identification and quantitation of indoor airborne micro-fungi during 12 month from 44 Danish houses. Acta Allergologia 27: 337-354.

76. 	Miller, JD. 1992. Fungi as contaminant of indoor air. Atmos.Env. 26A: 2163-2172.

77. 	Tobin, RS, Baranowski, E, Gilman, AP, Kuiper-Goodman, T, Miller, JD, Giddings, M. 1987. Significance of fungi in indoor air: Report of a working group. Can.J.Public.Health 78: S1-S32

78. 	Lübeck, M, Poulsen, SK, Lübeck, PS, Jensen, DF, Thrane, U. 2000. Identification of Trichoderma strains from building materials by ITS1 ribotypning, UP-PCR fingerprinting and UP-PCR cross hybridization. FEMS micro.biol.lett. 185: 129-134.

79. 	Bissett, J. 1987. Fungi associated with urea-formaldehyde foam insulation in Canada. Mycopath. 99: 47-56.

80. 	Pitt, JI. 1975. Xerophilic fungi and the spoilage of foods of plant origin. In Duckworth RB. (ed.), Water relations of foods.  Academic press, New York.

81. 	Andersen, B, Nissen, A. 2000. Evaluation of media for detection of Stachybotrys and Chaetomium species associated with water-damaged buildings. Int.Biodet.Biodegr. 46: 111-116.

82. 	Biological Particles in Indoor Environments. Report No. 12. European Collaborative Action. Indoor Air Quality & its Impact on Man1993. In. Verhoeff AP(ed.). Commission of the European Communities, Brussels.

83. 	Field Guide for the Determination of Biological Contaminants in Environmental Samples1996. In Dillon HK, Heinsohn PA, Miller JD(Eds.). American Industrial Hygiene Association,

84. 	Wanner, H, Verhoeff, AP, Colombi, A, Flannigan, B, Gravesen, S, Mouilleseaux, A, Nevalainen, A, Papadakis, J, Seidel, K. 1993. Biological Particles in indoor environments.

85. 	Dillon, HK, Miller, JD, Sorenson, WG, Douwes, I, Jacobs R.R. 1999. Review of methods applicable to the assessment of mold exposure to children. Env.Health Persp. 107: 473-480.

86. 	Palmgren, U, Ström, G, Blomquist, G, Malmberg, P. 1986. Collection of airborne micro-organismems on Nucleopore filters and analysis - CAMNEA method. J.Appl.Bacter. 61: 401-406.

87. 	Larsson, L, Saraf, A. 1997. Use of Gas Chromatography-Ion Trap Tandem Mass Spectrometry for the Detection and Characterization of Microorganisms. Molec.Biotech. 7: 279-287.

88. 	Dales, RE, Miller, JD, White, J. 1999. Testing the association between residential fungus and health using ergosterol measures and cough recordings. Mycopath. 147: 21-27.

89. 	Haugland, RA, Vesper, SJ, Wymer, LJ. 1999. Quantitative measurements of Stachybotrys chartarum conidia using realtime detection of PCR products with the TaqMan fluorogenic system. Mol.Cell.Prob. 13: 329-340.

90. 	Pasanen, A-L, Kujanpää, L, Pasanen, P, Kalliokoski, P, Blomquist, G. 1997. Culturable and total fungi in dust accumulated in air ducts in single-family houses. Indoor Air 7: 121-127.

91. 	Kildesø, J, Würtz, H, Nielsen, KF, Wilkins, CK, Gravesen, S, Nielsen, PA, Thrane, U, Schneider, T. 2000. THE RELEASE OF FUNGAL SPORES FROM WATER DAMAGED BUILDING MATERIALS. Proceedings of Healthy Buildings 2000, Espoo.   p. 313-318.

92. 	Pasanen, A-L, Nhninnen, M, Kalliokoski, P, Nevalainen, A, Jantunen, MJ. 1992. Airborne Cladosporium and other fungi in damp versus reference residences. Atmos.Env. 26B: 121-124.

93. 	Garrett, MH, Rayment, PR, Hooper, MA, Abramson, MJ, Hooper, BM. 1998. Indoor airborne fungal spores, house dampness and associations with environmental factors and respiratory health in children. Clin.Exp.Allergy 28: 459-467.

94. 	Nevalainen, A, Pasanen, A-L, Niininen, M, Reponen, T, Kalliokoski, P, Jantunen, MJ. 1991. The indoor air quality in Finnish homes with mold problems. Env.Int. 17: 299-302.

95. 	Dales, RE, Miller, JD, McMullen, ED. 1997. Indoor air quality and health: Validity and determination of reported home dampness and mould. Int.J.Epidemol. 26: 120-125.

96. 	Gosset, P, Malaquin, F, Delneste, Y, Wallaert, B, Capron, BA, Joseph, M, Tonnel, A. 1993. Interleukin-6 and interleukin-1 production is associated with antigen-induced late nasal response. J.Allergy Clin.Immunol. 92: 878-890.

97. 	Hirvonen, M-R, Ruotsalainen, M, Roponen, M, Hyvärinen, A, Husman, T, Kosma, V-M, Komulainen, H, Savolainen, K, Nevalainen, A. 1999. Nitric Oxide and proinflammatory cytokines in nasal lavage fluid associated with symptoms and exposure to moldy building microbes. Am.J.Resp.Crit.Care Med. 160: 1943

98. 	Wålinder, R, Wieslander, G, Norbäck, D, Wessen, B. 2001. Nasal lavage biomarkers: Effects of water damage and microbial growth in an office building. Arch.Env.Health 56: 30-36.

99. 	Panasenko, VT. 1967. Ecology of microfungi. The Botanical review 33: 189-215.

100. 	Land, CJ, Banhidi, ZG, Albertson, AC. 1985. Surface discoloring and blue stain by cold-tolerant filamentous fungi on outdoor softwood in Sweden. Mat.Organis. 20: 133-156.

101. 	Smith, SL, Hill, ST. 1982. Influence of temperature and water activity on germination and growth of Aspergillus restrictus and A. versicolor. Trans.Brit.Myc.Soc. 79: 558-559.

102. 	Gervais, P, Grajek, W, Bensoussan, M, Molin, P. 1988. Influence of the water activity of a solid substrate on the growth rate and sporogenesis of filamentous fungi. Biotechnol.Bioeng. 31: 457-463.

103. 	Gervais, P, Berlin, JM, Sarrette, M. 1988. Influence of water activity on aroma production by Trichoderma viride growing on solid substrate. J.Ferment.Tech. 66: 403-407.

104. 	Clayton, CN. 1942. The germination of fungus spores in relation to controlled humidity. Phytopathology 32: 921-943.

105. 	Groom, P, Panisset, T. 1933. Studies of  Penicillium chrysogenum Thom in relation to temperature and relative humidity of the air. Ann.Appl.Biol. 20: 633-660.

106. 	Ayerst, G. 1969. The effect of moisture and temperature on growth and spore germination of some fungi. J.Stored Prod.Res. 5: 127-141.

107. 	Pitt, JI, Hocking, AD. 1977. Influence of solute and hydrogen ion concentration on the water relations of some xerophilic fungi. J.General Microb. 101: 35-40.

108. 	Hocking, AD, Miscamble, BF, Pitt, JI. 1994. Water relations of Alternaria alternata, Cladosporium sphaerospermum, Curvularia lunata, and Curvularia pallescens. Mycol.Res. 98: 91-94.

109. 	Rowan, NJ, Johnstone, CM, McLean, RC, Anderson, JG, Clarke, JA. 1999. Prediction of toxigenic fungal growth in buildings by using a novel modelling system. Appl.Env.Microb.  65: 4814-4821.

110. 	Chang, JCS, Forade, KK, Vanosdell, DW. 1995. Growth evaluation of fungi (Penicillium spp. and Aspergillus spp.) on ceiling Tiles. Atmos.Env. 29: 2331-2337.

111. 	Galloway, LD. 1935. The moisture requirements of molds fungi with special reference to mildew in textiles. J.Textile Inst. 26: 123-129.

112. 	Ezeonu, IM, Noble, JA, Simmons, RB, Prince, DL, Crow, SA, Ahearn, DG. 1994. Effects of Relative Humidity on Fungal Colonization of Fiberglass Insulation. Appl.Env.Microb. 60: 2149-2151.

113. 	Nikulin, M, Pasanen, A-L, Berg, S, Hintikka, E-L. 1994. Stachybotrys atra growth and toxin production in some Building Materials and Fodder under different Relative Humidities. Appl.Env.Microb. 60: 3421-3424.

114. 	Pasanen, A-L, Nikulin, M, Berg, S, Hintikka, E-L. 1994. Stachybotrys atra Corda may produce Mycotoxins in Respiratory Filters in Humid Environments. Am Ind.Hyg.Assoc.J 55: 62-65.

115. 	Coppock, JBM, Cookson, ED. 1951. The effect of humidity on mould growth on construction materials. J.Sci.Food Agric. 534-537.

116. 	Chung, WY, Wi, SG, Bae, HJ, Park, BD. 1999. Microscopic observation of wood-based composites exposed to fungal deterioration. J.Wood Sci. 45: 64-68.

117. 	Block, SS. 1953. Humidity requirements for mould growth. Appl.Env.Microb. 1: 287-293.

118. 	Illman, WI, Weatherburn, MW. 1940. Development of mould on cotton fabrics. American Dyestuff Reptr. 36: 343-344.

119. 	Viitanen, HA. 1994. Factors affecting the development of biodeterioration in wooden constructions. Mater.Struct. 27: 483-493.

120. 	Atkins, PW. 1990. Physical Chemistry.  Oxford University Press, Oxford.

121. 	Becker, R. 1984. Condensation and mould growth in dwellings-parametric and field study. Build.Env. 19: 243-250.

122. 	Viitanen, HA, Bjurman, J. 1995. Mould growth on wood at fluctuating humidity conditions. Mat.Organis. 29: 27-46.

123. 	Bjurman, J. 1989. Effect of humidity fluctuation on mould on pine sapwood. International Research on Wood Preservation,

124. 	Moriyama, Y, Nawata, WC, Tsuda, T, Nitta, M. 1992. Occurrence of moulds in Japanese bathrooms. Int.Biodet.Biodegr. 30: 55

125. 	Park, D. 1982. Phylloplane fungi: tolerance of hyphal tips to drying. Trans.Brit.Myc.Soc. 79: 174-179.

126. 	Viitanen, HA. 1997. Modelling the time factor in the development of mould fungi - Effects of critical humidity and temperature conditions in pine and spruce sapwood. Holzforschung 51: 6-14.

127. 	Pasanen, P, Korpi, A, Kalliokoski, P, Pasanen, A-L. 1997. Growth and volatile metabolite production of Aspergillus versicolor in house dust. Env.Int. 23: 425-432.

128. 	Korpi, A, Pasanen, A-L, Pasanen, P, Kalliokoski, P. 1997. Microbial Growth and Metabolism in house dust. Int.Biodet.Biodegr. 40: 19-27.

129. 	Bjurman, J. 1994. Ergosterol as an Indicator of Mould Growth on Wood in Relation to Culture Age, Humidity Stress and Nutrient Level. Int.Biodet.Biodegr. 33: 355

130. 	Seifert, KA, Frisvad JC. 2000. Penicillium on solid wood products. In Samson RA, Pitt JI. (eds.), Integration of modern taxonomic methods from Penicillium and Aspergillus classification. p. 285-298. Harwood academic publishers, Amsterdam.

131. 	Thelander, O, Bjurman, J, Boutelje, J. 1993. Increase in the content of low molecular carbon hydrates at lumber suracces during drying and correlation with nitrogen content, yellowing and mould growth. Wood Sci.Tech. 27: 381-389.

132. 	Suttie, ED, Hill, CAS, Jones, D, Orsler, RJ. 1998. Chemically modified solid wood - I. Resistance to fungal attack. Mat.Organis. 32: 159-182.

133. 	Mankowski, M, Morrell, JJ. 2000. Patterns of fungal attack in wood-plastic composites following exposure in a soil block test. Wood.Fibre Sci. 32: 340-345.

134. 	Pasanen, A-L, Juutinen, T, Jantunen, MJ, Kalliokoski, P. 1992. Occurrence and moisture requirements of microbial growth in building materials. Int.Biodet.Biodegr. 30: 273-283.

135. 	Morgenstern, J. 1982. Einfluss von polyvinylacetat-zusätzen in potzmörtel auf die Schimmelbildung. Mat.Organis. 17: 241-251.

136. 	Webb, JS, Nixon, M, Eastwood, IM, Greenhalg, M, Robson, GD, Handley, PS. 2000. Fungal colonization and biodeterioration of plasticized polyvinyl chloride. Appl.Env.Microb. 66: 3194-3200.

137. 	Berk, S, Ebert, H, Teitell, L. 1957. Utilisation of plasticisers and related organic compounds by fungi. Ind.Eng.Chem. 49: 1115-1124.

138. 	Ezeonu, IM, Prince, DL, Simmons, RB, Crow, SA, Ahearn, DG. 1994. Fungal Production of Volatiles during Growth on Fibreglass. Appl.Env.Microb. 60: 4172-4173.

139. 	Seal, KJ, Pathirana, RA. 1982. The microbiological susceptibility of polyurethanes: a review. Int.Biodet.Bull. 18: 81-85.

140. 	Bravery, AF. 1988. Biodeterioration of paints a state of the art review. In Houghton DR, Smith RN, Eggins HOW. (eds.), Biodeteroriation 7. p. 466-485. Elsevier, London.

141. 	Jakubowski, J. 1971. The preweather Technique. Paint mildrewcide evaluation in the laboratory parallels field performance. Am.Paint J. 56: 56-76.

142. 	Winters, H, Isquith, IR, Coll, M. 1975. A study of the ecological succession in Biodegradation of a vinyl acrylic paint film. Dev.Ind.Microbiol. 17: 167-171.

143. 	Simmons, RB, Price, DL, Noble, JA, Crow, SA , Ahearn, DG. 1997. Fungal colonization of air filters from hospitals. Am Ind.Hyg.Assoc.J 58: 900-904.

144. 	Chang, JCS, Forade, KK, Vanosdell, DW. 1996. Assessment of fungal (Penicillium chrysogenum) growth on three HVAC duct materials. Env.Int. 22: 425-431.

145. 	Ahearn, DG, Simmons, RB, Switzer, F, Ajello, L, Pierson, DL. 1991. Colonization by Cladosporium spp. of painted metal surfaces associated with heating and air conditioning. J.Ind.Microb. 8: 277-280.

146. 	Ahearn, DG, Crow, SA, Simmons, RB, Prince, DL, Noble, JA, Mishra, SK, Pierson, DL. 1996. Fungal colonization of fiberglass insulation in the air distribution system of a multi-story office building: VOC production and possible releation to a sick building syndrome. J.Ind.Microb.  16: 280-285.

147. 	Hukka, A, Viitanen, HA. 1999. A mathematical model of mould growth on wooden materials. Wood Sci.Tech. 33: 475-485.

148. 	Gravesen, S, Larsen, L, Gyntelberg, F, Skov, P. 1986. Demonstration of Microorganisms and Dust in Schools and Offices. Allergy 41: 520-525.

149. 	Kuby, J. 1997. Immunology.  Freeman, New York.

150. 	Sorenson, WG. 1997. Aerosolized Mycotoxins: Implications for Occupational settings. In Johanning E, Yang CS. (eds.), Fungi and Bacteria in Indoor Air Environments. p. 57-67. Eastern New York Occupational Program, New York.

151. 	Sumi, Y, Nagura, H, Takeuchi, M. 1994. Granulomatous lesions in the lung induced by inhalation of mold spores. Virchow Arc. 424: 661-668.

152. 	Cooley, JD, Wong, WC, Jumper, CA, Straus, DC. 1999. Cellular and humorale responses in an animal model inhaling Penicillium chrysogenum spores. In Johanning E (Ed.), Bioaerosols, Fungi and Mycotoxins: Health effects, Assessment, Prevention and Control. Eastern New York Occupational & Environmental Health Center, New York

153. 	Shahan, TA, Sorenson, WG, Paulauskis, JD, Morey, R, Lewis, DM. 1998. Concentration- and time-dependent upregulation and release of the cytokines MIP-2, KC, TNF, and MIP-1 alpha in rat alveolar macrophages by fungal spores implicated in airway inflammation. Am.J.Resp.Cell Mol.Biol. 18: 435-440.

154. 	Ruotsalainen, M, Hirvonen, M-R, Nevalainen, A, Meklin, T, Savolainen, K. 1998. Cytotoxicity, production of reactive oxygen species and cytokines induced by different strains of  Stachybotrys sp. from mouldy buildings in RAW264.7 macrophages. Env.Tox.Pharm. 6: 193-199.

155. 	Smith, JE, Anderson, JG, Lewis, CW, Murad, YM. 1992. Cytotoxic fungal spores in the indoor atmosphere of damp domestic environment. FEMS micro.biol.lett. 200: 337-337.

156. 	Smith, JE, Lewis CW, Murad YM, Anderson JG. 1993. A survey of mycotoxin-associated fungal spora with cytotoxic properties collected from the home environment. In Scudamore KA. (ed.), p. 109-117. Central Science Laboratory, Berks.

157. 	Murtoniemi, T, Nevalainen, A, Suutari, M, Toivola, M, Komulainen, H, Hirvonen, M-R. 2001. Induction of cytotoxicity and production of inflammatory mediators in RAW264.7 macrophages by spores grown on six different plasterboards. Inhalation Toxicology 13: 233-247.

158. 	Hirvonen, M-R, Nevalainen, A, Makkonen, N, Mönkkönen, J, Salvolainen, K. 1997. Induced production of nitric oxide, tumor necrosis factor, and interleukin-6 in RAW 264.7 macrophages by streptomycetes from indoor air of mouldy houses. Arch.Env.Health 52: 426-432.

159. 	Abraham, E, Jesmok, G, Tuder, R, Allbee, J , Chang, Y-H. 1995. Contribution of tumor necrosis factor-alpha to pulmonary cytokine expression and lung injury after hemorrhage and resuscitation. Critical Care Medicine 23: 1319-1326.

160. 	Cantry, D, Feldman, M. 1990. The role of cytokines in autoimmunity. Biotech.Ther. 1 : 361-409.

161. 	Strachan, DP, Sanders, CH. 1989. Damp housing and childhood asthma. Respiratory effects of indoor air temperature and relative humidity. Journal of Epidemiology and Community Health, 43: 7-14.

162. 	Johanning, E, Morey PR, Jarvis BB. 1993. Clinical-epidemiological investigation of health effects caused by Stachybotrys atra building contamination. In Jaakkola JJK, Ilmarinen R, Seppänen O. (eds.), Procedings of Indoor Air '93. Vol 1. p. 225-230. Indoor Air '93, Helsinki.

163. 	Johanning, E. 1995. Health problems related to fungal exposure - the example of toxigenic Stachybotrys chartarum (atra). In Johanning E, Yang CS. (eds.), Fungi and Bacteria in Indoor Air Environments. p. 169-182. Eastern New York Occupational Program, New York.

164. 	Dearborn, DG, Infeld, MD, Smidth, PG. 1997. Update. Pulmonary hemorrhage/hemosiderosis among infants 1993-1996. MMWR 46: 33-35.

165. 	Montana, E, Etzel, RA, Allan, TM. 1997. Environmental risk factors associated with pediatric idiopatic pulmonary hemosiderosis in a Cleveland community. Pediatrics 99: 117

166. 	Dearborn, DG. 1997. Pulmonary hemorrhage in infants and children. Curr.Opin.Pediatr. 9: 219-224.

167. 	CDC. 1994. Acute pulmonary hemorrhage/hemasiderosis among infants - Cleveland, January 1993 - November 1994. MMWR 43: 881-883.

168. 	Anonymous1995. Acute pulmonary hemorrhage among infants. Chicago, April 1992 to November 1994. MMWR 44: 67-74.

169. 	Pappas, MD, Sarnaik, AP, Meert, KL, Hasan, RA, Lieh-Lai, MW. 1996. Idiopathic Pulmonary Hemorrhage in Infancy: Clinical Features and Management With High Frequency Ventilation. Chest 110: 553-555.

170. 	CDC. 2000. Update: Pulmonary hemorrhage/hemosiderosis among infants - Cleveland, Ohio, 1993-1996 (Reprinted from MMWR, vol 49, pg 180-184, 2000). JAMA 283: 1951-1953.

171. 	Flappan, SM, Portnoy, J, Jones, P, Barnes, C. 1999. Infant pulmonary hemorrhage in a suburban home with water damage and mold (Stachybotrys atra). Env.Health Persp.Supp. 107: 927-930.

172. 	Knapp, JF, Michael, JG, Hegenbartk, MA, Jones, PE, Black, PG. 1999. Case records of the Children's Mercy Hospital, case 02-1999: A 1-moth-old infant with respiratory distress and chock. Ped.Emerg.Care 15: 288-293.

173. 	Vesper, SJ, Dearborn, DG, Elidermir, O, Haugland, RA. 2000. Quantification of siderophore and hemolysin from Stachybotrys chartarum strains, including a strain isolated from the lung of a child with pulmonary hemorrhage and hemosiderosis. Appl.Env.Microb. 66: 2678-2681.

174. 	Tripi, PA, Modlin, S, Sorenson, WG, Dearborn, DG. 2000. Acute pulmonary haemorrhage in an infant during induction of general anaesthesia. Paed.Anesthes. 10: 92-94.

175. 	Frisvad, JC. 1998. Secondary metabolites and species models in Penicillium and Aspergillus. Dr. Tech. Dissertation. Department of Biotechnology, Technical University of Denmark, Lyngby.

176. 	Williams, DH, Stone, MJ, Hauck, PR, Rahman, SK. 1989. Why are secondary metabolites (natural products) biosynthesised? J.Nat.Prod. 52: 1189-1208.

177. 	Gloer, JB. 1995. THE CHEMISTRY OF FUNGAL ANTAGONISM AND DEFENSE. Canadian Journal Of Botany-Revue Canadienne De Botanique 73: S1265-S1274

178. 	Smith, JE, Solomons, GL. 1994. Mycotoxins in Human Nutrition and health. European Commision, Directorate-General XII,

179. 	Sorenson, WG. 1989. Health implications of mycotoxins in the home and workplace: an overview. In O'Rear CE, Llewellyn GC. (eds.), Biodeteroriation Research 2. p. 201-215. Plenum, New York.

180. 	Dowd, PF, Miller, JD, Greenhalgh, R. 1989. Toxicity and interactions of some Fusarium graminearum metabolites to caterpillars. Mycologia 81: 646-650.

181. 	Frisvad, JC, Thrane U, Filtenborg O. 1998. Role and use of secondary metabolites in fungal taxonomy. In Frisvad JC, Bridge PD, Arora DK. (eds.), Chemical fungal taxonomy. p. 289-319. Marcel Dekker, New York.

182. 	Ueno, Y. 1985. Toxicology of Mycotoxins. Crit.Rev.Toxicol 14: 99-132.

183. 	Creasia, DA, Thurmann, JD, Wannemacher, RWJ. 1990. Acute inhalation toxicity of T-2 toxin in the rat and guinea pig. Fund.Appl.Tox. 14: 54-59.

184. 	Smedsgaard, J, Frisvad, JC. 1997. Terverticillate penicillia studied by direct electrospray mass spectrometric profiling of crude extracts. I. Chemosystematics. Biochem.Syst.Ecol. 25: 51-64.

185. 	Jong, SC, Davis, EE. 1976. Contribution to the knowledge of Stachybotrys and Memnoniella in cultures. Mycotaxon 3: 409-485.

186. 	McKenzie, EHC. 1991. Dematiaceous hyphomycetes on freycinetia (pandanaceae). 1. Stachybotrys. Mycotaxon 41: 179-188.

187. 	Dorai, M, Vittal, BPR. 1986. A new Stachybotrys from eucalyptus litter. Trans.Brit.Myc.Soc. 87: 642-644.

188. 	Hua-zhong, K. 1997. Stachybotrys yunnanensis sp. Nov. and Neosatorya delicata sp. Nov. isolated from yunna, China. Mycotaxon 62: 427-433.

189. 	Miyazaki, W, Tamaoka, H, Shinohara, M, Kaise, H, Izawa, T, Nakano, Y , Kinoshita, T, Inoue, K. 1980. A complement inhibitor produced by Stachybotrys complementi, nov. sp. K-76, a new species of fungi imperfecti. Microbiol.Immunol 24: 1091-1108.

190. 	Eppley, RM, Bailey, WJ. 1973. 12,13-Epoxy-9-Trichothecenes as the Probable Mycotoxins Responsible for Stachybotryotoxicosis. Science. 181: 758-760.

191. 	Eppley, RM, Mazzola, EP, Highet, RJ, Bailey, WJ. 1977. Structure of Satratoxin H, a metabolite of Stachybotrys atra. Application of Proton and Carbon-13 Nuclear Magnetic Resonance. J.Org.Chem. 42: 240-243.

192. 	Bata, A, Harrach, B, Ujszászi, K, Kis-Tamás, A, Lasztity, R. 1985. Macrocyclic Trichothecene Toxins Produced by Stachybotrys atra Strains Isolated in Middle Europe. Appl.Env.Microb. 49: 678-681.

193. 	Forgacs, J, Carl, WT, Herring, AS, Hinshaw, WR. 1958. Toxicity of Stachybotrys atra for animals. Trans.New York Acad.Soc. 20: 787-808.

194. 	Korpinen, E-L, Uoti, J. 1974. Studies on Stachybotrys alternans. II. Occurence, morphology and toxigenity. Acta Path.Microbiol.Scand.Sec.B. 82: 1-6.

195. 	Sarkisov, AK, Orshanskaiya, VN. 1944. Laboratory diagnosis of toxic strains Stachybotrys alternans. Veterinariya 21: 38-40.

196. 	Forgacs, J. 1972. Stachybotrytoxicosis. In Kadis S, Ciegler A, Ajl SJ. (eds.), Microbial toxins. Vol. VIII. p. 95-128. Academic Press, New York.

197. 	Krustjev, N. 2001.

198. 	Forgacs, J, Carll, WT. 1962. Mycotoxicosis. Adv.Vet.Sci. 7: 273-293.

199. 	Gutzwiller, J, Mauili, R, Sigg, HP, Tamm, C. 1964. Die konstitutionen von verrucarol und roridin C. Helv.Chim.Acta 47: 2234-2262.

200. 	Eppley, RM, Mazzola, EP, Stack, ME, Dreifuss, PA. 1980. Structure of Satratoxin F and Satratoxin G, a metabolites of Stachybotrys atra. Application of Proton and Carbon-13 Nuclear Magnetic Resonance Spectroscopy. J.Org.Chem. 45: 2522-2523.

201. 	Ueno, Y. 1983. Trichothecenes - chemical, biological and toxicological aspects. In. Ueno Y(ed.). Elsevier, Amsterdam.

202. 	Bamburg, JR. 1976. Mycotoxins and Other Fungal Related Food Problems. In Rodricks JV. (ed.), Advances in Chemistry Series 149. p. 144-162. American Chemical Society,

203. 	Trapp, SC, Hohn, TM, McCormick, S, Jarvis, BB. 1998. Characterization of the gene cluster for biosynthesis of macrocyclic trichothecenes in Myrothecium roridum. Mol Gen Genet 257: 421-432.

204. 	Rizzo, I, Varavky, E, Haidukowski, M. 1997. Macrocyclic trichothecenes in Baccharis coridifolia plants and endophytes and Baccharis artemissioides Plants. Toxicon 35: 753-757.

205. 	Zamir, LO. 1989. Biosynthesis of 3-acetylnivalenol and sambucinol. Tetrahedron 45: 2277-2305.

206. 	Desjardins, AE, Hohn, T, McCormick, SP. 1993. Trichothecene Biosynthesis in Fusarium Species: chemistry, genetics, and significance. Microb.Rev. 57: 595-604.

207. 	Fekete, C, Logrieco, A, Giczey, G, Hornok, L. 1997. Screening of fungi for the presence of the trichodiene synthase encoding sequence by hybridization to the Tri5 gene from Fusarium poae. Mycopath. 138: 91-97.

208. 	Wilkins, CK. 2000. Volatile sesquiterpenes from Stachybotrys chartarum. Indicators for trichothecene producing mold species? Env.Sci.Pollut.Res. 7: 77-78.

209. 	Jelen, HH, Latus-Zietkiewicz, D, Wasowicz, E, Kaminski, E. 1997. Trichodiene as a volatile marker for trichothecenes biosynthesis. J.Microbiol.Meth. 31: 45-49.

210. 	Jarvis, BB. 1991. Macrocyclic trichothecenes. In Sharma RP, Salunkhe DK. (eds.), Mycotoxins and Phytoalexins. p. 361-421. CRC Press, Boca Raton.

211. 	Pasanen, A-L, Nikulin, M, Tuomainen, M, Parikka, P, Hintikka, E-L. 1993. Laboratory Experiments on membrane filter sampling of airborne mycotoxins produced by Stachybotrys atra Corda. Atmos.Env. 27A: 9-13.

212. 	Tuomi, T, Reijula, K, Johnsson, T, Hemminki, K, Hintikka, E-L, Lindroos, O, Kalso, S, Koukila-Kähköla, P, Mussalo-Rauhamaa, H, Haahtela, T. 2000. Mycotoxins in crude building materials from water-damaged buildings. Appl.Env.Microb. 66: 1899-1904.

213. 	Andriienko, OV, Zaichenko, OM. 1997. Certain peculiarities of biological action of the stachybotryotoxin preparations. Mikrobiol.Z. 59: 41-46.

214. 	Jarvis, BB, Lee, Y-W, Comezoglu, SN, Yatawara, CS. 1986. Trichothecenes Produced by Stachybotrys atra from Eastern Europe. Appl.Env.Microb. 51: 915-918.

215. 	Hinkley, SF, Jiang, J, Mazzola, EP, Jarvis, BB. 1999. Atranones: Novel diterpenoids from the toxigenic mold Stachybotrys atra. Tetrahedron Lett. 40: 2725-2728.

216. 	Yang, GH, Jarvis, BB, Chung, YJ, Pestka, JJ. 2000. Apoptosis induction by the satratoxins and other trichothecene mycotoxins: relationship to ERK, p38 MARK, and SAPK/JNK activation. Toxicol.Appl Pharmacol. 164: 149-160.

217. 	Parent-Massin, D, Parchment, RE. 1998. Haematotoxicity of mycotoxins. Rev.Med.Vet. 149: 591-598.

218. 	Hughes, BJ, Hsieh, GC, Jarvis, BB. 1989. Effects of macrocyclic Trichothecene Mycotoxins on the Murine immune System. Arch.Env.Contam.Tox. 18: 388

219. 	Pestka, JJ, Bondy, GS. 1990. Alternations of immune function following dietary mycotoxin exposure. Can.J.Physiol.Pharmac. 68: 1009-1016.

220. 	Creasia, DA, Thurmann, JD, Jones III, LJ, Nealley, ML, York, CG, Wannemacher, RWJ, Bunner, DL. 1987. Acute Inhalation Toxicity of T-2 mycotoxin i Mice. Fund.Appl.Tox. 8: 230-235.

221. 	Pang, VF, Lambert, RJ, Felsburg, PJ. 1988. Experimental T-2 toxicosis in swine following inhalation exposure: clinical signs and effect on hematology, serum biochemistry and immune response. Fund.Appl.Tox. 11: 100-109.

222. 	Nikulin, M, Reijula, K, Jarvis, BB, Veijalaninen, P, Hintikka, E-L. 1997. Effects of intranasal exposure to spores of Stachybotrys atra in mice. Fund.Appl.Tox. 35: 182-188.

223. 	Mason, CD, Rand, TG, Oulton, M, MacDonald, JM, Scott, JE. 1998. Effects of Stachybotrys chartarum (atra) conidia and isolated toxin on lung surfactant production and homeostasis. Natural Toxins 6: 27-33.

224. 	Mason, CD, Rand, TG, Oulton, M, MacDonald, J, Anthes, M. 2001. Effects of Stachybotrys chartarum on surfactant convertase activity in juvenile mice. Toxicol.Appl Pharmacol. 172: 21-28.

225. 	Rao, CY, Brain, JD, Burge, HA. 2000. Reduction of pulmonary toxicity of Stachybotrys chartarum spores by methanol extraction of mycotoxins. Appl.Env.Microb. 66: 2817-2821.

226. 	Roggo, BE, Hug, P, Moss, S, Stämpfli, A, Kriemler, H-P, Peter, HH. 1996. Novel spirodihydrobenzofuranlactams as antagonists of endothelin and as inhibitors of HIV-1 protease produced by Stachybotrys sp. II. Structure determination. J.Antib. 49: 374-379.

227. 	Tomishige, T, Miyazaki, K.1992.Tumor necrosis factor-liberation inhibitors containing sesquiterpene analogs or their salts.  Application: JP  90-116524  19900501.

228. 	Kaise, H, Shinohara, M, Miyazaki, W, Izawa, T, Nakano, Y, Sugawara, M, Sugiura, K, Sasaki, K. 1979. Structure of K-76, a complemet inhibitor. J.Chem.Soc.,Chem.Com. 726-727.

229. 	Kaneto, R, Dobashi, K, Kojima, I, Sakai, K , Shibamoto, N, Yoshioka, T, Nishid, AH, Okamoto, R, Akagawa, H, Mizuno, S. 1994. Mer-nf5003b, mer-nf5003e and mer-nf5003f, novel sesquiterpenoids as avian-myeloblastosis virus protease inhibitors produced by Stachybotrys sp. J.Antib. 47: 727-730.

230. 	Hasumi, K, Ohyama, S, Kohyama, T, Ohsaki, Y, Takayasu, R, Endo, A. 1998. Isolation of SMTP-3, 4, 5 and -6, novel analogs of staplabin, and their effects on plasminogen activation and fibrinolysis. J.Antib. 1059-1068.

231. 	Hu, W, Ohyama, S, Hasumi, K. 2000. Activation of fibrinolysis by SMTP-7 and -8, novel staplabin analogs with a pseudosymmetric structure. J.Antib. 53: 241-247.

232. 	Kohyama, T, Hasumi, K, Hamanaka, A, Endo, A. 1997. SMTP-1 and -2, novel analogs of staplabin produced by Stachybotrys microspora IFO30018. J.Antib. 50: 172-174.

233. 	Hinkley, SF, Mazzola, EP, Fettinger, JC, Lam, YKT, Jarvis, BB. 2000. Atranones A-G, from the toxigenic mold Stachybotrys chartarum. Phytochem 55: 663-673.

234. 	Rodriguez, AD, González, E, Ramírez, C. 1998. The structural chemistry, reactivity, and total synthesis of dolabellane diterpenes. Tetrahedron  54: 11683-11729.

235. 	Vesper, SJ, Dearborn, DG, Yike, I, Allen, T, Sobolewski, J, Hinkley, SF, Jarvis, BB, Haugland, RA. 2000. Evaluation of Stachybotrys chartarum in the House of an Infant with Pulmonary Hemmorrhage: Quantitative Assessment before, during, and after Remediation. J.Urb.Health 77: 68-85.

236. 	Sakamoto, K, Tsujii, E, Miyauchi, M. 1993. FR901459, a novel immunosuppressant isolated from Stachybotrys chartarum No. 19392. Taxonomy of the producing organism, fermentation, isolation, physicochemical properties and biological activities . J.Antib. 46: 1788-1798.

237. 	Peltola, J, Anderson, MA, Raimo, M, Mussalo-Rauhamaa, H, Salkinoja-Salonen, M. 1999. Membrane toxic substances in water-damaged construction materials and fungal pure cultures. In Johanning E (Ed.), Eastern New York Occupational & Environmental Health Center, New York,  p. 432-443.

238. 	Vesper, SJ, Dearborn, DG, Yike, I, Sorenson, WG, Haugland, RA. 1999. Hemolysis, toxicity, and randomly amplified polymorphic DNA analysis of Stachybotrys chartarum strains. Appl.Env.Microb. 3175-3181.

239. 	Vesper, SJ, Magnuson, ML, Dearborn, DG, Yike, I, Haugland, RA. 2001. Initial Characterization of the Hemolysin Stachylysin from Stachybotrys chartarum. Infect.immun. 69: 912-916.

240. 	Otto, BR, Verweij-van, MJJ, Maclaren, DM. 1992. Transferrins and the heme-compounds as iron source from phatogenic bacteria. Crit.Rev.Microbiol. 18: 217-233.

241. 	Bullen, JJ. 1981. The significance of ion in infections. Rev.Infect.Dis. 3: 1127-1138.

242. 	Payne, SM, Finkelstein, RA. 1978. The critical role of iron in host-bacterial interactions. J.Clin.Invest. 61: 1428-1440.

243. 	Weinberg, ED. 1978. Iron and infections. Microb.Rev. 42: 45-66.

244. 	Holzberg, M, Artis, WM. 1983. Hydroxamate siderophore production by opportunistic and systemic fungal phatogens. Infect.immun. 40: 1134-1139.

245. 	Raper, KB, Fennell, DI. 1977. The Genus Aspergillus.  Robert E. Kriger Publishing Company, New York.

246. 	Integration of modern taxonomic methods from Penicillium and Aspergillus classification2000. In Samson RA, Pitt JI(Eds.). Harwood academic publishers, Amsterdam.

247. 	Modern concepts in Penicillium and Aspergillus classification1990. In Samson RA, Pitt JI(Eds.). Plenum Press, New York.

248. 	Sunesson, A-L, Nilsson, C-A, Carlson, R, Blomquist, G, Andersson, B. 1997. Production of volatile metabolites from Streptomyces albidoflavus cultivated on gypsum board and tryptone glucose extract agar - Influence of temperature, oxygen and carbon dioxide levels. Ann.Occup.Hyg. 41: 393-413.

249. 	Kikuchi, T, Shigetoshi, K, Suehara, H, Nishi, A, Tsubaki, K. 1981. Odorous metabolite of a fungus, Chaetomium globosum, Kinze ex Fr. Identification of geosmin, a musty-smelling compound. Chem.Pharm.Bull. 29: 1782-1784.

250. 	Bjurman, J, Kristensson, J. 1992. Volatile production by Aspergillus versicolor as a possible cause of odor in houses affected by fungi. Mycopath. 118: 173-178.

251. 	Steyn, PS. 1998. The biosynthesis of mycotoxins. Rev.Med.Vet. 149: 469-478.

252. 	McConnell, IR, Garner RC. 1994. DNA adducts of aflatoxins, sterigmatocystins and other mycotoxins. In Hemminki K, Dipple A, Shuker DEG, Kadlubar FF, Segerbäck D, Bartsch H. (eds.), DNA adducts: Identification and Biological Significance. IARC Scientific publication No. 125. p. 29-55. IARC, Lyon.

253. 	Jesenská, Z, Bernat, D. 1994. Effect of Mycotoxins on in Vitro Movement of Tracheal Cilia from One-Day-Old Chicks. Folia Microbiologica 39: 155-158.

254. 	Piecková, E, Jesenská, Z. 1998. Mold on house walls and the effect of their chloroform-extractable metabolites on the respiratory cilia movement of one-day-old chicks in vitro. Folia Microbiologica 63: 672-678.

255. 	Bokhari, FM, Flannigan B. 1996. Effect of storage environments on growth of Aspergillus versicolor and sterigmatocystin production in cereals. Proceedings of the Tenth International Biodeterioration and Biodegradation Symposium. p. 287-293. DECHEMA, Frankfurt am Main.

256. 	Ohmomo, S, Sugita, M, Abe, M. 1973. Isolation of cyclopiazonic acid, cyclopiazonic acid imine and bissecodehydrocycpiazonic acid from cultures of Aspergillus versicolor (Vuill.) Tiraboschi. J.Agric.Chem.Jpn. 47: 57-63.

257. 	Kingston, GD, Chen, PN, Vercellotti, JR. 1976. Metabolites of Aspergillus versicolor: 6,8-dimethylnidurufin, griseofulvin, dechlorogriseofulvin and 33,8.dihydroxy-6-methylxanthone. Phytochem 1037-1039.

258. 	Jesus, AE, Horak, RM, Steyn, PS, Vleggaar, R. 1987. Metabolites of Aspergillus ustus. Part 4. Stable isotope labeling on the biosyntheisi of the austalides. J.Chem.Soc.Perkin I 2253-2257.

259. 	Steyn, PS, Vleggaar, R. 1975. Dihydrofuro[3',s': 4,5]furo,3,2-b-xanthenones: the structures of austocystins G, H and I. Journal of South Afric.Chem.Inst. XXVIII: 375-377.

260. 	Vleggaar, R, Steyn, PS, Nagel, DW. 1974. Constitution and absolute configuration of austdiol, the main toxic metabolite from Aspergillus ustus. J.Chem.Soc.Perkin I 1: 45-49.

261. 	Steyn, PS. 1973. The structures of five diketopiperazines from Aspergillus ustus. Tetrahedron 29: 107-120.

262. 	Steyn, PS, Vleggaar, R. 1976. The structure of dihydrodeoxy-8-epi-austdiol and the absolute configuration of the azaphilones. J.Chem.Soc.Perkin I 204-206.

263. 	Steyn, PS, Vleggaar, R. 1974. Austocystins. Six novel dihydrofuro[3',s': 4,5]furo,3,2-b-xanthenones: from Aspergillus ustus. J.Chem.Soc.Perkin I 1: 2250-2256.

264. 	Singh, SB, Smith, JL, Sabnis, GS, Dombrowski, AW, Schaeffer, JM, Goetz, MA, Bills, GF. 1991. Structure and conformation of ophiobilin K and 6-epiophioboiln K from Aspergillus ustus as a nematocidal agent. Tetrahedron Lett. 47: 6931-6938.

265. 	Cutler, HG, Crumley, FG, Cox, RH, Springer, JP, Arrendale, RF, Cole, RJ, Cole, PD. 1984. Ophibolins G and H: New fungal metabolites from a novel source Aspergillus ustus. J Agr.Food Chem. 32: 778-782.

266. 	Kohno, J, Sakurai, M, Kameda, N, Shi, N, Matsubara, S. 1999. Production, isolation and biologically properties of TMC-120A, B and C, novel inhibitors of eosinophil survival from Aspergillus ustus. J.Antib. 52: 913-916.

267. 	Kohno, J, Hiramatsu, H, Nishio, M. 1999. Structures of TMC-120A, B and C, Novel Isoquinoline Alkaloids from Aspergillus ustus TC 1118. Tetrahedron 55: 11247-11252.

268. 	Varga, J, Kevei F, Hamari Z, Toth B, Teren J, Croft JH,  Kozakiewicz Z. 2000. Genotypic and phenotypic variability among black Aspergilli. In Samson RA, Pitt JI. (eds.), Integration of modern taxonomic methods from Penicillium and Aspergillus classification. p. 397-411. Harwood academic publishers, Amsterdam.

269. 	Kobbe, B, Cushman, M, Wogan, GN, Demain, AL. 1977. Production and antibacterial activity of malformin C, a toxic metabolite of Aspergillus niger. Appl.Env.Microb. 33: 996-997.

270. 	Kim, K-W, Sugawara, F, Yoshida, S, Murofushi, N, Takahashi, N, Curtis, RW. 1993. Structure of malformin B, a phytotoxic metabolite produced by Aspergillus niger. Biosci.Biotech.Biochem. 57: 787-791.

271. 	Richard, JL, Plattner, RD, Mary, J, Liska, SL. 1999. The occurrence of Ochratoxin A in dust collected from a problem household. Mycopath. 146: 99-103.

272. 	Ren, P, Ahearn, DG, Crow, SA. 1999. Comparative study of Aspergillus mycotoxin production on enriched media and construction material. J ind.microbiol.biotechnol. 23: 209-213.

273. 	Rao, CY, Fink, RC, Wolfe, LB, Liberman, DF, Burge, HA. 1997. A study of aflatoxin production by Aspergillus flavus growing on wallboard. J.Am.Biolog.Safety Assoc. 2: 36-42.

274. 	Land, CJ, Hult, K, Fuchs, R, Hagelberg, S, Lundström, H. 1987. Tremorgenic mycotoxins from Aspergillus fumigatus as a possible occupational health problems in sawmills. Appl.Env.Microb. 53: 787-790.

275. 	Pitt, JI, Samson RA, Frisvad JC. 2000. List of accepted species and their synonyms in the family Trichocomaceae. In Samson RA, Pitt JI. (eds.), Integration of modern taxonomic methods from Penicillium and Aspergillus classification. p. 9-49. Harwood academic publishers, Amsterdam.

276. 	Skouboe, P, Frisvad, JC, Taylor, JW, Lauritsen, D, Boysen, M, Rossen, L. 1999. Phylogenetic analysis of nucleotide sequences from the ITS region of terverticillate Penicillium species. Mycol.Res. 103: 873-881.

277. 	Frisvad, JC, Filtenborg O. 1990. Revision of Penicillium Furcatum based on secondary metabolites and conventional characters. In Samson RA, Pitt JI. (eds.), Modern concepts in Penicillium and Aspergillus classification. p. 159-172. Plenum Press, New York.

278. 	Frisvad, JC, Filtenborg O. 1990. Secondary metabolites as consistent criteria in Penicillium taxonomy and a synoptic Penicillium subgenus  Penicillium. In Samson RA, Pitt JI. (eds.), Modern concepts in Penicillium and Aspergillus classification. p. 373-384. Plenum Press, New York.

279. 	Frisvad, JC, Filtenborg O, Lund F, Samson RA. 2000. The momogeneous species and series in subgenus Penicillium  are related tom mammal nutrition and excretion. In Samson RA, Pitt JI. (eds.), Integration of modern taxonomic methods from Penicillium and Aspergillus classification. p. 265-283. Harwood academic publishers, Amsterdam.

280. 	Domsch, KH, Gams, W, Anderson, T-H. 1980. Compendium of soil fungi.  Academic Press, London.

281. 	Steyn, PS. 1970. The isolation, structure and absolute configuration of secalonic acid D, the toxic metabolite of Penicillium oxalicum. Tetrahedron 26: 51-57.

282. 	Andersen, R, Büchi, G, Kobbe, B, Demain, AL. 1977. Secalonic acids D and F are toxic metabolites of Aspergillus aculeatus. J.Org.Chem. 42: 352-353.

283. 	Kurobane, I, Vining, LC, McInnes, AG. 1979. Biosynthetic relationships among the secalonic acids. Isolation of emodin, endocrin and secalonic acids from Pyrenochaeta terrestris and Aspergillus aculeatus. J.Antib. 31: 1256-1266.

284. 	Frisvad, JC, Filtenborg, O. 1983. Classification of Terverticillate Penicilia based on profile of Mycotoxins and other Secondary Metabolites. Appl.Env.Microb. 46: 1301-1310.

285. 	Dai, MC, Tabacchi, R, Saturnin, C. 1993. Nitrogen-containing aromatic compounds from the culture medium of Penicillium chrysogenum Thom. Chimai 47: 226-229.

286. 	Stolk, AC, Samson RA, Frisvad JC, Filtenborg O. 1990. The systematics of the terverticillate Penicillia. In Samson RA, Pitt JI. (eds.), Modern concepts in Penicillium and Aspergillus classification. p. 121-137. Plenum Press, New York.

287. 	Bentley, R. 2000. Mycophenolic acid:  A one hundred year Odyssey from antibiotic to immunosuppressant. Chem.Rev. 100: 3801-3825.

288. 	Fujimoto, Y, Kamiya, M, Tsunoda, H, Ohtsubo, K, Tatsuno, T. 1980. Reserche toxicologique des substances metaboliques de Penicillium carneo-lutescens. Chem.Pharm.Bull. 248: 1062-1067.

289. 	Moreau, S, Lablache-Combier, A, Biguet, J, Foulon, C, Delfosse, M. 1982. Botrydiplodin, a mycotoxin synthetised by a strain of P. roqueforti. J.Org.Chem. 47: 2358-2359.

290. 	Moule, Y, Decloitre, F, Hamon, G. 1981. Mutagenicity of the mycotoxin botryodiplodin in the Salmonella typhimurium/Microsomal activation test. Env.Mutagen. 3: 287-291.

291. 	Castillo, M-A, Moya, P, Couillaud, F, Carcera, MD, Marinez-Pardo, R. 1998. A heterocyclic oxime from a fungus with anti-juvenile hormone activity. Arch.Insect Biochem.Physiol 37: 287-294.

292. 	Macias, FA, Varela, RM, Simonet, AM, Cutler, HG, Cutler, SJ, Ross, SA, Dunbar, DC, Dugan, FM, Hill, RA. 2000. Allelochemicals from New Zealand fungi. (+)-Brevione A. The first member of a novel family of bioactive spiroditerpenoids isolated from Penicillium brevicompactum Dierckx. Tetrahedron Lett. 41: 2683-2686.

293. 	Moya, P, Primo-Yufera, E. 1997. Brevioxime: A New Juvenile Hormone Biosynthesis Inhibitor Isolated from Penicillium brevicompactum. J.Org.Chem. 62: 8544-8545.

294. 	Frisvad, JC, Lund F. 1993. Toxic and secondary metabolite production by Penicillium species growing in stored cereals. In Scudamore KA. (ed.), p. 146-171. Central Science Laboratory, Berks.

295. 	Lund, F, Frisvad, JC. 1994. Chemotaxonomy of Penicillium aurantiogriseum and related species. Mycol.Res. 98: 481-492.

296. 	Steyn, PS, Vleggaar, R. 1985. Tremorgenic mycotoxins. Fortschr.Chem Org.Naturst. 48 : 1-80.

297. 	Sorenson, WG, Simpson, JP. 1986. Toxicity of penicillic acid for rat alveolar macrophages. Environmental Research 41: 505-513.

298. 	Nielsen, KF, Gravesen, S, Nielsen, PA, Andersen, B, Thrane, U, Frisvad, JC. 1999. Production of mycotoxins on artificially and naturally infested building materials. Mycopath. 145: 43-56.

299. 	Land, CJ, Hult, K. 1987. Mycotoxin production by some wood-associated Penicillium spp. Lett.Appl.Microbiol 4: 41-44.

300. 	Bourdiol, D, Escolula, L, Salvayre, R. 1990. Effects on patulin on microbicidal activity of mouse peritoneal macrophages. Food Chemical Toxicology  28: 29-33.

301. 	Godtfredsen, WO, Vangedal, S. 1964. Trichodermin, a new Antibiotic, Related to Trichothecin. Proc.Chem.Soc. 188-188.

302. 	Godtfredsen, WO, Vangedal, S. 1965. Trichodermin, a new Sesquiterpene Antibiotic. Acta Chem.Scand. 19: 1088-1102.

303. 	Corley, DG, Miller-Wideman, M, Durley, RC. 1994. Isolation and structure if harzianum A: A new Trichothecene from Trichoderma harzianum. J.Nat.Prod. 57: 442-425.

304. 	Cvetnic, Z, Pepelnjak, S. 1997. Distribution and Mycotoxin-producing ability of some fungal isolates from the air. Atmos.Env. 31: 491-495.

305. 	Dennis, C, Webster, J. 1971. Antagonistic properties of species-groups of Trichoderma. I. Production of non-volatile antibiotics. Trans.Brit.Myc.Soc. 57: 25-39.

306. 	LIN, A, Chen, CK, Chen, YJ. 1991. Molecular action of tricholin, a ribosome-inactivating protein isolated from Trichoderma viride. Mol.Micro. 5: 3013

307. 	Hou, CT, Ciegler, A, Hesseltine, CW. 1972. New mycotoxin, trichotoxin A, from Trichoderma viride isolated from southern leaf blight-infected corn. App.Microb. 23: 183-185.

308. 	Brückner, H, König, WA, Greiner, M, Jung, G. 1979. The sequences of the membrane-modifying peptide antibiotic trichotoxin A-40. Angew.Chem Int Ed.Engl. 18: 476-477.

309. 	Haugland, RA, Vesper, SJ, Harmon, SM. 2001. Phylogenetic relationship of Memnoniella and Stachybotrys species and evaluation of morphological features for Memnoniella species identification. Mycologia 93: 54-65.

310. 	Hinkley, SF, Fettinger, JC, Dudley, K, Jarvis, BB. 1999. Memnobotrins and Memnoconols: Novel Metabolites from Memnoniella echinata. J.Antib. 52: 988-997.

311. 	Lam, YKT, Wichman, CF, Huang, L, Burg, RW, Monagham, RL, Jackson, R, Reid, G, Maguire, JJ, McKnight, AJ, Ragan, CI. 1992. A novel inositol mono-phosphatase inhibitor from Memnoniella echinata. J.Antib. 45: 1397-1403.

312. 	Giocobbe, RA, Huang, L, Kong, YL, Lam, YT, Del, SM, Wichman, CF.1991.Drug for treating manic depression. 4981980.,US  89-407162  19890914.

313. 	Stefanelli, S, Sponga, F, Ferrari, P, Sottani, C, Corti, E, Brunati, C, Islam, K. 1996. Inhibitors of myo-inositol monophosphatase, ATCC 20928 factors A and C isolation, physicochemical characterization and biological properties. J.Antib. 49: 611-616.

314. 	Jarvis, BB, Zhou, Y, Jiang, J, Wang, S, Sorenson, WG, Hintikka, E-L, Nikulin, M, Parikka, P, Etzel, RA, Dearborn, DG. 1996. Toxigenic Moulds in Water-Damaged Buildings: Dechlorogriseofulvins from Memnoniella echinata. J.Nat.Prod. 59: 553-554.

315. 	Woody, MA, Chu FS. 1992. Toxicology of Alternaria mycotoxins. In Chelkowski J, Visconti A. (eds.), Alternaria. Biology, plant disease and metabolites. p. 409-434. Elsevier, Amsterdam.

316. 	Caldas, ED, Jones, AD, Ward, B, Winter, CK , Gilchrist, DG. 1994. Structural characterization of three new AAL toxins produced by Alternaria alternata f.sp. lycopersici. J Agr.Food Chem. 42: 327-333.

317. 	Winter, CK, Gilchrist, DG, Dickman, MB, Jones, C. 1996. Chemistry and biological activity of AAL toxins. Adv.Exp.Med.Biol. 392: 307-316.

318. 	Chen, J, Mirocha, CJ, Xie, W, Hogge, LR, Olson, D. 1992. Production of the mycotoxin fumonisin B1 by Alternaria alternata f. sp. lycopersici. Appl.Env.Microb. 58: 3928-3931.

319. 	Grogan, RG, Kimble, KA, Misaghi, I. 1975. A stem canker disease of tomato caused by Alternaria alternata f. sp. lycopersici. Phytopathology 65: 880-886.

320. 	Shepard, GS, Thiel, PG, Marasas, WFO, Sydenham, EW. 1993. Isolation and determination of AAL phytotoxins from corn cultures of the fungus Alternaria alternata f. sp. lycopersici. J.Chrom. 641 : 95-100.

321. 	Shier, WT, Abbas, H, Mirocha, CJ. 1991. Toxicity of the mycotoxins fumonisins B1 and B2 and Alternaria alternata f.sp. lycopersici toxin (AAL) in cultured mammalian cells. Mycopath. 116: 97-104.

322. 	Ren, P, Ahearn, DG, Crow, SA. 1998. Mycotoxins of Alternaria alternata produced on ceiling tiles. J.Ind.Microb. 20: 53-54.

323. 	Udagawa, S. 1984. Taxonomy of mycotoxin-producing Chaetomium. In Kurata H, Ueno Y. (eds.), Toxigenic Fungi - Their toxins and health hazard. p. 139-147. Elsevier, Amsterdam.

324. 	Koyama, K, Natori, S. 1987. Chaetochromins B, C and D, bis(naphtho-gamma-pyrone) derivatives from Chaetomium gracile. Chem.Pharm.Bull. 35: 578-584.

325. 	Sekita, S, Yoshihira, K, Natori, S, Udagawa, S, Muroi, T, Sugiyama, Y, Kurata, H, Umeda, M. 1981. Mycotoxin production by Chaetomium spp. and related fungi. Can.J.Microbiol. 27: 766-772.

326. 	Achatz, G, Oberkofler, H, Lechenauer, E. 1995. Molecular cloning of major and minor allergens of Alternaria alternata and Cladosporium herbarum. Mol.Immunol. 32: 213-227.

327. 	Bjurman, J. 1993. Determination of microbial activity in moulded wood by the use of fluorescin diacetate. ? 1-16.

328. 	Miller, M, Palojärvi, A, Rangger, A, Reeslev, M, Kjøller, A. 1998. The use of fluorogenic substrates to measure fungal presence and activity in soil. Appl.Env.Microb. 64: 613-617.

329. 	Notermans, S. 1988. (1-5)-linked beta-D-galactosidases are immunodominant in extracellular polysaccharides of Penicillium and Aspergillus species. Mol.Immunol. 25: 975-979.

330. 	Sunesson, A-L, Nilsson, C-A, Andersson, B, Blomquist, G. 1996. Volatile metabolites produced by two fungal species cultivated on building materials. Ann.Occup.Hyg. 40: 397-410.

331. 	Swift, MJ. 1973. The estimation of mycelial biomass by determination of hexosamine content of wood tissue decayed by fungi. Soil Biol Biochem. 5: 321-332.

332. 	Szponar, B, Larsson, L. 2000. Determination of Microbial Colonisation in Water-Damaged buildings using chemical Marker analysis by gas chromatography - mass spectrometry. Indoor Air 10: 13-18.

333. 	Miller, JD, Young, JC. 1997. The use of ergosterol to measure exposure to fungal propagules in indoor air. Am Ind.Hyg.Assoc.J 58: 39-43.

334. 	Johanning, E, Gareis, M, Chin, YS, Hintikka, E-L, Jarvis, BB, Dietrich, R. 1998. Toxicity screening of materials from buildings with fungal indoor air quality problems (Stachybotrys chartarum). Mycotoxin Res. 14: 60-73.

335. 	Hanelt, MM, Gareis, M, Kollarczik, B. 1994. Cytotoxicity of mycotoxin evaluated by the MTT cell-culture assay. Mycopath. 128: 167-174.

336. 	Yike, I, Allan, T, Sorenson, WG, Dearborn, DG. 1999. Highly sensitive protein translation assay for trichothecene toxicity in airborne particulates: Comparison with cytotoxicity assays. Appl.Env.Microb.  65: 88-94.

337. 	Mercer, EI, Barlett, K. 1974. Sterol esters of Phycomyces blakesleeanus. Phytochem 14: 1099-1105.

338. 	Rezanka, T. 1992. Analysis of sterol esters from alga and yeast by high- performance liquid chromatography and capillary gas chromatography-mass spectrometry with chemical ionization. J.Chrom. 598: 219

339. 	Bermingham, S, Maltby, L, Cooke, RC. 1995. A critical assessment of the validity of ergosterol as an indicator of fungal biomass. Mycol.Res. 99: 479

340. 	Gessner, MO, Chauvet, E. 1993. Ergosterol-to-biomass conversion factors for aquatic hyphomycetes. Appl.Env.Microb. 59: 502-507.

341. 	Newell, SY. 1995. Minimizing Ergosterol Loss during Preanalytical Handling and Shipping of Samples of Plant Lit. Appl.Env.Microb. 61: 2794

342. 	Suberkopp, K, Gessner, MO, Chauvet, E. 1993. Comparison of ATP and ergosterol as indicators of fungal biomass associated with decomposing leaves in streams. Appl.Env.Microb. 59: 3367-3372.

343. 	Davis, MW, Lamar, RT. 1992. Evaluation of methods to extract ergosterol for quantification of soil fungal biomass. Soil Biol Biochem. 24: 189

344. 	Young, JC. 1995. Microwave-assisted extraction of the fungal metabolites ergosterol and total fatty acids. J Agr.Food Chem. 43: 2904-2910.

345. 	Gessner, MO, Schmitt, AL. 1996. Use of Solid-Phase Extraction To Determine Ergosterol Concentrations in Plant Tissue Colonized by Fungi. Appl.Env.Microb. 62: 415

346. 	Axelsson, B-O, Saraf, A, Larsson, L. 1995. Determination of ergosterol in organic dust by gas chromatography-mass spectrometry. J.Chrom.B 666: 77-84.

347. 	Saraf, A. 1999. Microorganisms in the indoor environment. Analysis and structure-bioactivity relationships. Dissertation, Department of infectious diseases and microbiology, University of Lund, Sweden.

348. 	Pasanen, A-L, Yli-Peitla, K, Pasanen, P, Kalliokoski, P, Tarhanen, J. 1999. Ergosterol content in various fungal species and biocontaminated building materials. Appl.Env.Microb. 65: 138-142.

349. 	Saraf, A, Larsson, L. 1996. Use of gas chromatography/ion-trap tandem mass spectrometry for the determination of chemical markers of microorganisms in organic dust. Journal of Mass spectrometry 31: 389-396.

350. 	Dales, RE, Miller, JD. 1999. Residential Fungal Contamination and Health: Microbial Cohabitants as Covariates. Env.Health Persp.Supp. 107: 481-483.

351. 	Chu, FS. 1992. Resent Progress on analytical techniques for mycotoxins in feedstuffs. J Anim.Sci 70: 3950-3963.

352. 	Gilbert, J. 1993. Recent advances in analytical methods for mycotoxins. Food addit.contam. 10: 37-48.

353. 	Lin, L, Zhang, J, Wang, P, Wang, Y, Chen, J. 1998. Thin-layer chromatography of mycotoxins and comparison with other chromatographic methods. J.Chrom.A 815: 3-20.

354. 	Langseth, W, Rundberget, T. 1998. Instrumental methods for determination of nonmacrocyclic trichothecenes in cereals, foodstuffs and cultures. J.Chrom.A 815: 103-121.

355. 	Novak, TJ, Quinn-Dogget, K. 1991. 2-(Diphenylacetyl)-1,3-indanedione-1-hydrozone (dipain) derivatives for detection of trichothecene mycotoxins. Analytical Letters 24: 913-924.

356. 	Ramakrishna, Y, Bhat, RV. 1987. Comparison of different spray reagents for the identification of trichothecenes. Curr Sci 56: 524-526.

357. 	Sano, A, Asabe, Y, Takatani, S, Ueno, Y. 1982. Fluorodensitometric determination of trichothecene mycotoxins with nicotinamide and 2-acetylpyridine on a silica gel layer. J.Chrom. 235: 257-265.

358. 	Takatani, S, Asabe, Y, Kato, T, Suzuki, M, Ueno, Y. 1979. Spectrodensitometric determination of trichothecene mycotoxins with 4-(p-nitrobenzyl)pyridine on silica gel thin-layer chromatograms. J.Chrom. 172: 355-342.

359. 	Yagen, B, Sintov, A, Bialer, M. 1986. New, Sensitive thin-layer chromatographic-high-performance liquid chromatographic method for detection of trichothecene mycotoxins. J.Chrom. 356: 195-201.

360. 	Septien, I, Blanco, JL, Suratz, G, Cutuli., MT. 1994. Solubility and stability of sterigmatocystin in aqueous solutions. Mycotoxin Res. 10: 15-20.

361. 	Scott, PM. 1993. Gas Chromatography of Mycotoxins. In Betina V. (ed.), Chromatography of Mycotoxins: Techniques and applications. Journal of Chromatography Library, Vol 54. p. 3-11. Elsevier, Amsterdam.

362. 	Giddings, JC. 1991. Unified Separation Science.  John Wiley & Sons, Inc, New York.

363. 	Scott, PM. 1993. Methods for the detection and determination of nitrogen-containing mycotoxins. ? 617-625.

364. 	Scott, PM, Weber, D, Kanhere, SR. 1997. Gas chromatography-mass spectrometry of some Alternaria mycotoxins. J.Chrom.A 765: 255-263.

365. 	Thorpe, CW, Johnson, RL. 1974. Analysis of penicillic acid by gas-liquid chromatography. J Assoc.Off.Anal.Chem 57: 861-865.

366. 	Rychlik, M, Schieberle, P. 1999. Quantitation of the mycotoxin patulin by a stable isotope dilution assay. J Agr.Food Chem. 47: 3749-3755.

367. 	Begley, P, Foulger, BE, Jeffery, PD, Black, RM, Read, RW. 1986. Detection of trace levels of trichothecenes in human blood using capillary gas chromatography-electron-capture negative ion chemical ionisation mass spectrometry. J.Chrom. 367: 87-1014.

368. 	Black, RM, Clarke, RJ, Read, RW. 1986. Detection of trace levels of trichothecene mycotoxins in human urine by gas chromatography-mass spectrometry. J.Chrom. 367: 103-115.

369. 	D'agostino, PA, Provost, LR, Drover, DR. 1986. Analysis of trichothecene mycotoxins in human blood by capillary column gas chromatography-ammonia chemical ionization mass spectrometry. J.Chrom. 367: 77-86.

370. 	Mirocha, CJ, Pawliszyn J, Hewetson DW. 1986. Gas chromatography/mass spectral analysis of trichothecenes. In Richard JL, Thurston JR. (eds.), p. 305-322. Kluwer, Dordrecht.

371. 	Rosen, J, Rosen, RT, Hartman, TG. 1986. Capillary gas chromatography-mass spectrometry of several macrocyclic trichothecenes. J.Chrom. 355: 241-251.

372. 	Krishnamurthy, T, Sarver, WE, Greene, SL, Jarvis, BB. 1987. Mass Spectral Investigation on Trichothecene Mycotoxins. II. Detection and Quantification of Macrocyclic Trichothecenes by Gas Chromatography/Negative Ion Chemical Ionization Mass Spectrometry. J.AOAC. 70: 132-140.

373. 	Scott, PM, Lombaert, GA, Pellaers, P, Bacler, S, Kanhere, SR, Sun, WF, Lau, P-Y, Weber, D. 1989. Application of capillary gas chromatography to a survey of wheat for five trichothecenes. Food addit.contam. 6: 489-500.

374. 	Schwandorf, K, Müller, H-M. 1991. Determination of Trichothecenes in Cereals by Gas Chromatography with Ion Trap Detection. Chromatographia 32: 137-143.

375. 	Möller, TE, Gustavsson, HF. 1992. Determination of Type A and Type B Trichothecenes in cereal by gas chromatography with electron capture detection. J AOAC Int. 75: 1049-1053.

376. 	Seidel, V, Fraissler, S, Lang, C, Schiller, K, Lindner, FW. 1993. Analysis of trace levels of trichothecene mycotoxins in Austrian cereals by gas chromatography with electron capture detection. Chromatographia 37: 191-201.

377. 	Croteau, SM, Prelusky, DB, Trenholm, HL. 1994. Analysis of Trichothecene Mycotoxins by gas chromatography with Electron Capture Detection. J Agr.Food Chem. 42: 926-933.

378. 	Furlong, EB, Soares, LMV. 1995. Gas Chromatographic method for Quantitation and Confirmation of Trichothecenes in Wheat. J.AOAC. 78: 386-390.

379. 	Ryu, J-S, Yang, J-S, Song, Y-S, Kwon, O-S, Park, J, Chang, I-M. 1997. Survey of natural occurrence of trichothecene mycotoxins and zearaleone in Korean cereals harvested in 1993 using gas Chromatography/mass spectrometry. Food addit.contam. 13: 333-341.

380. 	Schollenberger, M, Lauber, U, Jara, HT, Suchy, S, Drocher, W, Müller, H-M. 1998. Determination of eight trichothecenes by gas chromatography-mass spectrometry after sample clean-up by a two stage solid-phase extraction. J.Chrom.A 815: 123-132.

381. 	Lee, RK, Kee, SYK, Ng, WF, Gopalakrishnakone, R. 1999. Determination of Trichothecene Toxin (T2 Mycotoxin) in Aqueous Sample with Solid Phase Microextraction Technique Followed by Gas Chromatography with Flame Ionization Detection. J.High Res.Chrom. 122: 424-426.

382. 	Hewetson, DW, Mirocha, CJ. 1987. Development of Mass Spectra Library of Trichothecenes Based on Positive Chemical Ionization Mass Spectra. J.AOAC. 70: 647-653.

383. 	Krishnamurthy, T, Sarver, WE. 1987. Detection and Quantification of Picogram Amounts of Macrocyclic Trichothecenes in Brazilian Baccharis Plants by Direct Chemical Ionization Tandem Mass Spectrometry. Analytical Chemistry 59: 1272-1278.

384. 	Konstiainen, R, Rizzo, A. 1988. The Characterization of Trichothecenes as their Hepatfluorobutyrate esters by negative-ion chemical ionization tandem mass spectrometry. Analytica Chimica Acta 204: 233-246.

385. 	Krishnamurthy, T, Sarver, WE. 1986. Mass spectral Investigation on Trichothecene Mycotoxins. III. Synthesis, characterization and application of pentafluoropropionyl and trifluoroacetyl esters of simple trichothecenes. J.Chrom. 355: 253-264.

386. 	Grob, K. 1993. Split and Splitless Injection in Capillary Gas Chromatography.  Hüthig, Heidelberg.

387. 	Frisvad, JC, Thrane, U. 1987. Standardised High-Performance Liquid Chromatography of 182 mycotoxins and other fungal metabolites based on alkylphenone retention indices and UV-VIS spectra (Diode Array Detection). J.Chrom. 404: 195-214.

388. 	Hurst, WJ, Snyder, KP, Martin, JrRA. 1987. High-Performance Liquid chromatographic determination of the mycotoxins Patulin, Penicillic acid, Zearalenone and Sterigmatocystin in artificially contaminated cocoa beans. J.Chrom. 392: 389-396.

389. 	Frisvad, JC, Thrane U. 1993. Liquid chromatography of mycotoxins. In Betina V. (ed.), Chromatography of mycotoxins: Techniques and applications. Journal of Chromatography Library. p. 253-372. Elsevier, Amsterdam.

390. 	1996. Criteria of analytical methods for mycotoxins. European Committee for standardization,

391. 	Smedsgaard, J. 1997. Micro-scale extraction procedure for standardized screening of fungal metabolite production in cultures. J.Chrom.A 760: 264-270.

392. 	Aschroft, AE. 1997. Ionization methods in organic mass spectrometry.  The Royal Society Chemistry, Cambridge.

393. 	Jørgensen, K, Vahl, M. 1999. Analysis of ochratoxin A in pig kidney and rye flour using liquid chromatography tandem mass spectrometry (LC/MS/MS). Food Addit.Contam 16: 451-456.

394. 	Josephs, J. 1996. Detection and characterization of fumonisin mycotoxins by liquid chromatography electrospray ionization using ion trap and triple quadrupole mass spectrometry. Rapid communications in mass spectrometry 10: 1333-1344.

395. 	Wheat, TE, Lilley, KA, Banks, JF. 1997. Capillary electrophoresis with electrospray mass spectrometry detection for low molecular-mass compounds. J.Chrom.A 781: 99-105.

396. 	Berger, U, Oehme, M, Kuhn, F. 1999. Quantitative determination and structure elucidation of type A- and B-trichothecenes by HPLC/ion trap multiple mass spectrometry. J Agr.Food Chem. 47: 4240-4245.

397. 	Rosenberg, E, Krska, R, Wissiack, R, Kmetov, V, Josephs, R, Razzazi, E, Grasserbauer, M. 1998. High-Performance liquid chromatography-atmospheric-pressure chemical ionization mass spectrometry as a new tool for the determination of the mycotoxin zearalenone in foof and feed. J.Chrom.A 819: 277-288.

398. 	Scudamore, KA, Hetmanski, MT, Clarke, PA, Barnes, KA, Startin, JR. 1996. Analytical methods for the determination of sterigmatocystin in cheese bread and corn products using HPLC with atmospheric pressure ionisation mass spectrometric detection. Food addit.contam. 13: 343-358.

399. 	Shepard, GS. 1998. Chromatographic determination of the fumonisin mycotoxins. J.Chrom.A 815: 31-39.

400. 	Sewram, V, Nieuwoudt, TW, Marasas, WFO, Shephard, CS, Ritieni, A. 1999. Determination of Fusarium mycotoxins, fusaproliferin and beauvericin by high-performance liquid chromatography-electrospray ionization mass spectrometry. J.Chrom.A 858: 175-185.

401. 	Sewram, V, Nieuwoudt, TW, Marasas, WFO, Shephard, CS, Ritieni, A. 1999. Determination of the mycotoxin moniliformin in cultures of Fusarium subglutinans and in naturally contaminated maize by high-performance liquid chromatography - atmospheric pressure chemical ionization mass spectrometry. J.Chrom.A 848: 185-191.

402. 	McComb, ME, Krutchinsky, AN, Ens, W, Standing, KG, Perreault, H. 1998. Sensitive high-resolution analysis of biological molecules by capillary zone electrophoresis coupled with reflecting time-of-flight mass spectrometry. J.Chrom.A 800: 1-11.

403. 	Tomlinson, AJ, Benson, LM, Braddock, WD, Oda, RP. 1994. On-line preconcentration-capillary electrophoresis-mass spectrometry (PC-CE-MS). Journal of High Resolution Chromatography 17: 729-731.

404. 	Nielsen, MS, Nielsen, PV, Frisvad, JC. 1996. Micellar electrokinitic capillary chromatography of fungal metabolites resolution optimized by experimental design. J.Chrom.A 721: 337-344.

405. 	Naylor, S, Tomlinson, AJ. 1998. Membrane preconcentation-capillary electrophoresis tandem mass spectrometry (mPC-CE-MS/MS) in the sequence analysis of biologically derived peptides. Talanta 45: 603-612.

406. 	Corneli, S, Maragos, CM. 1994. Capillary electrophoresis with laser-induced fluorescence: Method for the mycotoxin ochratoxin A. J Agr.Food Chem. 3162-3165.

407. 	Maragos, CM, Greer, JI. 1997. Analysis of Aflatoxin B1 in Corn Using Capillary Electrophoresis with Laser-Induced Fluorescence Detection. J Agr.Food Chem. 45: 4337-4341.

408. 	Park, JJ, Chu, FS. 1996. Assessment of Immunochemical Methods for the Analysis of Trichothecene Mycotoxins in Naturally Occurring Moldy Corn. J AOAC Int. 79: 465

409. 	Pestka, JJ, Abouzied, MN, Sutikno. 1995. Immunological assays for mycotoxin detection. Food Technol. 120-128.

410. 	Chu, FS. 1986. Immunochemical methods for diagnosis of mycotoxicosis. In Richard JL, Thurston JR. (eds.), p. 163-178. Kluwer, Dordrecht.

411. 	Visconti, A, Pascale, M. 1998. Determination of zearalenone in corn by means of immunoaffinity clean-up and high-performance liquid chromatography with fluorescence detection. J.Chrom.A 815: 133-140.

412. 	Usleber, E, Märtlbauer, E, Dietrich, R, Terplan, G. 1991. Direct enzym-linked immunosorbent assay for the detection of the detection of the 8-ketotrichothecene mycotoxins deoxynivalenol, 3-acetyldeoxynivaleol, and 15-acetyldeoxynivaleol in buffer solutions. J Agr.Food Chem. 39: 2091-2095.

413. 	Usleber, E, Schneider, E, Märtlbauer, E, Terplan, G. 1993. Two formats of enzyme immunoassay for 15-acetyldeoxynivaleol applied to wheat. J Agr.Food Chem. 41: 2019-2023.

414. 	Collin, R, Schneider, E, Briggs, L, Towers, N. 1998. Development of immunodiagnostic field tests for the detection of the mycotoxin, sporidesmin A. Food And Agricultural Immunology 10: 91-104.

415. 	Hack, R, Märtlbauer, E, Terplan, G. 1988. Production and characterization of monoclonal antibodies to the macrocyclic trichothecene roridin A. Appl.Env.Microb. 54: 2328-2330.

416. 	Dietrich, R, Johanning, E, Gareis, M, Schneider, E, Usleber, E, Märtlbauer, E. 1999. Immunochemical detection of mycotoxins associated with Stachybotrytoxicosis. In Johanning E (Ed.), Eastern New York Occupational & Environmental Health Center, New York,  p. 482-491.

417. 	Märtlbauer, E, Gareis, M, Terplan, G. 1988. Enzyme Immunoassay for the Macrocyclic Trichothecene Roridin A: Production, Properties, and Use of Rabbit Antibodies. Appl.Env.Microb. 54: 225-230.

418. 	Bodon, L, Palyusik, M. 1970. Cytotoxicity of toxic extracts from the fungus Stachybotrys alternans. Acta.Vet.Acad.Sci.Hung. 20: 289-294.

419. 	Langseth, W, Bernhoft, A, Rundberget, T, Kosiak, B, Gareis, M. 1999. Mycotoxin production and cytotoxicity of Fusarium strains isolated from Norwegian cereals. Mycopath. 144: 103-113.

420. 	Mosmann, T. 1983. Rapid colorimetric assay for cellular growth and survival: application to proliferation and cytotoxicity assay. J.Immunol.Methods 65: 55

421. 	Saraf, A, Larsson, L, Larsson, B-M, Larsson, K, Palmberg, L. 1999. House dust induces IL-6 and IL-8 response in A549 epithelial cells. Indoor Air 9: 219-225.

422. 	Anderson, MA, Mikkola, R, Kroppensted, RM, Rainey, FA, Peltola, J. 1998. The mitochondrial toxin produced by Streptomyces griseum strains isolated from an indoor environment is valinomycin. Appl.Env.Microb. 64: 4767-4773.

423. 	Mikkola, R, Anderson, JM, Peltola, J, Saris, N-E, Grigoriev, P, Salkinoja-Salonen, M. 1999. Purification and properties of toxins isolated from Streptomyces griseus and Bacillus cereus found in construction materials of buildings. Proceedings of the 8th International Conference on Indoor Air Quality and Climate, Indoor Air `99,   p. 1110-1111.

424. 	Peltola, J, Andersson, M, Haatela, T, Mussalo-Rauhamaa, H, Salkinoja-Salonen, M. 1999. Toxigenic indoor Actinimyceres and fungi case study. The 8th International Conference on Indoor Air Quality and Climate,   p. 560-561.

425. 	Piecková, E, Jesenská, Z. 1995. The Effect of Chloroform-Extractable Secondary Metabolites of Filamentous Fungi on the Movement of Respiratory Tract Cilia from One-Day- Old Chicks in vitro. Folia Microbiologica 40: 123-127.

426. 	Brown, RF, Wildman, JD. 1968. Temperature-Dose Relationship with Aflatoxin on the Brine Shrimp  Arthemia salina. J.AOAC. 51: 905-906.

427. 	Engler, KH, Coker, R, Evans, IH. 1994. A novel colorimetric yeast bioassay for detecting trichothecene mycotoxins. J.Microbiol.Meth. 207-218.

428. 	Hinkley, SF, Jarvis BB. 2000. Chromatographic method for Stachybotrys toxins. In Pohland A, Trucksess MW. (eds.), Methods Molecular Biology. 157. Mycotoxin Protocols. p. 173-194. Humana Press, Totowa.

429. 	Black, RM, Clarke, RJ, Read, RW. 1987. Detection of trace levels of trichothecene mycotoxins in environmental residue and foodstuffs using gas chromatography with mass spectrometric or electron-capture detection. J.Chrom. 388: 365-378.

430. 	Jarvis, BB. 1992. Macrocyclic trichothecenes from Brazilian Baccharis species: from microanalysis to large-scale isolation. Phytochem.Anal. 3: 241-249.

431. 	Palmgren, U, Ström, G, Malmberg, P, Blomquist, G. 1986. The Nucleopore Method: a technique for enumaration of viable and non viable airborne microorganisms. Am J Ind.Med. 10: 325-327.

432. 	Sorenson, WG. 1990. Mycotoxins as potential occupational hazards. Developments Industrial Microbiol. 31: 205-211.

433. 	Smoragiewicz, W, Cossette, B, Boutard, A, Krzystyniak, K. 1993. Trichothecene mycotoxins in the dust ventilation system in office buildings. Int.Arch.Occup.Health 65: 113-117.

434. 	Smoragiewicz, W, Cossette B, Boutard A, Krzystyniak K. 1993. Trichothecene mycotoxins in the dust ventilation system in office buildings. CSCE-ASCE National conference on environmental engineering. p. 9-16. CSCE-ASCE, Montreal.

435. 	Anonymous. 1990. Fungal Resistance of panel Products made of or containing materials of organic origin, Part 3. British Standard 1982.

436. 	Grove, JF. 1988. Non-macrocyclic trichothecenes. Nat.Prod.Rep. 5: 187-209.

437. 	Larsen, FO, Clementsen, P, Hansen, M, Maltbæk, N, Gravesen, S, Skov, P, Norn, S. 1996. The microfungi Trichoderma viride potentiates histamine release from human bronchoalveloar cells. APMIS 104: 673-679.

438. 	Ayer, WA, Miao, S. 1993. Secondary metabolites of the aspen fungus Stachybotrys cylindrospora. Can.J.Chem. 71: 487-493.

439. 	El-Maghraby, OMO, Bean, GA, Jarvis, BB, Aboul-Nasr, MB. 1991. Macrocyclic trichothecenes produced by Stachybotrys isolated from Egypt and Eastern Europe. Mycopath. 113: 109-115.

440. 	Shinohara, C, Hasumi, K, Hatsumi, W, Endo, A. 1996. Staplabin, a novel fungal triprenyl phenol which stimulates the binding of plasminogen to fibrin and U937 cells. J.Antib. 49: 961-966.

441. 	Orii, Y, Kawamura, Y, Mizobe, F, Sakai, N, Hanada, K.1994.Extraction of nerve growth factor enhancer from cultured Stachybotrys parvispora F-4708. Application: JP  93-27093  19930217.

442. 	Nozawa, Y, Yamamoto, K, Ito, M, Sakai, N, Mizoue, K, Mizobe, F, Hanada, K. 1997. Stachybotrin C and parvisporin, novel neuritogenic compounds .1. Taxonomy, isolation, physico-chemical and biological properties. J.Antib. 50: 635-640.

443. 	Rao, CY, Burge, HA, Brain, JD. 2000. The time course of response to intratracheally instilled toxic Stachybotrys chartarum spores in rats. Mycopath. 149: 27-34.

444. 	Caserett and Doull's Toxicology. The basic Science of Poisons1996. In. Klaassen CD(ed.). McGraw-Hill, New York.

445. 	Dhar, AK, Bose, SK. 1968. Studies on versicolin, a new antifungal antibiotic from Aspergillus versicolor.  II.  Isolation and purification. Appl.Microbiol 16: 749-752.

446. 	Dhar, AK, Bose, SK. 1969. Studies on versicolin, a new antifungal antibiotic from Aspergillus versicolor. Tetrahedron Lett. 55: 4871-4874.

447. 	Rickards, RW. 1971. Structure of the antifungal antibiotic versicolin. J.Antib. 24: 715-716.

448. 	Anonymous. 1999. Aflatoxins in corn and peanut butter. AOAC official method 990.33. In Cunniff P. (ed.), Official methods of analysis of AOAC international.  AOAC International, Gaithersburg.

449. 	Malmstrøm, J, Christophersen, C, Frisvad, JC. 2000. Secondary metabolites characteristic of Penicillium citrinum, Penicillium steckii and related species. Phytochem 54: 301-309.

450. 	Enk, M. 1996. Chemotaxonomy of Eurotium. M.Sc. Project, Department of Biotechnology, Technical University of Denmark (In Danish).

451. 	Malmstrøm, J. 2000. Marine fungal chemistry. Ph.D. Thesis. The Marine Chemistry section. University of Copenhagen, Denmark.

452. 	Hass, U, Lund, SP, Simonsen, L, Fries, AS. 1995. Effects of prenatal exposure to xylene on postnatal development behavior in rats. Neurotoxicology and Teratology 17: 341-349.